## Slide 1: COAT Test Analysis of TMC 1005-5
Elisa Santos, Jim Gutzwiller and David Brass
May 17, 2021

## Slide 2: Testing of TMC 1005-5
Lab A
10.1% at 27 hours
12.2% at 50 hours
11.6% at 41 hours
Lab B
12.2% at 37 hrs
11.9% at 50 hours
9.95% at 21 hours
9.40% at 38 hours
Lab G
There is concern about the drop in aeration in the middle of these tests
These tests did not have enough time to establish stable aeration values
Unknown cause of air being evacuated from oil needs to be investigated
11.51% at
50 hours
12.7% at
50 hours
11% at
50 hours

## Slide 3: Effect of Dip in Aeration Value – Lab A
11.6% at 41 hours
12.2% at 50 hours
10.1% at 27 hours
AAVE4050 = 11.81%
A continued flat line after 30 hours would correspond to a final aeration value closer to 12.6% (consider a lower bound if we assume that aeration is still rising at 30 hrs.)
AAVE4050 = 12%
Aeration level is still rising through end of test
12.2% at 50 hours
12.6% at 29 hours

## Slide 4: Effect of Dip in Aeration Value – Lab B
12.2% at 40 hrs. and it goes down
Inflection around 9 hrs.
11.51 % at
50 hours
11.9 % at
50 hours
AAVE4050 = 11.49%
Inflection points in middle of tests are atypical, what impact is this having on the final aeration?
AAVE4050 = 11.97%
If aeration level remained flat after 40 hours the final value would have been 12.2%. At 40 hours there was still a rise in aeration

## Slide 5: Effect of Dip in Aeration Value – Lab G
9.95% at 21 hours
12.7% at
50 hours
9.40% at 38 hours
11% at
50 hours
AAVE4050 = 10.31%
Sharp sloped rise during the last 12 hours of the test
AAVE4050 = 12.64%
Aeration level is still rising slowly through end of test

## Slide 6
Lab G
Lab A
Recent Test Results of 832-1 and 833-1
Aeration plot shapes appear to be similar within a lab for both reference oils
Large deviations in aeration were not noticed in these tests.
832-1
833-1
832-1
833-1

## Slide 7: Reference Oils 832-1 and 833-1: Trend over time by Lab, limited data, new MM only
Lab B (3Q 2020):
Fresh Oil Stirring rules implemented as a result
Discrimination between reference oils: OK
The two high tests results from Lab B led to the adoption of rules for stirring fresh oils (10/29/2020 SP meeting)
10.23%
11.94%

## Slide 8
Connecting EOAT and COAT: Plot below shows Aeration % by test type, Oil and Lab
EOAT 1005-5 results as expected
COAT 1005-5 test aeration profiles show dips and at EOT aeration clearly still rising.
Lab G results highlighted below. 1005-5 test results differ by ~ 8 std deviations
Discrimination between 832-1 and 833-1: OK
Two high tests led to change in stirring rules
12.1%
9.9%
Discrimination between 832-1 and 833-1: OK
Old MM
New MM

## Slide 9: 1005-5 aeration profiles Operational Data (1005-5): selected correlations

## Slide 10: Gallery Pressure
Lab A
Lab G
Lab B
1005-5 Aeration profile is on the top panel and Gallery Pressure is on the lower panel
Aeration
Gallery
Pressure

## Slide 11: MicroPumpCont% Output
1005-5 Aeration profile is on the top panel and MicroPumpCont % Output is on the lower panel
Lab A
Lab B
Lab G

## Slide 12: IVA Oil Press kPag
Lab A
Lab B
Lab G
1005-5 Aeration profile is on the top panel and IVA Oil Press kPag is on the lower panel

## Slide 13: MM_OilP Target V
Lab G 144699
Lab G 158051
Lab B 158054 and 158055
1005-5 Aeration profile is on the top panel and MM_OilP Target V is on the lower panel

## Slide 14: MMD Temp C
Lab G 144699
Lab G 158051
Lab A 144700
Lab A 158053
1005-5 Aeration profile is on the top panel and MMD Temp C is on the lower panel
Lab B 158054 and 158055

## Slide 15
T5_MM Inlet TC C
T6_MM Outlet TC C
Lab B
Lab B
1005-5 Aeration profile is on the top panel and T5 and T6 is on the lower panel

## Slide 16
T6_MM Outlet TC C
Lab A
T5_MM Inlet TC C
Lab A
1005-5 Aeration profile is on the top panel and T5 and T6 is on the lower panel

## Slide 17
T6_MM Outlet TC C
Lab G
T5_MM Inlet TC C
Lab G
1005-5 Aeration profile is on the top panel and T5 and T6 is on the lower panel

## Slide 18
Lab G PressController % Output

## Slide 19
Lab A PressController % Output

## Slide 20
Lab B PressController % Output

## Slide 21
Lab A Oil Pre Filter_Pres kPag
Lab B
Lab G

## Slide 22
Lab A
Lab G
Lab B

## Slide 24: 1- Old MM Data

## Slide 25: 40 to 50 hr. Aeration % by Oil and Lab: ordered from highest to lowest oil mean
COAT controlled to a target pressure
Data before New MM

## Slide 26
Data from OLD MM
1005 Aeration Profile by Lab based on old MM