## Slide 1: DD13 Scuffing Test TEI Data Review Ring Batch Comparison
Kevin O’Malley
The Lubrizol Corporation
December 2016

## Slide 2: Summary
Kit measurements from 11 reference oil tests using B Batch Top Rings are compared to the measurements observed in prior reference tests (12 matrix tests + 3 post-matrix)
Largest Differences:
  Test using B Batch Top Rings generally have
    larger ring gap & face peak height location measurements
    smaller face width, Rk, Rpk, and back of ring width measurements
Other Observed Differences:
Top Ring:
  Test using B Batch Top Rings generally have
    higher 180° ring thickness, and 1” after the gap face peak height to 0.2mm diff measurements
    smaller Ra and Rz measurements
The tests using B batch Top Rings tend to also have lower 2nd Ring and Oil Ring ring tension as well as lower Oil Ring 180° from gap rail height differential measurements
Percent Scuffing tends to be higher when the top ring face peak height to 2.75mm diff is lower.

## Slide 3: Top Ring Differences Ring Gap
B Rings generally have larger top ring gap measurements than observed on prior rings

## Slide 4: Top Ring Differences Face Width
B Rings have lower face width measurements than observed on prior rings
Note: A 120065 180 degree result close to zero is not plotted

## Slide 5: Top Ring Differences Face Peak Height Location
B Rings tend to have face peak height location measurements on the upper end of what was observed on prior rings

## Slide 6: Top Ring Differences Face Peak Height to 0.2mm Diff
B Ring 1” after the gap face peak height to 0.2 mm diff measurements are on upper end of measurements observed on prior rings

## Slide 7: Top Ring Differences Ra
B Ring Ra 180 degrees from gap measurements tend to be on the lower end of measurements observed on prior rings

## Slide 8: Top Ring Differences Rk
B Ring Rk measurements are generally lower than those observed on prior rings

## Slide 9: Top Ring Differences Rpk
B Ring Rpk measurements are generally lower than those observed on prior rings

## Slide 10: Top Ring Differences Rz
B Ring Rz measurements tend to be on the lower end of what was observed on prior rings

## Slide 11: Top Ring Differences Back of Ring Width
B Rings generally have lower back of ring width measurements than the prior rings

## Slide 12: Top Ring Differences Ring Thickness
B Rings generally have higher 180 degree ring thickness measurements than the prior rings

## Slide 13: Second Ring Differences Ring Tension @ 132 mm
B Rings tend to have lower ring tension measurements than the prior rings

## Slide 14: Oil Ring Differences
B Rings tend to have lower ring tension & 180° from gap rail height differential measurements compared to the prior rings

## Slide 15: Percent Scuffing by Cylinder
Percent Scuffing tends to be higher when the top ring face peak height to 2.75mm diff is lower

## Slide 16
Appendix
TEI Measurements