# Mack Surveillance Panel Report

Report to B

Automotive Lubricants

## June 18, 2003

Prepared By

Wim van Dam, Chairman Mack Surveillance Panel

Mack T-6/T-7/T-8/T-9/T-10 Surveillance Panel

June 18, 2003

Table of Contents

1.	Scope and Objectives

2. 	Membership

3.	Previous Meetings

4.	Activity Reports

5. 	B0.02 Action Items

#### MACK TEST SURVEILLANCE PANEL

April 21, 2003

SCOPE AND OBJECTIVES

SCOPE

The Mack Test Surveillance Panel is responsible for the Mack T-6, T-7, T-8A, T-8, T-8E, T-9, T-10, and T-10A tests procedures.  The Panel works with the ASTM Test Monitoring Center to monitor test operations, test statistics, test severity and test precision. The Mack T-6 and T-7 tests are no longer monitored by the TMC. The overall improvements in the test operation and test monitoring are accomplished with the cooperation of the test developer, the Test Monitoring Center and ASTM Subcommittee B0.02.

##### OBJECTIVES______							__________

- Develop an ASTM engine test method for the evaluation of a lubricant’s capability to control soot related viscosity increase, using Mack 2002 generation engine hardware. This engine test is intended to be included in Mack’s 2003 OEM specification for Heavy Duty Diesel Engine Oils and in the 2007 PC-10 specification.

- Develop an ASTM engine test method for the evaluation of a lubricant’s capability to control piston ring and liner wear, using  Mack post 2003 engine hardware. This engine test is intended to be included in the 2007 PC-10 specification for Heavy Duty Diesel Engine Oils.

- Evaluate any correlations between the different generations of engine tests measuring the same parameter(s), to support a possible replacement of older tests.

- Evaluate alternative viscosity measurement methods for use with engine tests in future categories.

# Mack Surveillance Panel

Membership

Ron Buck					Test Engineering

Bob Campbell				Ethyl

Jeff Clark					TMC

Mark Cooper 				Chevron Oronite

Pat Fetterman				Infineum

Ken Goshorn				Mack

Jim Gutzweiller				Infineum

Ricardo Conti				ExxonMobil

Aimin Huang				Equilon

Jim Matasic					Lubrizol

Jim Moritz					Perkin Elmer

Charles Passut 				Ethyl

Dick Patrick					Citgo

Scott Richards				SwRI

Bill Runkle					Valvoline

Jim Rutherford				Chevron Oronite

Greg Shank					Mack

Hap Thompson				Facilitator

Wim van Dam				Chevron Oronite

Jim Wells					SwRI

Mack T-6/T-7/T-8/T-9/T-10 Surveillance Panel

Previous Meetings

- May 7, 2003 Teleconference

- April 21, 2003 San Antonio, TX

- February 13, 2003 Hagerstown, MD

- January 21, 2003 Teleconference

- November 26, 2002 Teleconference

- September 24, 2002 San Antonio, TX

- July 22, 2002 Teleconference

- June 17, 2002 Montreal, Canada

- December 5, 2001 Miami, FL

### Activity Reports

T-6/T-7 Information Letters:

No longer Monitored.

T-8 Information Letters and Reports :

A report was issued on April 4, 2003 (Memorandum 03-024), showing that 5 stands are calibrated. Over the reporting period 6 reference oil tests were run, 4 were operationally and statistically acceptable tests, one test was Operationally Invalid and one test was aborted. The test parameters, VI38, RV48, and RV2 (Relative Viscosity at 4.8% TGA soot, 100 % Din Shear Viscosity) are in control.

No Information Letters were issued this reporting period.

Previous Information Letters:

- Information Letter 02-1 was issued on September 27, 2002. Topics included the addition of 100% Din Shear Loss relative viscosity, the removal of report forms and data dictionary, revised precision and bias sections, and safety precautions.

- Information Letter 98-1 was issued January 26, 1998.  This information letter modified D-5967 to incorporate the extended length test, T-8E, into the T-8 method.  The information letter also revised the report form and the data dictionary.

- Information Letter 98-2 was issued June 26, 1998.  This information letter revised the low sulfur diesel fuel specification, the calculation method for viscosity increase at 3.8% soot, the oil sampling frequency and report forms and data dictionary.

- Information letter 98-3 was issued on August 24, 1998.  This information letter gave the shear test method number change, the fuel system revision schematics, viscosity measurement procedure revision and changes to the report forms and data dictionary.  A correction to the data dictionary was issued on September 8, 1998.

- Information letter 98-4 was issued December 11, 1998.  This information letter updated the critical parts list.

- Information letter 98-5 was issued in December 11, 1998 to define the Mack T-8A  in D 5967.

- Information Letter 97-1 Revised report forms and data dictionary.

- Contained two errors regarding test length and reference period.  Not all tests are running the 300 hour test length proposed for PC-7. The  surveillance panel voted to increase only reference test length to 300 hours.   Candidate TESTING MAY BE EITHER 250 OR 300 HOURS.  To help RSI the 300-hour test will be called the T-8E.

- The last T-8 Information letter in 1996,  96-1,  was issued June 28, 1996

-Oil consumption calculation correction.

-TMC address change

-Alpha numeric fields added to the Data Dictionary

Mack T-9 Information Letters and Reports:

A memorandum (03-020) was issued on April 2, 2003, indicating that there has been no reference test activity during the reporting period. A summary with the most recent reference test activity was issued on October 1, 2002 (Memorandum 02-072), stating that two operationally and statistically valid reference tests have been run over the reporting period. The average liner wear shows a slight trend in the severe direction, while top ring weight loss and delta Pb are trending mild.

No information letters were issued during this reporting period.

Previous Information Letters:

1) Information Letter 99-1 was issued February 19, 1999.  This Information Letter contains Draft No. 7 of the test procedure.

2)Information Letter 98-1 was issued June 26, 1998 with a revision on July 2, 1998.  Procedure changes were issued for the test cell fuel system, extension of calibration periods, outlier and flaked top ring screening, part numbers, and report forms and data dictionary.

3)Information Letter 98-2 was issued on Sept. 21, 1998. Test procedure changes were issued for: coolant additives, TBN/TAN measurements, viscosity measurement, part numbers, lead adjustment for outlier bearings, report forms and data dictionary.

T-10/T-10A Information Letters and Reports :

A report was issued on April 10, 2003 (Memorandum 03-034), showing that 4 operationally and statistically acceptable reference tests and one industry donated test were run during the reporting period. Delta Pb 0-300, Delta Pb 250-300, CWL, TRWL, and OC are considered in control. The MRV measurement in the T-10A test is in a severe warning alarm in the severe direction.

An Information Letter (03-1) was issued on February 14, 2003. Topics included oil pump, thrust washers, and connecting rod bearing part numbers.

Previous Information Letters:

- Information Letter 02-2 was issued on September 27, 2002. Topics include injector opening pressure, engine calibration requirements, MRV measurement, and sample handling.

- Information Letter 02-1 was issued on April 19, 2002.  This Information Letter specifies that engine calibration requirements have been dropped; calibration is determined by stand only. MRV viscosity is to be measured using the modified method only with sample handling as described in the T-8 procedure. It also mentions the issuing of Draft No. 6 of the test procedure and has the new and modified sections of the test attached.

### Action Items for B.02

The Surveillance Panel has no action items for B.02.