Surface Analysis of MACK T-10 Bearings

Doug Jayne

Lubrizol

2-27-2004

Lubrizol Confidential

Table I

| Element | New Bearing Light Spot |  | PE Near Crush |  | LZ Near Crush |  | SWRI Near Crush |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Surface | 10nm Below Surface | Surface | 10nm Below Surface | Surface | 10nm Below Surface | Surface | 10nm Below Surface |
| Carbon | 57 | 2.3 | 60 | 19 | 64 | 28 | 54 | 2.6 |
| Oxygen | 28 | 12 | 23 | 35 | 19 | 11 | 29 | 19 |
| Tin | 5.1 | 6.6 | 1.6 | 12 | 2.7 | 9.0 | 6.2 | 17 |
| Lead | 5.4 | 77 | 2.1 | 20 | 4.2 | 45 | 3.7 | 61 |
| Chlorine | - | - | - | - | - | - | 0.8 | - |
| Copper | - | - | - | - | - | 1.0 | 0.3 | - |
| Zinc | 1.3 | - | 0.4 | 1.0 | 0.1 | - | 0.3 | - |
| Phosphorus | - | - | - | 2.3 | - | - | 1.0 | - |
| Calcium | 0.6 | 2.9 | 3.8 | 5.4 | 2.7 | 2.2 | 0.7 | - |
| Sulfur | - | - | 3.0 | - | - | - | 0.8 | - |
| Fluorine | 1.3 | - | 4.2 | 4.9 | 4.1 | 3.7 | - | - |
| Nitrogen | 1.7 | - | 2.0 | - | 2.8 | - | 3.1 | - |

Table 2

| Element | New Bearing |  |
| --- | --- | --- |
|  | Surface Light Area | Surface Dark Area |
| Carbon | 61 | 55 |
| Oxygen | 26 | 28 |
| Tin | 4.5 | 3.1 |
| Lead | 6.8 | 10 |
| Fluorine | 2.1 | 3.0 |
| Nitrogen | - | 1.5 |