## Slide 1: Potential Replacement for T11 Reference Oil 820-3
May 2, 2012

## Slide 2: Background
Reference Oil 820-3 supply low
  TMC Inventory is ~55 gallons
  No more shipments from TMC at this time
Supplier of 820-3 has proposed replacement
  New oil is CJ-4 vs CI-4
  Both use Group II base oil
  New oil is low SAP vs high SAP content of 820-3

## Slide 3: Initial Test Results

## Slide 4: Test Result Plots: Critical Parameter
Chart: Candidate Results vs. LTMS Window Soot @ 12 cSt
| LTMS Window | LTMS History | Candidate
Soot @ 12 cSt | 5.92
Soot @ 12 cSt | 6.12
Min | 5.69
Mean | 6.1
Max | 6.7

## Slide 5
Test Result Plots: Noncritical Parameter
Chart: Candidate Results vs. LTMS Window Soot @ 4 cSt
| LTMS Window | LTMS History | Candidate
Soot @ 4 cSt | 3.95
Soot @ 4 cSt | 3.89
Min | 3.68
Mean | 3.97
Max | 4.49

## Slide 6
Test Result Plots: Noncritical Parameter
Chart: Candidate Results vs. LTMS Window Soot @ 15 cSt
| LTMS Window | LTMS History | Candidate
Soot @ 15 cSt | 6.51
Soot @ 15 cSt | 6.65
Min | 6.21
Mean | 6.67
Max | 7.05

## Slide 7
Test Result Plots: Noncritical Parameter
Chart: Candidate Results vs. LTMS Window 180 Hr MRV
| LTMS Window | LTMS History | Candidate
Corrected 180 Hr MRV @ -20C | 14981
Corrected 180 Hr MRV @ -20C | 16422
Min | 13256
Mean | 14523
Max | 16056

## Slide 8
Chart: Proposed T11 Reference Oil Soot Performance
| 0 | 12 | 24 | 36 | 48 | 60 | 72 | 84 | 96 | 108 | 120 | 132 | 144 | 156 | 168 | 180 | 192 | 204 | 216 | 228 | 240 | 252
Soot Window Min | 0 | 0.3125 | 0.625 | 0.9375 | 1.25 | 1.5625 | 1.875 | 2.1875 | 2.5 | 2.8312 | 3.1625 | 3.4937 | 3.825 | 4.1562 | 4.4875 | 4.8187 | 5.15 | 5.464 | 5.778 | 6.092 | 6.406 | 6.72
Soot Window Max | 0 | 0.375 | 0.75 | 1.125 | 1.5 | 1.875 | 2.25 | 2.625 | 3 | 3.3562 | 3.7125 | 4.0688 | 4.425 | 4.7813 | 5.1375 | 5.4938 | 5.85 | 6.224 | 6.598 | 6.972 | 7.346 | 7.72
Measured Soot | 0.11 | 0.56 | 0.87 | 1.21 | 1.61 | 1.84 | 2.32 | 2.58 | 2.9 | 3.16 | 3.73 | 4.09 | 4.46 | 4.93 | 5.19 | 5.54 | 5.8 | 5.95 | 6.19 | 6.47 | 6.71 | 6.94