Standard Test Method for

Evaluation of Automotive Engine Oils in the Sequence IVB Spark-Ignition Engine1

This standard is issued under the fixed designation D6891; the number immediately following the designation indicates the year of original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A superscript epsilon (ε) indicates an editorial change since the last revision or reapproval.

INTRODUCTION

Portions of this test method are written for use by laboratories that make use of ASTM Test Monitoring Center (TMC)2 services (see Annex A1).

The TMC provides reference oils and engineering and statistical services to laboratories that desire to produce test results that are statistically similar to those produced by laboratories previously calibrated by the TMC.

In general, the Test Purchaser decides if a calibrated test stand is to be used. Organizations such as the American Chemistry Council require that a laboratory utilize the TMC services as part of their test registration process. In addition, the American Petroleum Institute and the Gear Lubricant Review Committee of the Lubricant Review Institute (SAE International) require that a laboratory use the TMC services in seeking qualification of oils against their specifications.

The advantage of using the TMC services to calibrate test stands is that the test laboratory (and hence the Test Purchaser) has an assurance that the test stand was operating at the proper level of test severity. It should also be borne in mind that results obtained in a non-calibrated test stand may not be the same as those obtained in a test stand participating in the ASTM TMC services process.

Laboratories that choose not to use the TMC services may simply disregard these portions.

1.  Scope

1.1 This test method measures the ability of crankcase oil to control valve-train wear for spark-ignition engines at low operating temperature conditions. This test method is designed to simulate extended engine cyclic vehicle operation. The Sequence IVB Test Method uses a Toyota 2NR-FE water cooled, 4 cycle, in-line cylinder, 1.5 liter engine. The primary result is bucket lifter wear. Secondary results include cam lobe nose wear and measurement of iron wear metal concentration in the used engine oil. Other determinations such as fuel dilution of the crankcase oil, non-ferrous wear metal concentrations, total fuel consumption, and total oil consumption, can be useful in the assessment of the validity of the test results.2

1.2  The values stated in SI units are to be regarded as standard. No other units of measurement are included in this standard.

1.2.1  Exceptions—Where there is no direct SI equivalent such as pipe fittings, tubing, NPT screw threads/diameters, or single source equipment specified.

1.3  This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use. See Annex AX for specific safety precautions.

2.  Referenced Documents

2.1  ASTM Standards:3

D235  Specification for Mineral Spirits (Petroleum Spirits) (Hydrocarbon Dry Cleaning Solvent)

D287  Test Method for API Gravity of Crude Petroleum and Petroleum Products (Hydrometer Method)

D323  Test Method for Vapor Pressure of Petroleum Products (Reid Method)

D381  Test Method for Gum Content in Fuels by Jet Evaporation

D445  Test Method for Kinematic Viscosity of Transparent and Opaque Liquids (and Calculation of Dynamic Viscosity)

D525  Test Method for Oxidation Stability of Gasoline (Induction Period Method)

D664  Test Method for Acid Number of Petroleum Products by Potentiometric Titration

D2622 Test Method for Sulfur in Petroleum Products by Wavelength Dispersive X-ray Fluorescence Spectrometry

D3525  Test Method for Gasoline Diluent in Used Gasoline Engine Oils by Gas Chromatography

D4485  Specification for Performance of Active API Service Category Engine Oils

D4739 Test Method for Base Number of Petroleum Products by Potentiometric Titration

D5185  Test Method for Multielement Determination of Used and Unused Lubricating Oils and Base Oils by Inductively Coupled Plasma Atomic Emission Spectrometry (ICP-AES)

D5844  Test Method for Evaluation of Automotive Engine Oils for Inhibition of Rusting (Sequence IID) (Withdrawn 2003)4

E230  Specification and Temperature-Electromotive Force (EMF) Tables for Standardized Thermocouples

IR 5.8_6.1 Infrared Spectra Oxidation and Nitration Peak Area

2.2  API Standard:

API 1509  Engine Oil Licensing and Certification System5

2.3  SAE Standards:

SAE J183  Engine Oil Performance and Engine Service Classification6

SAE J254  Instrumentation and Techniques for Exhaust Gas Emissions Measurement6

2.4  ASME Standard:

B46.1  Standard for Surface Texture (Surface Roughness, Waviness, and Lay)7

2.5  JASO Standard:

M 328-95  Valve-train Wear Test Procedure for Evaluating Automobile Gasoline Engine Oils8

2.6  CEC Standard:

CEC-L-38-A-94   Peugeot TU-3M/KDX Valve-train Scuffing Wear Test9

3.  Terminology

3.1  Definitions:

3.1.1  blowby, n—that portion of the combustion products and unburned air/fuel mixture that leaks past piston rings into the engine crankcase during operation.

3.1.2  calibration test stand, n—a test stand on which the testing of reference material(s), conducted as specified in the standard, provided acceptable results.Sub. B Glossary10

3.1.2.1  Discussion—In several automotive lubricant standard test methods, the ASTM Test Monitoring Center provides testing guidance and determines acceptability.

3.1.3  reference oil, n—an oil of known performance characteristics, used as a basis for comparison.

3.1.3.1  Discussion—Reference oils are used to calibrate testing facilities, to compare the performance of other oils, or to evaluate other materials (such as seals) that interact with oils.

3.2  Definitions of Terms Specific to This Standard:

3.2.1  break-in, n—initial engine operation to reach stabilization of the engine performance after new parts are installed in the engine.

3.2.2  lifter volume loss, n—the difference between the post-test and pre-test volume of a valve-train bucket lifter as measured by a Keyence VR-3000 or later model 3D macroscope.

3.2.5.1  Discussion—The pass fail criteria is the average intake lifter volume loss, the average volume loss of all intake 8 lifters. The average exhaust lifter volume loss is also calculated.

3.2.4  cam lobe wear, n—the difference between pre-test and post-test measurement of a cam lobe from heel to nose in µm.

3.2.5  golden stand, n—Sequence IVA test stand built in accordance with the ASTM DXXXX Sequence IVA test method by the approved supplier(s).

3.2.5  lifter area loss, n

3.2.5  flushing, n—the installation of a fresh charge of lubricant and oil filter for the purpose of running the engine to reduce and eliminate remnants of the previous oil charge.

3.2.5.1  Discussion—Flushing may be carried out in an iterated process to ensure a more thorough process of reducing previous oil remnants.

3.2.6  reference plane, n—The depth above which volume is calculated for Keyence volume measurements.

3.2.7  lifter crown, n—the maximum difference in height measured along to reference axis of the bucket lifters.

3.2.8  cam lobe failure, n—very severe wear of a lobe surface that makes it impossible to complete a test.

3.2.8.1 Discussion—tests that experience cam lobe failure are considered non-interpretable because the phenomenon does not have a repeatable relationship with test oil.

4.  Summary of Test Method

4.1  Test Numbering Scheme—Use the test numbering scheme shown below:

AAAAA–BBBBB–CCCCC

AAAAA represents the stand number. BBBBB represents the number of tests since the last calibration test on that stand. CCCCC represents the total number of Sequence IVB tests conducted on that stand. For example, 6-10-175 represents the 175th Sequence IVB test conducted on test stand 6 and the tenth test since the last calibration test. Consecutively number all tests. Number the stand calibration tests beginning with zero for the BBBBB field. Multiple-length Sequence IVB tests are multiple runs for test numbering purposes, such as double-length tests which are counted as two runs and triple-length tests which are counted as three runs. For example, if test 1-3-28 is a doubled-length test, number the next test conducted on that stand 1-5-30.

4.2  Test Engine—This procedure uses a Toyota 2NR-FE water cooled, 4 cycle, in-line four cylinder, 1.5 liter engine as the test apparatus. The engine incorporates dual overhead camshafts, four valves per cylinder (2 intake; 2 exhaust), and a direct acting mechanical bucket lifter valve-train design. The critical test parts (camshafts, direct acting mechanical bucket lifters) are replaced prior to each test. A 95 min run-in schedule, followed by a 50 h aging schedule, for Silicon (Si) pacification, is conducted whenever the long block or cylinder head are replaced with new components.

4.3  Test Stand—The complete test stand is available from the Test Engineering Inc. Thermocouples are to be installed by individual test labs at the locations and depths shown in Annex A7.  Mount the engine so that there is a 4.5° incline from the exhaust to the intake side and an angle of 0° from front to back. Control the intake air, provided to the engine air filter housing, for temperature, pressure, and humidity. Control the backpressure of the exhaust leaving the engine.   Install the engine on a test stand equipped with computer control of engine speed, torque, various temperatures, pressures, flows, and other parameters outlined in the test procedure (see Section 11).

4.4  Test Sequence—After an engine run-in and aging schedule, or after the completion of a previous test, install new test camshafts and bucket lifters. Flush the external oil system with solvent and the oil pan with EF-411 using external pumps and connections. Perform four engine flushes, using fresh oil charges for each flush. After completing the fourth flush, drain and weigh the used oil from the 4th flush, and weigh and install the fresh test oil charge. Run the test for a total of 200 h, with no scheduled shutdowns. A single test cycle is composed of two 7-s steady-state stages separated by 8-s transitions. This test cycle (two steady-state stages and two transitions) is repeated 24,000 times.

4.5  Analyses Conducted—At the completion of the test, the camshaft lobes are measured for heel-to-toe wear and the bucket lifters are measured for volume loss and mass  loss.  Use these measurements to determine the summation, average, minimum and maximum wear for the intake and exhaust bucket lifters and the intake and exhaust camshaft lobes. Determine the oil consumption by calculating the difference between the mass of the used drain oil and the mass of the engine’s initial oil charge taking into account oil removed for intermediate oil samples. Analyze the end of test used oil for wear metals, fuel dilution, kinematic viscosity at 40°C, total acid number, total base number, oxidation and nitration by FTIR, and Karl Fischer water content. Retain a final drain sample of 1 L for a minimum of 90 days. Retain the camshafts and bucket lifters for a minimum of 6 months.

5.  Significance and Use

5.1  This test method was developed to evaluate automotive lubricant’s effect on controlling camshaft lobe and bucket lifter wear for overhead camshaft engines with direct acting bucket lifters.

Note 1—This test method may be used for engine oil specifications such as ILSAC GF 6.

6.  Apparatus

6.1  Test Engine—This test method uses a fired 2011 model Toyota 2NR-FE, in-line 4-cylinder, 16 valve, 4-cycle, water-cooled, port fuel-injected gasoline engine with a displacement of 1.496 L.11 ,12 See Annex A6 for a parts lists. Nominal oil sump volume is 3 L. The cylinder block and cylinder head is aluminum. The engine features dual overhead camshafts and direct acting bucket lifters. The engine compression ratio is 10.5 to 1. The engine is rated to 132 N·m of torque at 3000 r/min. The ignition timing and multi-port fuel injection system is electronically controlled by a test-specific ECM.

6.1.1  Engine Buildup and Measurement Area—The ambient atmosphere of the engine buildup and measurement areas shall be reasonably free of contaminants and maintained at a uniform temperature. Maintain the specific humidity at a uniform level to prevent the accumulation of rust on engine parts. Use uniform temperatures background luminous intensity to ensure repeatable dimensional measurements. Use a Keyence macroscope on a base-plate free of external vibrations.

6.1.2  Engine Operating Area—The laboratory ambient atmosphere shall be reasonably free of contaminants and general wind currents, especially if and when the valve-train parts are installed while the engine remains in the operating area. The temperature and humidity level of the operating area is not specified.

6.1.3  Parts Cleaning Area—This test method does not specify the ambient atmosphere of the parts cleaning area (Warning—Use adequate ventilation in areas while using solvents and cleansers).

6.2  External Engine Modifications—Modify the test engine for the valve-train wear test. Install the modified front cover and oil pan from the approved supplier. Install an oil filter adapter at the location of the stock oil filter housing, as shown in Assembly manual section 1. Install fittings for various temperature and pressure measurements as required by the test method. Place the Toyota production valve cover with a specially manufactured aluminum jacketed valve cover. Route the engine coolant through this jacket.

6.3  Test Stand and Laboratory Equipment—This engine-dynamometer test is designed for operation using computer control instrumentation and computer data acquisition. Provide an intake air system for the precise control of engine intake air humidity, temperature, and cleanliness.

6.3.1  Computer Data Acquisition System—The procedure shown in 6.3.1.1 – 6.3.1.3 details the test stand log operational data with a computer data acquisition system using sensor configurations, and is in compliance with Data Acquisition and Control Automation II.10 Consider a test that has greater than 2 h without data acquisition on any controlled parameter to be operationally invalid.

6.3.1.1  Frequency of Logged Data—Log data at 1 Hz during all 4 stages of all test cycles.

6.3.1.2 Resolution of Logged Data—The laboratory provided data acquisition system must provide 32 analog to digital channels that meet the resolution requirements in Table 1.

6.3.1.3  System Time Response for Logged Data—Do not exceed the controlled operational parameters for system time response for measurement shown in Table 2. The system time response includes the total system of sensor, transducer, analog signal attenuation, and computer digital filtering. Use single-pole type filters for attenuation.

TABLE 1 Data Acquisition Resolution Requirements

| Parameter | Units | Required Resolution |
| --- | --- | --- |
| Engine Speed | r/min | 1 |
| Torque | N-m | 1 |
| Air-to-Fuel Ratio | afr | 0.05 |
| All Temperatures Except Exhaust | °C | 0.1 |
| Exhaust Temperature | °C | 1 |
| All Gauge Pressures | kPaG | 0.1 |
| Barometer | KpaA | 0.1 |
| Humidity | g/kg | 0.01 |

TABLE 2 System Time Response

| Parameters | Time Response, max (one time constant) |
| --- | --- |
| Temperatures | 2.8 s |
| Pressures | 1.7 s |
| Coolant Flow | 2.5 s |
| Torque | 2.0 s |
| Speed | 1.8 s |

6.3.1.4  Quality Index—The Quality Index (QI) is an overall statistical measure of the variation from test targets of the steady-state operational controlled parameters. The Sequence IVA Surveillance Panel has chosen the QI upper and lower control limits, shown in Table 3.

| where: |  |  |
| --- | --- | --- |
| Xi | = | values of the parameter measured, |
| U | = | allowable upper limit of X, |
| L | = | allowable lower limit of X, and |
| n | = | number of data points used to calculate QI. |

TABLE 3 QI Control Limits

| Parameter | U | L |
| --- | --- | --- |
| Intake Air Humidity | 12.00 | 11.00 |
| Engine Coolant Out Temperature | 53.5 | 50.5 |
| Exhaust Backpressure * | 107.50 | 101.50 |
| Fuel Rail Temperature | 24.50 | 23.50 |
| Intake Air Pressure | 0.50 | 0.00 |
| Intake Air Temperature | 32.75 | 31.25 |
| Oil Gallery Temperature | 58.00 | 50.00 |
| RAC Coolant Out Temperature | 20.75 | 19.25 |
| Torque | 26.50 | 23.50 |
| Engine Coolant Flow Rate | 80.40 | 79.60 |
| RAC Coolant Flow Rate | 120.75 | 119.25 |
| Blowby Gas Temperature | 29.50 | 28.50 |
| Load Cell Temperature | 49.00 | 41.00 |
| Engine Coolant Pressure | 80.00 | 60.00 |
| Fuel Rail Pressure | 345.00 | 325.00 |

Where missing data or Bad Quality Data (BQD), or both, are encountered, calculate the adjusted Quality Index (QIADJ) using the following equation:

| where: |  |  |
| --- | --- | --- |
| Q | = | QI calculated without missing/BQD, |
| I | = | points, |
| n | = | number of data points used to calculate QI, and |
| N | = | number of data points for a complete data set. |

If the QI calculation of a controlled parameter is less than zero, investigate the reason, assess its impact on test operational validity, and document such finding in the final test report. For calibration tests, review the operational validity assessment with the TMC. Annex A2 describes calibration procedures using the TMC reference oil, including their storage and conditions of use, the conducting of tests and the reporting of results.

6.3.2  Test Stand Configuration—Mount the engine on the test stand similar to its vehicle orientation (0° in front; sideways 4.5° up on intake manifold side). This orientation is important to the return flow of oil in the cylinder head, and ensures reproducible oil levels. Directly couple the engine flywheel to the Midwest MW1014A dynamometer through the approved driveshaft.

6.3.3 Dynamometer Excitation and Throttle Control—A DyneSystems Non-Interlock 5 which is provided as part of the golden stand assembly is the only system permitted to be used for dynamometer excitation and throttle control.

6.3.4 Intake-air Supply System—The intake air supply system shall be capable of delivering at least 1000 L/min (2000 L/min preferred) of conditioned and filtered air to the test engine during the 200 h test, while maintaining the intake-air parameters detailed in Table A.2.

6.3.4.1 Induction Air Humidity—Measure the intake air specific humidity in the main system duct or at the test stand. If using a main system duct dew point temperature reading to calculate the specific humidity, verify the dew point periodically at the test stand. Maintain the duct surface temperature above the dew point temperature at all points downstream of the humidity measurement point to prevent condensation and loss of humidity level.

6.3.4.2 Intake Air Filtering—Use the production intake air cleaner assembly with filter, at the engine. Use a snorkel adapter of that fits over the intake air box inlet to connect the controlled air duct to the air cleaner. Ensure that the top of the air cleaner assembly has been modified for installation of the intake pressure sensor line. Refer to 6.3.4.5 for installation position

6.3.4.3 Intake Air Flow—Do not measure for intake airflow.

6.3.4.4 Intake Air Temperature—For final control of the inlet air temperature, install an electric air heater strip within the air supply duct. The duct material and heater elements design shall not generate corrosion debris that could be ingested by the engine.

6.3.4.5 Intake Air Supply Pressure—Locate the pressure sensing tube on the top cover of the air cleaner 190 mm ± 10 mm from the front (straight edge of the top surface) and 65 mm ± 10 mm from the left (viewed from the front of the box). The tube should have a depth of 25 mm ± 4 mm into the air cleaner.

6.3.5 Fuel Supply System—This test method requires approximately 750 L of unleaded Haltermann KA24E Green test fuel per test (24000 cycles). Use a Motorcraft  E7T2-9C407-BA fuel pump. The fuel conditioning system is part of the golden stand and is detailed in

7.  Reagents and Materials

Note 6—Use 12 L and 2600 g and  of the non-reference test oil sample to perform the 200 h Valve-train Wear test.

7.1  Coolant for Engine and Rocker Arm Cover—Use distilled water mixed with Havoline Extended Life Antifreeze at a 70:30 ratio.

7.2  Fuel—Use Haltermann KA24E Green test fuel for this test method as shown in Annex AX. (Warning—Flammable. Health hazard.) It is dyed green to preclude unintentional contamination with other test fuels. Use approximately 750 L of fuel for each test (24000 cycles). This fuel has a hydrogen-to-carbon ratio of 1.80 to 1.

7.2.1  Fuel Approval Requirements—The fuel is blended to a sulfur content of 130 ± 10 ppm and the fuel supplier supplier’s requirements. Base the fuel batch acceptance upon the physical and chemical specifications given in Annex AX . Engine validation tests are not necessary for fuel batch acceptance.

7.2.2  Fuel Analysis—Monitor the test fuel using good laboratory practices. Analyze each fuel shipment to determine the value of each parameter for fuel sulfur as described in Test Method D2622, existent gum as described in Test Method D381, RVP as described in Test Method D323, and API Gravity as described in Test Method D287. Compare the results to the original values supplied by the fuel supplier. The analytical results shall be within the tolerances shown in parentheses beside each parameter. This provides a method to determine if the fuel batch is contaminated or has aged prematurely. If any analytical result falls outside the tolerances, the laboratory shall contact the fuel supplier for problem resolution.

7.2.2.1  Fuel Deterioration—Analyze the fuel semiannually to ensure the fuel has not deteriorated excessively or been contaminated in storage.

7.2.2.2  Analyze the fuels using Test Methods D2622, D287, D323, D381, and D525.

7.2.3  Fuel Shipment and Storage—Ship the fuel in containers with the minimum allowable venting as dictated by all safety and environmental regulations, especially when shipment times are anticipated to be longer than one week. Store the fuel in accordance with all applicable safety and environmental regulations. If the run tank has more than one batch of fuel, document the most recent batch in the test report. Do not top-off the run tank with the new fuel batch unless the tank is less than 10 % full.

7.3  Lubricating Oils:

7.3.1  Break-in Lubricating Oil—An engine break-in procedure (see 11.1.3) is immediately conducted following the replacement of new, major engine components (that is, engine short-block, or cylinder head, or both). Use the proper reference oil, REO 1006-2, from the TMC for the break-in procedure. Use approximately 3 L of this reference oil for each break-in procedure.

7.3.3  Short-block Assembly Lubricant—For engine short-block inspection and reassemble, use SAE 20 API SA grade oil as the assembly lubricant.

7.4  Miscellaneous Materials:

7.4.1  Solvents and Cleansers—No substitutions for 7.4.1.1 – 7.4.1.3 are allowed. Use adequate safety provisions with all solvents and cleaners.

7.4.1.1  Solvent—Use only mineral spirits meeting the requirements of Specification D235, Type II, Class C for Aromatic Content ((0 to 2) vol %), Flash Point (61 °C, min) and Color (not darker than +25 on Saybolt Scale or 25 on Pt-Co Scale). (Warning—Combustible. Health hazard.) Obtain a Certificate of Analysis for each batch of solvent from the supplier.

7.4.1.2  Pentane—(Warning—Flammable. Health hazard.) Available from petroleum solvent suppliers.

7.4.1.3  Cylinder Block and RAC Cleaning Detergent—Tri-sodium phosphate and any commercial coolant cleanser. (Warning— Caustic. Health hazard.)

7.4.2  Sealing Compounds—Use a silicone based gasketing compound during engine assembly (for example, oil pan). Use only the silicone gasket shown in Annex AX .

8.  Oil Blend Sampling Requirements

8.1  Sample Selection and Inspection—The non-reference oil sample shall be uncontaminated and representative of the lubricant formulation being evaluated.

Note 7—If the test is registered using the American Chemistry Council25 protocols, the assigned oil container formulation number shall match the registration form.

8.2  Non-reference Oil Sample Quantity—Use a minimum of 15 L of new oil to complete the Sequence IVB test, including the oil flushes. Normally the supplier provides a 19 L new oil sample to allow for inadvertent losses.

8.3  Reference Oil Sample Quantity—The TMC provides a 19 L reference oil sample for each stand calibration test.

10.  Data Acquisition, Reference Oil Application, and Equipment Calibration and Maintenance

10.1  Data Acquisition:

10.1.1  Computer Data Acquisition—The test stand should log operational data using a computer data acquisition system with sensor configurations process is described in 10.1.2 – 10.1.4.

10.1.2  Frequency of Logged Test Cycle Data—Log the test cycle data at a sampling rate of 1-Hz.

10.1.3  Signal Conditioning—Do not exceed the controlled operational parameters for system time response as shown in Table 1. The system time response includes the total system of sensor, transducer, analog signal attenuation, and computer digital filtering. Use single-pole type filters for attenuation. For temperature sensors only grounded thermocouples are acceptable.

10.1.3.1  Isolated Inputs—Use signal-conditioning modules to provide isolated inputs to the digital computer.

10.2  Reference Oil Application:

Note 9—10.2.6 and 10.2.7 and Annex A1 - 4 describe the involvement of the TMC in respect to calibration procedures and acceptance criteria for a testing laboratory and a test stand, and the issuance of Information Letters and memoranda affecting the test method.

10.2.1  Testing of Reference Oils—Periodically conduct tests on reference oils according to the following:

10.2.1.1  Conduct reference oil tests on each calibrated test stand within a laboratory according to TMC guidelines.

10.2.1.2  Obtain reference oils directly from the TMC. These oils are formulated or selected to represent specific chemical types or performance levels, or both. They are usually supplied directly to a testing laboratory under code numbers to ensure that the laboratory is not influenced by prior knowledge of acceptable results in assessing the test results. The TMC determines which specific reference oil the laboratory shall test.

10.2.1.3  Unless specifically authorized by the TMC, do not analyze reference oils, either physically or chemically. Identification of reference oils by such analyses could undermine the confidentiality required to operate an effective reference oil system. Therefore, reference oils are supplied with the explicit understanding that they will not be subjected to analyses other than those specified in this procedure, unless specifically authorized by the TMC. If so authorized, prepare a written statement of the circumstances involved, the name of the person authorizing the analysis, and the data obtained; furnish copies of this statement to the TMC.

10.2.2  Reference Oil Test Frequency—Conduct reference oil tests according to the following frequency requirements:

10.2.2.1  For a given, calibrated test stand, conduct an acceptable reference oil test after no more than XX test starts have been conducted, or after TBD have elapsed, whichever occurs first.

10.2.2.2  After starting a laboratory reference oil test, non-reference oil tests may be started on any other calibrated test stand.

10.2.2.3  Reference oil test frequency may be adjusted due to the following reasons:

10.2.3  Procedural Deviations—On occasions when a laboratory becomes aware of a significant deviation from the test method, such as might arise during an in-house review or a TMC inspection, the laboratory and the TMC shall agree on an appropriate course of action to remedy the deviation. This action may include the shortening of existing reference oil calibration periods.

10.2.4  Parts and Fuel Shortages—Under special circumstances, such as industry-wide parts or fuel shortages, the Surveillance Panel may direct the TMC to extend the time intervals between reference oil tests. These extensions shall not exceed one regular calibration period.

10.2.5  Reference Oil Test Data Flow—To ensure continuous severity and precision monitoring, calibration tests are conducted periodically throughout the year. There may be occasions when laboratories conduct a large portion of calibration tests in a short period of time. This could result in an unacceptably large time frame when very few calibration tests are conducted. The TMC can shorten or extend calibration periods as needed to provide a consistent flow of reference oil test data. Adjustments to calibration periods are made such that laboratories incur no net loss (or gain) in calibration status.

10.2.6  Special Use of the Reference Oil Calibration System—The Surveillance Panel has the option to use the reference oil system to evaluate changes that have potential impact on test severity and precision. This option is only taken when a program of donated tests is not feasible. The Surveillance Panel and the TMC shall develop a detailed plan for the test program. This plan requires all reference oil tests in the program to be completed as close to the same time as possible, so that no laboratory/stand calibration is left in an excessively long pending status. In order to maintain the integrity of the reference oil monitoring system, each reference oil test is conducted so as to be interpretable for stand calibration. To facilitate the required test scheduling, the Surveillance Panel may direct the TMC to lengthen and shorten reference oil calibration periods within laboratories such that the laboratories incur no net loss (or gain) in calibration status.

10.2.7  Donated Reference Oil Test Programs—The Surveillance Panel is charged with maintaining effective reference oil test severity and precision monitoring. During times of new parts introductions, new or re-blended reference oil additions, and procedural revisions, it may be necessary to evaluate the possible effects on severity and precision levels. The Surveillance Panel may choose to conduct a program of donated reference oil tests in those laboratories participating in the monitoring system, in order to quantify the effect of a particular change on severity and precision. Typically, the Surveillance Panel requests its panel members to volunteer enough reference oil test results to create a robust data set. Broad laboratory participation is needed to provide a representative sampling of the industry. To ensure the quality of the data obtained, donated tests are conducted on calibrated test stands. The Surveillance Panel shall arrange an appropriate number of donated tests and ensure completion of the test program in a timely manner.

10.2.8  Reporting of Reference Oil Test Results—Report the results of all reference oil tests to the TMC according to the following directives:

10.2.8.1  Transmit results to the TMC within five days of test completion by way of electronic data transfer protocol as outlined in the Data Communication Committee, Electronic Test Report Transmission Model (ETRTM). The ETRTM can be obtained from the TMC.

10.2.8.2  If the test was conducted during a time extension permitted by the TMC, so indicate in the Comments section of the test report.

10.2.8.3  For an acceptable reference oil test, conducted following an unacceptable reference oil test, provide sufficient information in the Comments section of the test report to indicate how the problem was identified and corrected, insofar as possible, and how it was related to non-reference oil tests conducted during the period of time that the problem was being solved.

10.2.9  Evaluation of Reference Oil Test Results—The TMC evaluates the reference-oil test results for both operational validity and statistical acceptability. The TMC may consult with the test laboratory in case of difficulty, as follows:

10.2.9.1  Immediately upon receipt of the reference-oil test results from the test laboratory, the TMC evaluates the laboratories decision on operational validity. For operationally valid tests, the TMC then evaluates the pass/fail parameters according to the Sequence IVB Lubricant Test Monitoring System (TBD). If the test is judged acceptable, the reference oil code is disclosed by the TMC to the test laboratory. The TMC conveys to the test laboratory its preliminary findings based on the limited information available to them.

10.2.9.2  Subsequently, upon receipt of the information detailed in 13.1.1 the TMC reviews all reference-oil test results and reports to determine final test acceptability.

10.2.9.3  In the event the reference oil test is unacceptable, the test laboratory shall provide an explanation of the problem relating to the failure. If the problem is not obvious, all test-related equipment shall be re-checked. Following this re-check, the TMC assigns another reference oil for testing by the laboratory.

10.2.9.4  The TMC decides, with consultation as needed with industry experts (testing laboratories, members of the ASTM Technical Guidance Committee and of the Surveillance Panel, and so forth), whether the reason for any failure of a reference oil test is a false alarm, testing stand, testing laboratory, or industry-related problem. The Sequence IVB Surveillance Panel shall adjudicate all industry problems.

10.2.10  Status of Non-Reference Oil Tests Relative to Reference Oil Tests—Non-reference oil tests may proceed within a given laboratory during reference oil testing based upon the following:

10.2.10.1  During the time of conducting a reference oil test on one test stand, non-reference oil tests may be conducted on other previously calibrated stands. If the reference oil test is acceptable to the TMC, the non-reference oil tests shall be considered to have been run in a satisfactorily calibrated laboratory.

10.2.10.2  If a reference oil test is unacceptable, and it is determined that the problem is isolated to an individual test stand, consider other test stands to remain calibrated, and testing of non-reference oils may proceed on those other stands.

10.2.10.3  If a reference oil test is unacceptable, and it is determined that the problem is laboratory related, non-reference tests running during the problem period shall be considered invalid unless there is specific evidence to the contrary for each test.

10.2.11  Status of Test Stands Used for Non-Standard Tests—If a non-standard test is conducted on a previously calibrated test stand, conduct a reference oil test on that stand to demonstrate that it continues to be calibrated, prior to running standard tests.

10.3  Equipment Calibration:

10.3.1  Instrumentation Calibration—Perform a thorough recalibration adjustment of all instrumentation and transducers, including computer channels, according to the requirements that follow. Perform additional calibration checks whenever operational data indicates an abnormality. Standards used for instrumentation calibration shall be traceable to that country’s specific national standards organization. The accuracy of the standard shall be a minimum of four times better than the accuracy of the test stand instrumentation.

10.3.2  Dynamometer Torque Measurement—Scale the final readout of engine torque (N·m). Calibrate the force measurement and readout system with deadweights. Coolant flow through the dynamometer, reaction forces due to coolant plumbing, and brinnelled trunnion bearings of the dynamometer may affect calibration by temperature excursions of the dynamometer electronic force transducer. When calibrating, ensure the dynamometer coolant flow indicator is in the green (Refer to Figure 10 in Section E) and that the load cell temperature has been stabilized at 45°C ± 1°C for a minimum of one hour. The torque measurement accuracy shall be ± 0.2 N·m. Perform this calibration prior to every test start.

10.3.3 Instrument Calibration—Document all instrument calibrations.  Retain all calibration documentation for a minimum of 3 years.

10.3.3 Upon initial stand installation and every 12 months thereafter perform a full instrumentation calibration according to

TABLE 4 Parameters to be Calibrated Every 12 Months

Items

Temperatures

Intake Air Temperature, °C

Engine Oil Gallery Temperature, °C

Engine Oil Sump Temperature, °C

Coolant Temperature Into Engine, °C

Coolant Temperature Out of Engine, °C

Fuel Rail Temperature, °C

Exhaust Gas Temperature, °C

Valve Cover Coolant In Temperature, °C

Valve Cover Coolant Out Temperature, °C

Test Cell Air Temperature, °C

Blow-by Gas Temperature, °C

Blow-by Coolant Temperature, °C

Pressures

Crankcase Gas Pressure, kPa

Oil Gallery Pressure, kPa

Fuel Rail Pressure, kPa

Exhaust Pressure, kPa (absolute)

Intake Air Pressure, kPa

Intake Manifold Pressure, kPa (absolute)

Barometric Pressure, kPa (absolute)

Flows

Air Fuel Ratio, afr

Blowby Flow Rate, sl/min

Fuel Flow Rate, kg/h

Engine Coolant Flow Rate, L/min

Valve Cover Coolant Flow Rate, L/min

General

Intake Air Humidity, grains/kg

Engine Speed, r/min

Engine Torque (N-m)

10.3.4  Humidity of Induction Air Calibration:

10.3.4.1  Calibrate the primary laboratory measurement system at each test stand every 6 months using a hygrometer with a minimum dew point accuracy of ± 0.55 °C at 16 °C. Locate the sample tap on the air supply line to the engine, between the main duct and 1000 mm upstream of the intake air cleaner. The calibration consists of a series of paired humidity measurements comparing the laboratory system with the calibration hygrometer. The comparison period lasts from 20 min to 2 h with measurements taken at intervals of (1 to 6) min, for a total of 20 paired measurements. The measurement interval shall be appropriate for the time constant of the humidity measurement instruments.

10.3.4.2  Verify that the flow rate is within the equipment manufacturer’s specification and that the sample lines are non-hygroscopic. Correct dew point hygrometer measurements to standard conditions (101.12 kPa) using the appropriate equation. Compute the difference between each pair of readings and calculate the mean and standard deviation of the twenty-paired readings. The absolute value of the mean difference shall not exceed 1.43 g/kg, and the standard deviation shall not be greater than 0.714 g/kg. If these conditions are not met, investigate the cause, make repairs, and recalibrate. Maintain calibration records for 2 years.

10.3.5  Profilometer Calibration—Follow the manufacturer’s instruction for calibration and verification checks of the profilometer. Calibrate the profilometer at least annually.

10.3.6  Keyence Measurement Device —Confirm the calibration of the Keyence measurement device at least once every 6 months.

11. Procedure

NOTE 11—When installing a new engine and cylinder head or both, conduct a break-in procedure, see 11.1.4, before running official 200 h tests. After completing the break-in, install the official test valve-train parts as shown in the Assembly Manual. Then conduct and external system flush, an oil pan flush, and four fired oil-flushes as shown in 11.2.1. After performing the four fired oil-flushes, conduct the 200 h test as shown in 11.2.2.

11.1 Pre-test Procedure:

11.1.1 Pre-test stand cleaning—Clean all pressure traps and the external oil system prior to starting all tests.

11.1.1.1 Remove, spray clean with specification D235 solvent, and air dry the exhaust backpressure and crankcase pressure filters. Re-install the filters using new O-rings (part XX).

11.1.1.2 Disconnect the external oil supply and oil return lines from the remote oil filter housing adapter that is mounted on the engine (refer to figure 1).

Figure Error! No text of specified style in document..1 Remote Oil Filter Housing Adapter

11.1.1.2 Connect the external oil supply and external oil return lines to a portable oil cleaning flush cart of minimum 1 gallon capacity that is equipped with a circulation pump. Charge the flush cart with solvent and energize the flush cart pump. Allow the solvent to circulate for one hour.

11.1.1.3 After solvent has circulated for at least one hour, de-energize the flush cart pump and open both heat exchanger drain valves and allow the external oil system to drain.

11.1.1.4 Disconnect the external oil supply and external oil return lines from the flush cart and connect the external oil system to a clean and dry compressed air supply at 15 to 30 psi. Allow the air to flow through the system for at least 15 minutes to dry the system.

11.1.1.5 Disconnect the supply and return lines from the compressed air source and connect the external oil supply and external return lines back to the remote oil filter housing adapter that is mounted on the engine. Close the heat exchanger drain valves.

11.1.1.6 Remove the Oberg oil filter element for cleaning. Clear any debris retained in the Oberg oil filter element with solvent and air dry. Re-install the Oberg oil filter element in the Oberg filter housing and secure the four retaining bolts.

11.1.1.7 Disconnect the oil pressure sense line between the engine and oil sample valve. Rinse this line using clean solvent and air dry.

11.1.1.8 Disconnect the oil pressure sense line between the oil sample valve and the oil pressure transducer. Rinse this line using clean solvent and air dry.

11.1.1.9 Open the oil sample valve and allow any trapped oil to drain. Then close the valve and reconnect both oil pressure/sample lines to their respective locations.

11.1.2 Oil pan flush—Flush the oil pan with EF-411 oil supplied by an external pump prior to all tests.

11.1.2.1 Pour 1 gallon of new EF-411 into a clean oil flush apparatus.

11.1.2.2 Ensure the apparatus utilizes a NAPA 1-8429 oil filter adapter, and unused Motorcraft FL 1A oil filter, GP-201-12L pump, and only clean tygon hose, stainless steel, or black pipe connections.

11.1.2.3 Connect the apparatus supply to the #8 AN fitting on the side of the modified Sequence IVB oil pan and the return to the rear oil pan drain plug.

11.1.2.4 Run the pump and circulate the EF-411thorugh the oil pan for 10 minutes.

11.1.2.5 Turn off the pump, remove the apparatus, and allow the EF-411 to drain for 5 minutes.

11.1.2.6 Re-install a stainless steel cap on the #8 fitting on the side of the oil pain and re-install the oil pan drain plug.

11.1.3 Blow-by system flush—Flush the tube side of the external blow-by system with solvent prior to all tests.

11.1.3.1 Pour 1 gallon of new solvent into a portable solvent flush cart.

11.1.3.2 Connect the cart supply to the barbed hose fitting at the top of blow-by heat exchanger and the return to the pipe nipple that connects the external blow-by system to the valve cover. Charge the flush cart with solvent and energize the flush cart pump. Allow the solvent to circulate for one hour

11.1.3..3 After solvent has circulated for at least one hour, de-energize the flush cart pump and allow the external blow-by system to drain.

11.1.3.4 Disconnect the flush cart and connect the external blow-by system to a clean and dry compressed air supply at 15 to 30 psi. Allow the air to flow through the system for at least 15 minutes to dry the system.

11.1.3.5 Disconnect the supply and return lines from the compressed air source.

11.1.3.6 Remove all the short tygon hose sections between the valve cover and external blow-by system heat exchanger and replace them.

11.1.3.7 Reconnect the external blow-by system to the valve cover and blow-by gas filter.

11.1.4 Engine coolant fill procedure—Charge the engine coolant, valve cover coolant, and blow-by heat exchanger coolant tanks with a 70%/30% mixture of deionized water and Havoline DEX-COOL prior to the start of all tests.

11.1.4.1 Pressurize the coolant system to approximately 70 kPa.

11.1.5 Dynamometer load cell calibration—Calibrate the load cell in accordance with the specifications in Table 4 below.

TABLE 5 Dynamometer Load Cell Calibration Reference

| Calibration Point | Reference Calibration Target Mass, kg | Resulting Reference Torque, N-m | Maximum Error |
| --- | --- | --- | --- |
| Zero | 2.535 | 9.94 | 0.5% |
| Mid-rage | 7.130 | 27.97 | 0.5% |
| Span | 11.335 | 44.47 | 0.5% |

11.1.6 Engine break-in procedure—Conduct the break-in procedure prior to lubricant evaluation testing when installing a new engine block or cylinder head assembly on a test stand. The break-in allows for monitoring test stand performance and pacification of silicone sealant on the cylinder head, front cover, and oil pan. Use the engine block assembly for XX tests and the head for XX tests. Follow the break in conditions in Table A.1. Use the following break-in steps:

11.1.6.1 Install break-in parts according to Assembly Manual Section 2. A stock unmodified Toyota intake camshaft and unmeasured bucket lifters may be used for break-in.

11.1.6.2 Install the stock black plastic valve train cover and stock crankcase ventilation setup.

11.1.6.3 Connect the PCV valve in the valve cover to the intake manifold with the stock 19 mm ventilation hose.

11.1.6.4 Connect the valve cover port to the intake air filter housing port with a 15 mm diameter Tygon hose.

11.1.6.5 Connect the braided stainless steel hose from the crankcase pressure transducer to the quick disconnect on the modified oil fill cap.

11.1.6.6 Perform all pre-test procedures, sections 11.1.1 to 11.1.3.

11.1.6.7 Fill the engine with 3.0 L of ASTM REO 1006-2 break-in oil.

11.1.6.8 Start the engine and begin the break-in schedule provided in Table A.1.

11.1.6.9 Control the parameters specified in Table 5 below to constant setpoints over the entire course of the break-in procedure.

TABLE 6 Break-in Constant Setpoints

| Parameter | Setpoint |
| --- | --- |
| Fuel rail temperature, °C | 24 ± 3 |
| Coolant flow rate, L/min | 80 ± 1 |
| Exhaust backpressure. kPaA | 103.5 ± 1.0 |
| Intake air pressure, kPaA | 0.25 ± 0.3 |
| Intake air temperature, °C | 32 ± 2 |
| Load cell temperature, °C | 45 ± 2 |

11.1.6.10 Following the completion of engine break-in step 8, establish the oil sampling conditions listed in Table 6.

TABLE 7 Oil Sampling Conditions

| Engine Speed, rpm | Engine Load, Nm | Gallery Oil Temperature, °C | Coolant Out Temperature, °C |
| --- | --- | --- | --- |
| 1000 | 10.0 | 50 | 52 |

11.1.6.11 Once the conditions have been reached, take a 240 ml purge sample followed by a 30 ml oil sample and return the 240 ml purge sample to the oil fill cap.

11.1.6.12 Turn off the engine and allow to rest for 10 minutes prior to checking the oil level with the Toyota stock dipstick that is located on the valve cover. The intake air hose should always be disconnected when checking the oil level.

11.1.6.13 After checking the oil level, restart the engine and run the aging conditions in Table 7 below for 25 hours.

TABLE 8 Engine Aging Conditions

| Engine Speed, rpm | Engine Load, Nm | Gallery Oil Temperature, °C | Coolant Out Temperature, °C |
| --- | --- | --- | --- |
| 3000 | 50.0 | 80 | 88 |

11.1.6.14 After 25 hours, turn off the engine and allow to rest for 10 minutes prior to checking the oil level with the Toyota stock dipstick that is located on the valve cover.

11.1.6.15 After checking the oil level, restart the engine and run the aging operating conditions for a final 25 hours.

11.1.6.16 After 25 hours, return to oil sampling conditions and take a final 240 ml purge sample followed by a 30 ml oil sample and return the 240 ml purge sample to the oil fill cap.

11.1.6.17 Turn off the engine and allow to rest for 10 minutes prior to checking the oil level with the Toyota stock dipstick that is located on the valve cover. This concludes engine break-in.

11.2 Test Procedure:

11.2.1 Engine flushes—Conduct four fired flushes with 2400 ml of test evaluation oil at the conditions listed in Table 8.

11.2.1.1 Conduct the 1st engine flush by filling the engine with 2400 ml and operating at the Table 8 conditions for 6 minutes.

11.2.1.2 After the first flush, turn the engine off and conduct a compression and leakdown test and record these values. Engine oil is required for the leakdown test

11.2.1.3 Drain the flush oil from the oil pain drain plug and the two external oil system heat exchanger drain valves for 30 minutes. Retain an oil sample for analysis.

11.2.1.4 Conduct the 2nd flush by filling the engine with 2400 ml and operating at the Table 8 conditions for 38 minutes.

11.2.1.5 Drain the flush oil from the oil pain drain plug and the two external oil system heat exchanger drain valves for 30 minutes. Retain an oil sample for analysis.

11.2.1.6 Repeat steps 11.2.1.4 and 11.2.1.5 for the 3rd flush.

11.2.1.6 For the 4th flush, weight the flush oil charge prior to repeating steps 11.2.1.4 and 11.2.1.5.

11.2.1.7 Weigh the 4th flush drain oil so that the mass of oil left in the engine before the test charge can be estimated.

11.2.2 Test Operation—Conduct a 200 hour test consisting of 24000 30 second 4-stage cycles under the conditions specified by Table 2, Table A.2 and Table A.3.

11.2.2.1 Remove the external oils system Oberg filter, clean with solvent, and air dry.

11.2.2.1 Weight out a 2100 g test charge and fill the engine.

11.2.2.2 Operate the engine at stage 1 idle conditions for 10 minutes then shutdown the engine and wait 10 minutes before measuring the oil level using the modified Sequence IVB dipstick that inserted into the side of the oil pan.

11.2.2.3 Start the engine in stage 1 conditions and remain there for at least 10 minutes and until reaching a coolant temperature of at least 45°C, an oil gallery temperature of at least 45 °C.

11.2.2.4 Begin first cycle of test operations.

11.2.2.4.1 Intermediate oil samples are required at 25, 50, 75, 100, 105, 110, 115, 120, 125, 130, 135, 140, 145, 150, 155, 160, 165, 170, 175, 180, 185, 190, and 195 test hours. 1 oz oil samples are taken at every 25 hour interval and 3 ml samples are taken at every 5 hour interval that is not also a 25 hour interval.

11.2.2.4.2 The 0 hour sample should be analyzed with methods D5185, D445, D664, and D4739.

11.2.2.4.3 All 1 oz samples should be analyzed with methods D5185, D445, D664, D4739, D3525, and IR 5.8_6.1.

11.2.2.4.4 All 3 ml samples should be analyzed with method D5185.

11.2.2.5 At oil sampling intervals, operate the engine at stage 1 conditions. Remove a 240 ml purge sample and return it followed by a second 240 ml purge sample which is returned.

11.2.2.6 After both purges, take the volume of oil sample specified by the test hour and the instructions in step 11.2.2.4.

11.2.2.7 After 200 hours which should be approximately 24000 cycles, the test is concluded.

11.2.3 Shutdowns and test resumes—In the event of a non-end-of-test shutdown, restart the engine once ready by first operating at stage 1 conditions for at least 4.5 minutes and until reaching a coolant temperature of at least 45°C, an oil gallery temperature of at least 45 °C, the blow-by temperature is blow-by temperature of at least 28.5 °C. Then return to the test speed at shutdown over the course of a 30 second ramp before re-entering the test. The engine should not be started until the blow-by coolant tank reaches 30 °C.

11.2.3.1 If a test shutdowns due to cam lobe failure(s), that test cannot be resumed and is deemed non-interpretable.

11.2.3.2 Any engines that experience lobe failure must be removed from service for full inspection of bearing and cylinder liner surfaces. A full rebuild with new main and rod bearings must be conducted in accordance with Assembly Manual Section 4 before an engine can be returned to service.

11.3 Post-test procedures

11.3.1 Oil level— After 200 hours of test operation, allow the engine to run at stage 1 conditions for 10 minutes before shutting down. Let the engine rest shutdown for 10 minutes and then measure the end-of-test level using the modified Sequence IVB dipstick inserted into the side of the oil pan.

11.3.2 Check the engine’s compression and leakdown.

11.3.3 Oil consumption— Drain the test oil from the oil pain drain plug and the two external oil system heat exchanger drain valves for 30 minutes. Retain an 8 oz oil sample for analysis

11.3.3.1 Weigh the drained test oil and calculate the oil consumption for the test by finding the difference between the initial charge and final drain and then subtracting the mass of the intermediate oil samples from that value.

11.3.4 Fuel consumption— Note how much fuel was consumed over the course of the test.

11.3.5 Post-test wear measurements:

11.3.5.1 All volume loss measurements are to be conducted with a Keyence 3D macroscope in accordance with the IVB Keyence VR-3000 Procedure.

Table 9 Engine Oil Flush Operating Parameters

| Parameter | Setpoint |
| --- | --- |
| Engine Speed | 1500 rpm |
| Torque | 10 N*m |
| Engine Coolant Out Temperature | 52 °C |
| Engine Oil Gallery Temperature | 49°C |
| Exhaust Back Pressure | 103.5 kPaa |
| Intake Air Pressure | 0.25 kPag |
| Intake Air Temperature | 32°C |
| Fuel Temperature | 24°C |
| Rocker Cover Outlet Temperature | 20°C |
| Coolant Flow Rate (Engine) | 80 L/min |
| Coolant Flow Rate (Rocker Arm Cover) | 120 L/min |
| Load Cell Temperature | 45°C |
| Blowby Gas Temperature | 29°C |
| Coolant Temperature Heater | Heater OFF |

TABLE A.1 Engine Break-in Schedule

| Break-in Step # | Duration, min | Engine Speed, rpm | Engine Load, N-m | Gallery Oil Temperature, °C | Coolant Out Temperature, °C |
| --- | --- | --- | --- | --- | --- |
| 1 | 10 | 800 | 6.3 | 50 | 50 |
| 2 | 10 | 1600 | 6.3 | 55 | 50 |
| 3 | 10 | 200 | 25.0 | 60 | 55 |
| 4 | 10 | 2400 | 25.0 | 65 | 60 |
| 5 | 10 | 2400 | 46.9 | 70 | 65 |
| 6 | 15 | 2800 | 46.9 | 75 | 70 |
| 7 | 15 | 3200 | 46.9 | 80 | 75 |
| 8 | 15 | 3200 | 46.9 | 85 | 80 |

TABLE A.2 Summary of Sequence IVB Test Operating Conditions

| Parameter | Units | Ramp to Stage 1 | Stage 1 | Ramp to Stage 2 | Stage 2 |
| --- | --- | --- | --- | --- | --- |
| Duration | s | 8 | 7 | 8 | 7 |
| Engine Speed | Rpm | 4300 to 800 | 800 | 800 to 4300 | 4300 |
| Engine Torque | N-m | 25 ± 1.5 | 25 ± 1.5 | 25 ± 1.5 | 25 ± 1.5 |
| Coolant Out Temperature | °C | 52 ± 1.5 | 52 ± 1.5 | 52 ± 1.5 | 52 ± 1.5 |
| Coolant Flow (Engine) | L/min | 80 ± 0.4 | 80 ± 0.4 | 80 ± 0.4 | 80 ± 0.4 |
| Coolant Flow (RAC) | L/min | 120 ± 0.75 | 120 ± 0.75 | 120 ± 0.75 | 120 ± 0.75 |
| Oil Gallery Temperature | °C | 54 ± 5 | 54 ± 5 | 54 ± 5 | 54 ± 5 |
| RAC Coolant Out Temperature | °C | 20 ± 0.75 | 20 ± 0.75 | 20 ± 0.75 | 20 ± 0.75 |
| Fuel Rail Temperature | °C | 24 ± 0.5 | 24 ± 0.5 | 24 ± 0.5 | 24 ± 0.5 |
| Load Cell Temperature | °C | 45 ± 4 | 45 ± 4 | 45 ± 4 | 45 ± 4 |
| Intake Air Temperature | °C | 32 ± 0.75 | 32 ± 0.75 | 32 ± 0.75 | 32 ± 0.75 |
| Blowby Gas Temperature | °C | 29 ± 0.5 | 29 ± 0.5 | 29 ± 0.5 | 29 ± 0.5 |
| Intake Air Pressure | kPa | 0.25 ± 0.25 | 0.25 ± 0.25 | 0.25 ± 0.25 | 0.25 ± 0.25 |
| Intake Air Humidity | g/kg | 11.5 ± 0.5 | 11.5 ± 0.5 | 11.5 ± 0.5 | 11.5 ± 0.5 |
| Exhaust Pressure | kPaA | - | - | - | 104.5 ± 3 |
| Engine Coolant Pressure | kPa | 70 ± 10 | 70 ± 10 | 70 ± 10 | 70 ± 10 |
| Fuel Rail Pressure | kPa | 335 ± 10 | 335 ± 10 | 335 ± 10 | 335 ± 10 |
| Air-to-Fuel Ratio (Not Controlled) | :1 | Record | 14.5 ± 0.5 | Record | 14.5 ± 0.5 |

TABLE A.3 RPM Setpoints and QI Control Limits

| Cycle Time, s | Setpoint, rpm | U, rpm | L, rpm |
| --- | --- | --- | --- |
| 1 | 800 | 950 | 650 |
| 2 | 800 | 900 | 700 |
| 3 | 800 | 875 | 725 |
| 4 | 800 | 850 | 750 |
| 5 | 800 | 850 | 750 |
| 6 | 800 | 850 | 750 |
| 7 | 800 | 850 | 750 |
| 8 | 927 | 1077 | 777 |
| 9 | 1357 | 1607 | 1107 |
| 10 | 1888 | 2288 | 1488 |
| 11 | 2300 | 2700 | 1900 |
| 12 | 2731 | 3131 | 2331 |
| 13 | 3168 | 3568 | 2768 |
| 14 | 3610 | 4010 | 3210 |
| 15 | 4041 | 4441 | 3641 |
| 16 | 4300 | 4400 | 4200 |
| 17 | 4300 | 4375 | 4225 |
| 18 | 4300 | 4350 | 4250 |
| 19 | 4300 | 4325 | 4275 |
| 20 | 4300 | 4325 | 4275 |
| 21 | 4300 | 4325 | 4275 |
| 22 | 4300 | 4325 | 4275 |
| 23 | 4136 | 4236 | 4036 |
| 24 | 3734 | 3984 | 3484 |
| 25 | 3283 | 3683 | 2883 |
| 26 | 2829 | 3229 | 2429 |
| 27 | 2382 | 2782 | 1982 |
| 28 | 1946 | 2346 | 1546 |
| 29 | 1523 | 1923 | 1123 |
| 30 | 1116 | 1516 | 716 |

A7. THERMOCOUPLES

A7.1 This annex This annex illustrates the locations and depths of the required IVB thermocouples which are supplied by Test Engineering Inc.

TABLE A7 Thermocouple List

| # | Description | Thermocouple Size | Depth (mm) | Depth Reference |
| --- | --- | --- | --- | --- |
| 1 | Engine Coolant Out | E-Type 1/8” x 4” | 78 | Rear of Head |
| 2 | Engine Coolant In | E-Type 1/8” x 4” | 75 | Coolant Pipe |
| 3 | Engine Oil Gallery | E-Type 1/8” x 4” | 92 | Engine Block |
| 4 | Load Cell | E-Type 1/8” x 4” | 9 | Top of Swage Nut |
| 5 | Intake Air | E-Type 1/8” x 4” | 60 | Adaptor Plate |
| 6 | Test Cell | E-Type 1/8” x 2” | N/A | N/A |
| 7 | Fuel | E-Type 1/8” x 4” | 98 | Center of Tee |
| 8 | Oil Sump | E-Type 1/8” x 3” | 5 | Top of Swage Nut |
| 9 | Valve Cover Gas Out | E-Type 1/8” x 4” | 39 | Center of Tee |
| 10 | Valve Cover Coolant In | E-Type 1/8” x 4” | 100 | Center of Tee |
| 11 | Valve Cover Coolant Out | E-Type 1/8” x 4” | 100 | Center of Tee |
| 12 | Exhaust Gas | E-Type 1/4” x 4” | 21 | Top of Swage Nut |
| 13 | Dynamometer Coolant Out | E-Type 1/8” x 4” | 100 | Center of Tee |
| 14 | Blow-by Gas | E-Type 1/8” x 4” | 100 | Center of Tee |
| 15 | Blow-by Coolant Out | E-Type 1/8” x 3” | 2 | Top of Swage Nut |

Figure A7. 1 Engine Coolant Out

Figure A7. 1 Engine Coolant Out

Figure A7. 2 Engine Coolant In

Figure A7. 2 Engine Coolant In

Figure A7. 3 Engine Oil Gallery

Figure A7. 3 Engine Oil Gallery

Figure A7. 4 Load Cell

Figure A7. 4 Load Cell

Figure A7. 5 Intake Air

Figure A7. 5 Intake Air

Figure A7. 6 Test Cell

Figure A7. 6 Test Cell

Figure A7. 7 Fuel

Figure A7. 7 Fuel

Figure A7. 8 Oil Sump

Figure A7. 8 Oil Sump

Figure A7. 9 Valve Cover Gas

Figure A7. 9 Valve Cover Gas

Figure A7. 10 Valve Cover Coolant In

Figure A7. 11 Valve Cover Coolant Out

Figure A7. 11 Valve Cover Coolant Out

Figure A7. 12 Exhaust Gas

Figure A7. 12 Exhaust Gas

Figure A7. 13 Dynamometer Coolant Out

Figure A7. 13 Dynamometer Coolant Out

Figure A7. 14 Blow-by Gas

Figure A7. 14 Blow-by Gas

Figure A7. 15 Blow-by Coolant Out

Figure A7. 15 Blow-by Coolant Out

This test method is under the jurisdiction of ASTM Committee D02 on Petroleum Products, Liquid Fuels, and Lubricants   and is the direct responsibility of Subcommittee D02.B0 on Automotive Lubricants.

Current edition approved May 1, 2014. Published June 2014. Originally approved in 2003. Last previous edition approved in 2013 as D6891 – 13a. DOI: 10.1520/D6891-14.

The ASTM Test Monitoring Center will update changes in this test method by means of Information Letters. Information letters may be obtained from the ASTM Test Monitoring Center (TMC), 6555 Penn Ave., Pittsburgh, PA 15206-4489, Attention: Administrator. www.astmtmc.cmu.edu. This edition incorporates all Information Letters through No. 13–1.

For referenced ASTM standards, visit the ASTM website, www.astm.org, or contact ASTM Customer Service at service@astm.org. For  Annual Book of ASTM Standards volume information, refer to the standard’s Document Summary page on the ASTM website.

The last approved version of this historical standard is referenced on www.astm.org.

Available from The American Petroleum Institute (API), 1220 L. St., NW, Washington, DC 20005.

Available from Society of Automotive Engineers (SAE), 400 Commonwealth Dr., Warrendale, PA 15096-0001.

Available from American Society of Mechanical Engineers (ASME), ASME International Headquarters, Three Park Ave., New York, NY 10016-5990.

Available from Japanese Standards Organization (JSA), 4-1-24 Akasaka Minato-Ku, Tokyo, 107-8440, Japan.

Available from the Coordinating European Council for the Development of Performance Tests Transportation Fuels, Lubes, and other Fluids, Madou Plaza , 25 Floor Place, Madou B-1210, Brussels, Belgium.

Available from ASTM Test Monitoring Center (TMC), 6555 Penn Avenue, Pittsburgh, PA 15206-4489, Attention: Administrator.

American Chemistry Council, 1300 Wilson Boulevard, Arlington, VA 22209.