Date: May 03 , 2019

To: Subcommittee D02.B0 members

# Technical Contact: Terry Bates, batesterryw@aol.com

# Work Item #: 54716

# Ballot Action: New engine oil test method

Rationale: This new test method will likely be in the new ILSAC GF-6 engine oil specification

# Prepared by Terry Bates

# Standard Test Method for

Evaluation of Performance of Automotive Engine Oils in the Mitigation of Low-Speed, Preignition in the Sequence IX Gasoline Turbocharged Direct-Injection, Spark-Ignition Engine

This standard is issued under the fixed designation X XXXX; the number immediately following the designation indicates the year of original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A superscript epsilon () indicates an editorial change since the last revision or reapproval.

# INTRODUCTION

Portions of this test method are written for use by laboratories that make use of ASTM Test Monitoring Center (TMC), services (see Annexes A1 to A4).

The TMC provides reference oils, and engineering and statistical services to laboratories that desire to produce test results that are statistically similar to those produced by laboratories previously calibrated by the TMC.

In general, the test purchaser decides if a calibrated test stand is to be used. Organizations such as the American Chemistry Council require that a laboratory utilize the TMC services as part of their test registration process. In addition, the American Petroleum Institute and the Gear Lubricant Review Committee of the Lubricant Review Institute (SAE International) require that a laboratory use the TMC services in seeking qualification of oils against their specifications.

The advantage of using the TMC services to calibrate test stands is that the test laboratory (and hence the Test Purchaser) has an assurance that the test stand was operating at the proper level of test severity. It should also be borne in mind that results obtained in a non-calibrated test stand may not be the same as those obtained in a test stand participating in the ASTM TMC services process.

Laboratories that choose not to use the TMC services may simply disregard these portions.

ASTM International policy is to encourage the development of test procedures based on generic equipment. It is recognized that there are occasions where critical/sole-source equipment has been approved by the technical committee (surveillance panel/task force) and is required by the test procedure. The technical committee that oversees the test procedure is encouraged to clearly identify if the part is considered critical in the test procedure. If a part is deemed to be critical, ASTM encourages alternate suppliers to be given the opportunity for consideration of supplying the critical part/component providing they meet the approval process set forth by the technical committee.

An alternate supplier can start the process by initiating contact with the technical committee (current chairs shown on ASTM TMC website). The supplier should advise on the details of the part that is intended to be supplied. The technical committee will review the request and determine feasibility of an alternate supplier for the requested replacement critical part. In the event that a replacement critical part has been identified and proven equivalent the sole-source supplier footnote shall be removed from the test procedure.

- Scope

  - This laboratory engine test evaluates the ability of an automotive engine to mitigate preignition in the combustion chambers in gasoline, turbocharged, direct-injection (GTGI) engines under low-speed and high-load operating conditions. This test method is commonly known as the Sequence IX test.

    - In vehicles, equipped with relatively small GTDI spark-ignition engines, preignition has occasionally occurred when the vehicles are operated under low-speed and high-load conditions. Uncontrolled, preignition may cause destructive engine damage.

  - The values stated in SI units are to be regarded as standard. No other units of measurement are included in this standard.

1.2.1 Exceptions—Where there is no direct SI equivalent such as screw threads, national pipe threads/diameters, tubing size, wire gage, or specified single source equipment.

1.3 This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use.

2. Referenced Documents

2.1 ASTM Standards:

D86 Test Method for Distillation of Petroleum Products and Liquid Fuels at Atmospheric Pressure

D130 Test Method for Corrosiveness to Copper from Petroleum Products by Copper Strip Test

D235  Specification for Mineral Spirits (Petroleum Spirits) (Hydrocarbon Dry Cleaning    Solvent)

D323 Test Method for Vapor Pressure of Petroleum Products (Reid Method)

D525 Test Method for Oxidation Stability of Gasoline (Induction Period Method)

D381 Test Method for Gum Content in Fuels by Jet Evaporation

D1298 Test Method for Density, Relative Density, or API Gravity of Crude Petroleum and Liquid Petroleum Products by Hydrometer Method

D1319 Test Method for Hydrocarbon Types in Liquid Petroleum Products by Fluorescent Indicator Adsorption

D2622 Test Method for Sulfur in Petroleum Products by Wavelength Dispersive X-ray Fluorescence Spectrometry

D2699 Test Method for Research Octane Number of Spark-Ignition Engines

D2700 Test Method for Motor Octane Number of Spark-Ignition Engine Fuel

D2709 Test Method for Water and Sediment in Middle Distillate Fuels by Centrifuge

D3120 Test Method for Trace Quantities of Sulfur in Light Liquid Petroleum Hydrocarbons by Oxidative Micrcoulometry

D3231 Test Method for Lead in Gasoline by Atomic Absorption Spectroscopy

D3237 Test Method for Lead in Gasoline by Atomic Absorption Spectroscopy

D4175 Terminology Relating to Petroleum, Petroleum Products, and Lubricants

D5453 Test Method for Determination of Total Sulfur in Light Hydrocarbons, Spark Ignition Engine Fuel, Diesel Engine Fuel, and Engine Oil by Ultraviolet Fluorescence

2.2 American National Standards Institute Standards

ANSI MC96.1 Temperature Measurement-Thermocouples

# 3 Terminology

# 3.1 Definitions:

3.1.1 engine oil, n—a liquid that reduces friction or wear, or both, between the moving parts within an engine; removes  heat, particularly from the underside of pistons; and serves as a combustion  gas sealant for piston rings.

3.1.1.1 Discussion—It may contain additives to enhance certain properties.  Inhibition of engine rusting, deposit formation, valve train wear, oil oxidation, and foaming are examples.    D4175

3.1.2 lambda, n—the ratio of actual air mass induced, during engine operation, divided by the theoretical air mass requirement at the stoichiometric air-fuel ratio for the given fuel.

3.1.2.1 Discussion—A lambda value of 1.0 denotes a stoichiometric air-fuel ratio.	D6593

3.1.3 lubricant test monitoring system (LTMS), n—an analytical system in which ASTM calibration test data are used to manage test precision and severity (bias).		D4175

3.1.4 PCM, n—an engine control unit, most commonly called the powertrain control module (PCM), is an electronic device that instantaneously controls a series of actuators on an internal combustion engine to ensure optimal engine performance.

3.1.5 preignition, n—in a spark-ignition engine, ignition of the mixture of fuel and air in the combustion chamber before the passage of the spark.        D4175

3.1.6 quantity, n—in the SI, a measurable property of a body or substance where the property has a magnitude expressed as the product of a number and a unit; there are seven, well-defined base quantities (length, time, mass, temperature, amount of substance, electric current and luminous intensity) from which all other quantities are derived (for example, volume whose SI unit is the cubic metre).

3.1. 6.1  Discussion—symbols for quantities must be carefully defined; are written in italic font, can be upper or lower case, and can be qualified by adding further information in subscripts, or superscripts, or in parentheses (for example, tfuel = 40 C, where t is used as the symbol for the quantity Celsius temperature and tfuel is the symbol for the specific quantity fuel temperature).												D8047

3.2 Acronyms and Abbreviations (italic font denotes the symbol for a quantity):

AvPIE—-average preignition events

CAN—controller area network

DAC—digital-to-analog converter

DACA—data acquisition and control automation

ei —prediction error

ECU—electronic control unit

F—quantile

G—skewness

GTDI—gasoline turbocharged direct injection

IBP—initial boiling point

ID—internal diameter

ip—intermediate precision

K—kurtosis

LCR—lower compression ring

LTMS—lubricant test monitoring system

LSPI—low-speed preignition

M—mean

MAF—mass air flow

MAP—manifold absolute pressure

MAPT —manifold absolute pressure and temperature

MFB—mass fraction burn

MFB2—mass fraction burn at 2 %

PCM—powertrain control module

PCV—positive crankcase ventilation

PID —parameter identification

PIE—preignition event

PMAX—maximum pressure (see Note 5)

PMAXV—pressure maximum voltage

PMINV—pressure minimum voltage

PP—peak pressure (see Note 5)

P/N—part number

R—reproducibility

S—standard deviation

UCR—upper compression ring

VCT—variable valve timing

WOT—wide open throttle

Zi—exponentially weighted moving average

4. Summary of Test Method

4.1 The test procedure is a “flush and run” test, that is, the test engine is used for multiple tests and the next test oil is used to flush the previous test oil from the engine.

# 4.2 The test procedure is conducted in four valid iterations. Each valid iteration is 175,000 engine cycles in length.

4.3 Low-engine speed and high-load, steady-state conditions are used to generate preignition  (PIE) events, which are counted throughout each of the four 175,000 engine cycles.

# 4.4 Combustion pressure is measured directly in each cylinder to provide documentary evidence of the occurrence of PIEs.

5. Significance and Use

5.1 This test method evaluates the ability of an automotive engine to mitigate preignition in the combustion chambers in turbocharged, direct injection, gasoline engines under low-speed and high-load operating conditions.

5.2 Varying quality reference oils, with known preignition tendencies, were used in developing the operating conditions of the test procedure.

5.3 The test method has applicability in gasoline-engine-oil specifications and is expected to be used in specifications and classifications of engine lubricating oils, such as the following:

    - Specification D4485

    - ILSAC GF-6.

    - SAE Classification J183.

6. Apparatus (General Description)

  - Test Engine—The test engine is a spark-ignition, four-stroke, four-cylinder, gasoline, turbocharged, direct-injection engine with a displacement of 2.0 L. Features of this engine include variable camshaft timing, dual overhead camshafts driven by a timing chain, four valves per cylinder, and electronic direct-fuel injection. It is based on the Ford Motor Co. 2012 Explorer engine,.

  - Configure the test stand to accept the test engine. All special equipment necessary for conducting this test is listed below.

  - Use appropriate air-conditioning apparatus to control the temperature, pressure, and humidity of the inlet air to meet the requirements in Table 6.

6.4 Use an appropriate fuel supply system. A typical system is shown in Fig. 1.

Note 1—The fuel may need to be heated to maintain the fuel temperature in Table 6. As a consequence, heat may buildup in the fuel system during shutdown thereby increasing the pressure in the fuel lines. It is good practice, therefore, to include a pressure relief valve in the fuel line to relieve the pressure and to send the excess fuel back to the tank before the shutoff valve.

  - 6.5 The control and data acquisition system shall meet the requirements listed in Annex A5.

  - 6.6. Engine Cooling System:

  - 6.6.1 Use the coolant-inlet and -outlet system from OH Technologies,6. Typical plumbing for the external coolant system is shown in Figs. A6.2 and A6.3.  Use a coolant flowmeter with an accuracy of ± 1 %. Install the flowmeter at either the coolant inlet or coolant outlet sides of the engine. Install the flow-control valve in the line running from the engine-coolant outlet to the heat exchanger. ITT standard heat exchangers,6 have been found suitable. Use 38 mm (1.5 in.) pipe to plumb the coolant system. Minimize the number of elbows in the cooling system. Ensure that the engine coolant flows through the tube side of the heat exchanger.

6.6.2 A radiator cap is used to limit system pressure to 105 kPa. Motorcraft RS40 P/N D2YY-8100-A,6 has been found suitable for this application. Pressurize the coolant system to 70 kPa ± 10 kPa at the top of the coolant reservoir.

6.6.3 Control the engine-coolant flow rate and outlet temperature to meet the requirements in Table 6.

6.6.4.  Inspect engine-coolant components external to the engine every three months and clean as necessary.

  - 6.7 Oil System Components—All oil-system components in the engine are production configuration with the exception of the modified oil pan (Fig. A6.1) and oil-filter housing (Fig. A6.12).

  - 6.8 Using the production oil cooler, control the oil temperature by running process water through the water side of the oil cooler. Locations of oil-temperature thermocouples are shown in Fig. A6.12.

  - 6.9 Dynamometer—Use Midwest dynamometer model MW-1014A,6.

  - 6.10 Combustion Analysis Equipment—Use the AVL IndiSmart GigaBit 612 combustion analysis system and the AVL IndiCom combustion analysis software,6. For the latter, use the amplifier and pressure settings and the standard results settings given in A11.1.1 and A11.1.2, respectively. Report the channels shown in A11.2.

FIG. 1  Typical Fuel Supply System

  - 6.11 Fuel and Fuel System:

    - 6.11.1 System Description—Fig. 1 is a schematic diagram of a typical fuel-supply system. Supply an excess volume of fuel to the high-pressure fuel pump and fuel rail at all times. Introduce make-up fuel (that is, fuel used by the engine) into the loop from an external source. Mix the make-up fuel with fuel that is returned from the fuel rail (that is, fuel not used by the engine). Pump the fuel through a mixing chamber, or a small heat exchanger, to mix the two streams and to provide fuel of consistent temperature to the engine. Deliver the fuel to a high-pressure pump (Ford P/N AG9Z-9350-B/AG9E-9D376-AB5,6) that boosts the pressure and supplies the fuel to the fuel rail.

    - 6.11.2 Controls—Maintain the fuel temperature to the high-pressure pump at 30 °C ± 0.5 °C. To ensure good atomization of the fuel, maintain the fuel pressure to the high-pressure pump at 450 kPa ± 37 kPa. Maintain constant fuel pressure throughout the test to ensure good speed, power, and air-fuel ratio control.

    - 6.11.3 Test Fuel—Approximately 340 L of Haltermann HF2021 EPA Tier 3 EEE Lube Cert test fuel,6 are required for each test. (Warning—Flammable, health hazard.)

    - 6.11.4 Fuel Batch—Ensure each new batch of fuel is accompanied by a certificate of analysis showing that it meets the requirements shown in Table A7.1. Record the fuel batch identification number in the appropriate field in the test report.  If co-mingling fuel batches, document the most prevalent fuel batch in the test report.  There are no restrictions on the percentages of co-mingled batches but it is always a good practice to minimize the dilution.

    - 6.11.4.1 Fuel from a new batch can be added to a laboratory’s fuel tank at any time provided it meets the requirements in Table A7.1 – see also 6.11.4.2.

    - 6.11.4.2 Fuel Batch Analysis—Fuel shall be analyzed in accordance with industry standards.  Refer to the recommendations of the Fuels Task Force which is a subgroup of the ASTM D02.B0 Technical Guidance Committee.

7. Apparatus (The Test Engine)

  - 7.1 Sequence IX Test Engine—The test engine parts are available from the Ford Motor Company5,6.  A detailed listing of all parts and P/Ns is given in Annex A8.

  - 7.2 Required New Engine Parts—A new short block is required when initially referencing a stand and engine combination. This short block can be re-used provided it remains within service limits and is capable of being referenced. New crush washers and gaskets are required whenever the engine/short block is disassembled (for example, for pretest measurements or repair). New camshafts and buckets are required when first building a cylinder head. New valves are required when rebuilding a cylinder head.

  - 7.3 Reusable Engine Parts—The cylinder head can be used on subsequent short blocks as long as it remains within the service limits in the workshop manual. The parts listed in Tables A8.2, A8.6, and A8.7 can be used for multiple tests as long as they are in good condition and meet the service limits in the workshop manual.

  - 7.4 Specially Fabricated Engine Parts—The following subsections detail the specially fabricated engine parts required in this test method:

    - 7.4.1 Inlet Air System  (see Fig. A6.8)—Fabricate the inlet air system using the stock 2012 Explorer air cleaner assembly and mass air flow (MAF) sensor as detailed in Table A8.6. Install the fresh-air tube, air-cleaner assembly, and new air filter. Modify the air-cleaner assembly to accept fittings for an inlet-air-temperature thermocouple and pressure tap. Either use the 2012 Explorer fresh-air tubes or fabricate fresh-air tubes so as to provide a separation of 1,040 mm ± 25 mm from the MAF sensor to the turbocharger inlet.

    - 7.4.2 Oil Pan—Modify the stock 2012 Explorer oil pan to add an oil drain plug in one of the rear locations shown in Fig. A6.1.

    - 7.4.3 Cylinder Head—Use a modified cylinder head that allows the installation of in-cylinder pressure sensors. This engine part is available from TEI,6.

    - 7.4.4 Pressure Sensor Tubes—Install 3/8 in. OD steel tubing into the pressure sensor sleeves in the cylinder head to allow for installation of the in-cylinder pressure sensors.

    - 7.4.5 Valve Cover—Modify the stock valve cover to allow the pressure sensor tubes to protrude through the cover. Seal the location where the tubes protrude through the cover to prevent oil from leaking through the penetrations.

    - 7.4.6 Coolant Supply Manifold—To accept the coolant-in thermocouple (Fig. A6.2), use a coolant inlet purchased from OH Technolgies7,6 in place of the stock coolant inlet.

    - 7.4.7 Coolant Return Manifold—To accept the coolant-out thermocouple and provide a coolant return from the turbocharger (Fig. A6.2), use a coolant outlet purchased from OH Technologies7,6 in place of the stock thermostat housing.

7.4.8. Oil Filter Housing—Modify the oil-filter housing to accept a thermocouple on the front side of the housing, facilitating measurement of the oil temperature entering the oil cooler.

  - 7.5 Special Engine Measurement and Assembly Equipment—For assembly, use any special tools or equipment shown in the 2012 Explorer Service Manual. Complete any assembly instructions not detailed in Section 7 according to the instructions in the 2012 Explorer Service Manual. Apparatus routinely used in a laboratory or workshop are not included.

    - 7.5.1 Piston Ring Positioner—Use the piston-ring positioner to locate the piston rings down from the cylinder-block deck surface by 38 mm. This allows the compression rings to be positioned in a consistent location in the cylinder bore for the ring-gap measurement. Fabricate the positioner according to the details shown in Fig. A6.13.

    - 7.5.2 Engine Service Tools—A list of special tools for the test engine is shown in Table A8.8. The tools are designed to aid carrying out several service items, in addition to the specific service items that require special tools to perform the functions indicated (if not self-explanatory).

  - 7.6 Engine Installation on the Test Stand:

  - 7.6.1 General—Functions that are to be performed in a specific manner or at a specific time in the assembly process are noted here.

    - 7.6.2 Mounting the Engine on the Test Stand—Mount the engine on the test stand so that the flywheel friction face is 0.0° ± 0.5° from vertical.  Use two motor mounts at the rear of the engine. Quicksilver P/N 66284-A2,6 has been found suitable for this purpose (see Table A8.7). An example of a rear- mount support is shown in Fig. A6.5.  Use a rubber mount at the front of the engine attached to the front-cover mount. Examples of front-mount supports are shown in Fig. A6.4. Ensure the engine is at 0.0° ± 0.5° role angle.

    - 7.6.3 Flywheel—Obtain the modified flywheel (P/N OHTVH-006-1) from OH Technologies7,6. Lightly coat the flywheel bolts with Loctite 565 to prevent any oil from seeping out of the holes. Torque the flywheel to 108 N•m to 115 N•m.

    - 7.6.4 Clutch and pressure plate—Obtain the clutch (Sachs P/N K0047-07) from OH Technologies7,6. Put the flat side on the clutch toward the engine and put the spacer between the flywheel and pressure plate. Torque the pressure plate bolts to 25 N•m to 33 N•m. Replace the clutch and pressure plate with every new engine.

    - 7.6.5 Driveline—Grease the driveline every test. The driveline specifications are as follows:

- Driveline angle degree: 1.5° ± 0.5°;

- Installed length from flange to flange: 450 mm to 610 mm;

- 1410 series flanges; 1550 joints;

- Driveshaft stiffness: 0.1° to 0.3°/136 N•m (100 ft•lbf).  Part number MSI-41/55S-22 from Machine Services Inc. has been found to be a suitable driveshaft.

  - 7.7 Exhaust System:

  - 7.7.1 Warning—Exhaust gas is noxious. (Caution: Any leaks in the connections to the sample probes will result in erroneous readings and incorrect air-fuel ratio adjustment.)

  - 7.7.2 A typical exhaust system, with fittings for backpressure probe, oxygen (O2) sensors and thermocouple, is illustrated in Fig. A6.6.

  - 7.7.3 Construct exhaust components from either solid or bellows pipe/tubing. Other flexible pipe type is not acceptable.

    - 7.7.4 Use the backpressure probes until they become unserviceable. If the existing probes are not cracked, brittle, or deformed, clean the outer surfaces and clear all port holes. Check the probes for possible internal obstructions and reinstall the probes in the exhaust pipe.

    - 7.7.4.1 Stainless steel probes are generally serviceable for several tests; mild steel probes tend to become brittle after one test.

  - 7.8 Fuel Management System:

  - 7.8.1 Fuel Injectors—Inspect the O-rings to ensure they are in good condition and will not allow fuel leaks. Replace if necessary. Install the fuel injectors into the fuel rail and the cylinder head.

  - 7.9 Powertrain Control Module:

7.9.1 Use a  Powertrain Control Module (PCM) provided by Ford Motor Company5,6 to run this test. The PCM contains a calibration developed for this test. The PCM calibration number is U502-HBBJ0-v1-7-VEP-371.VBF.  The PCM hardware required to accept this calibration is  SPN:BB5Z-12A650-AANP, EPN: RMBB5A-12A650-AA, HWPN:BB5A-12B684-AC.

7.9.1.1 The PCM is powered either by a 13.5 V ± 1.5 V battery or an alternative power supply that does not interrupt/interfere with proper PCM operation.

7.9.1.2 Connect the PCM battery/power supply to the engine wire harness with an appropriate gage wire of the shortest practical length so as to maintain a dc voltage of 12 V to 15 V and minimize PCM electrical noise problems. Ground the PCM ground wire to the engine. From the same ground point, run a minimum 2 gage wire back to the battery negative to prevent interruption/interference of the PCM operation. The power supply can also be used for the lambda (oxygen) sensors.

  - 7.10 Spark Plugs:

  - 7.10.1 Use either Motorcraft CYFS-12-Y29 or Bosch (PN HR7Mii30T) spark plugs which come pre-gapped.  Torque the spark plugs to 9 N·m to 12 N·m.  Do not use anti-seize compounds on spark plug threads.

  - 7.11 Crankcase-Ventilation System:

  - 7.11.1 The crankcase-ventilation system is vented to the atmosphere through the port in the valve cover and is not to be connected to the inlet.

  - 7.12 Water-to-Air Turbocharger Intercooler:

  - 7.12.1 Use water-to-air intercooler capable of achieving the required air-charge temperatures in Tables 3 to 6 and an average, system-pressure loss less than 3 kPa. Type 5 or Type 52 intercoolers from Frozenboost,6 have been found suitable.

    - When cleaning the intercooler as part of normal maintenance, spray clean the air side of the intercooler with solvent, rinse with hot water and leave to air-dry. Use commercial AquaSafe descaler to clean the water-side.

  - 7.13 Intercooler Tubing

  - 7.13.1 Fabricate the inlet-air system with 51 mm internal diameter (ID), stainless steel tubing from the turbocharger to the intercooler, and 64 mm ID, stainless steel tubing from the intercooler to the throttle body. The tubing length is not specified but should be the appropriate length to achieve the required air-charge temperature in Tables 3 and 6 and an average system pressure loss less than 3 kPa.

  - 7.13.1.1  Locate the sensors for measuring the Manifold Absolute Pressure and Temperature (MAPT) in accordance with Fig. A6.9. Place the probes for measuring the post-intercooler, turbo-boost pressure, and pre-intercooler pressures, in accordance with Fig. A6.9. A typical installation is shown in Fig. A6.10.  The engine vacuum system is shown in Fig. A6.15.

  - 7.14 External Hose Replacement:

  - 7.14.1 Inspect all external hoses used on the test stand and replace any hoses that have become unserviceable. Check for internal wall separations that could cause flow restrictions. Check all connections to ensure security.

  - 7.15 Wiring Harness

  - 7.15.1 There are two wiring harnesses used on the test stand - a dynamometer harness that connects to the stand power and PCM, and an engine harness. Obtain the dynamometer and engine-wiring harnesses from OH Technolgies7,6. Diagrams of these wiring harnesses are shown in Figs A6.16 and A6.17 identifying connections.

  - 7.16 Electronic Throttle Controller:

  - 7.16.1 Control the electronic-throttle controller using signals from the simulated, accelerator-pedal position. The dynamometer wiring harness is supplied with an Accelerator Pedal Position jumper cable with un-terminated pigtail leads.

  - 7.16.1.1 Connect the two voltage command signals, Acc Pos Sensor 1 and Acc Pos Sensor 2, to the Accelerator Pedal Position jumper cable. The voltage control ranges for each signal are shown in Table 1. The wiring schematic and pin-out description for this connection are shown in Fig. 2.

  - 7.16.1.2 ACC Pos Sensor 2 shall always equal 50 %  of  Acc Pos Sensor 1.

  - 7.16.1.3 Run the voltage signals through a voltage isolator otherwise interference will occur between the laboratory digital-to-analog converter (DAC) system and the engine electronic control unit (ECU) leading to erratic throttle control.

# TABLE 1  Accelerator Position Sensor Control Ranges

| Command Signal | Operating Range, VA | Min Signal (Idle), VA | Max Signal (WOT), VA |
| --- | --- | --- | --- |
| Acc Pos Sensor 1 | 0 to 5.0 | 0.75 (15 %) | 4.25 (85 %) |
| Acc Pos Sensor 2 | 0 to V | 0.375 (15 %) | 2.125 (85 %) |

A DC

FIG. 2   Accelerator Position Wiring Schematic

  - 7.17 Water Pump and Water-Pump Drive—Install the water pump and pulley, the crankshaft pulley, and the tensioner according to the 2012 Explorer service manual. These are the only components needed to drive the water pump. All other production, front-end, accessory-drive components do not need to be installed. The engine cannot be used to drive any external engine accessory other than the water pump. Pull back the tensioner and install the water-pump drive belt as shown in Fig. 3.

# FIG. 3  Water-Pump Drive Arrangement

  - 7.18 Cylinder-block oil separator

  - 7.18.1 Install a dummy positive crankcase ventilation (PCV) valve (that is, a PCV valve with the internal components removed) in the oil separator on the side of the engine block. Measure crankcase pressure at this location.

8. Engine Preparation

8.1 Environment for Engine Buildup and Measurement Areas—The ambient atmosphere of the engine buildup and measurement areas shall be reasonably free of contaminants. Control the temperature to within ± 3 °C to ensure acceptable repeatability in the measurement of parts dimensions. To prevent moisture forming on cold engine parts that are brought into the buildup or measurement areas, maintain the relative humidity at a nominal maximum of 50  %.

  - 8.2 Engine Disassembly

  - 8.2.1 Disassemble the engine and the cylinder head according to the 2.0 L Ecoboost disassembly procedures in the Ford 2012 Explorer Shop Manual. Note the position of all the engine components to ensure they are returned to the same positions when the engine is reassembled.

  - 8.3 Cleaning Engine Components:

  - 8.3.1 Cylinder Head Preparation and Cleaning:

    - 8.3.1.1 General—Use a modified cylinder head obtained from TEI13,6.

    - 8.3.1.2 New Cylinder Heads—A new cylinder head that has been modified with pressure-transducer tubes installed, and never used in a previous Sequence IX test, shall be cleaned with Stoddard solvent before assembly. Clean all debris left from the tube installation off the cylinder head.

8.3.1.3  Used Cylinder Heads—For a cylinder head that has been modified with pressure transducer tubes installed, and has been used in a previous Sequence IX test, clean the bare cylinder head, with tubes (but no valve-train components) in an ultrasonic parts cleaner (see 8.3.1.4). Rinse parts with cleaning soap (see 9.4) before putting them into the ultrasonic cleaner.

8.3.1.4 The Cleaning Procedure:

a) The TierraTech ultrasonic cleaner, model MOT-400N,6 (capacity 400 L), has been found suitable. Add ultrasonic cleaning solution once the temperature in the ultrasonic cleaner reaches a minimum of 60 °C (140 °F). Use Brulin AquaVantage 815 GD and 815 QR-NF,6 solutions with a volume fraction of 12.5 %. Mix equal volumes of these solutions. For the TierraTech model MOT-400N, the quantities involved are 25 L of each solution.

Note 2—Quantities will be different for a different size unit.

b) After 30 min, remove the parts and immediately spray with hot water, followed by solvent and left to air dry.

8.3.2 Cleaning Other Components—As needed, spray clean the following components with solvent, then blow out with pressurized air, and leave to air dry:

- camshafts and all valve train;

- intake manifold/throttle body (unseparated);

- fuel-pump housing with piston;

- vacuum pump and oil screen;

- oil screen and the intake and outlet of the turbocharger - wipe lightly, with a rag wet with solvent. (Do not clean the inside of the turbocharger);

- carbon build up on the injectors - wipe off; variable valve timing;

- variable valve timing (VCT) solenoids;

- valve cover;

- turbocharger oil lines.

  - 8.4 Engine Measurements:

    - 8.4.1. Cylinder-Bore and Piston Measurements—See Table A9.1.

    - 8.4.1.1 Measure and record the piston-to-bore clearances at the top-, second-, and third-ring lands and the piston skirt as shown in Fig. A6.13. Use the bore ladder shown in Fig. A6.14 to determine bore diameter positions. Measure the bore in both the longitudinal and transverse directions. To determining the piston-to-bore clearance, calculate the difference between the particular piston diameter location and the average bore diameter for both the transverse and longitudinal directions.

    - 8.4.1.2 Measure and record ring side clearances for the upper and lower compression rings (UCR, LCR). Determine ring side clearance by taking four measurements 90° apart. Either check clearance with a thickness gauge or by measuring the difference between the thickness of the ring and the height of the corresponding groove.

8.4.1.3 Measure and record ring tension. Obtain ring tension measurements from Test Engineering, Inc.13,6.

8.4.2  Cylinder-head Measurements—See Table A9.2.

8.4.2.1 To determine the valve stem-to-guide clearance, measure the diameter of the valve stem at 38 mm from the tip of the valve, and the valve guide at 19.5 mm from the top of the valve guide.

8.4.2.2 For the intake- and exhaust-valve springs, measure and record the spring free length and spring tension at a compressed height of 28.7 mm. Verify the compressed spring tension is 460 N ± 21 N. Reject any springs not meeting this criteria.

8.4.2.3  Set the valve lash according to the procedure in the workshop manual and record the valve lash.

  - 8.5 Miscellaneous Engine-Components Preparation:

8.5.1 Environment for Engine Buildup and Measurement Areas—The ambient atmosphere of the engine buildup and measurement areas shall be reasonably free of contaminants. Control the temperature to within ± 3 °C to ensure acceptable repeatability in the measurement of parts dimensions. To prevent moisture forming on cold engine parts that are brought into the buildup or measurement areas, maintain the relative humidity at a nominal maximum of 50 %.

    - Throttle Body:

      - Clean the butterfly and bore of the throttle body with Berryman Chemtool B12,6 carburetor cleaner and air-dry before each test. Do not disassemble the throttle body as this will cause excessive wear on the components. The idle air screw can be removed for the cleaning process. Fully close the idle air screw during test operation.

      - There is no specific life for the throttle body. However, the clearance between the bore and the butterfly will eventually increase and render the body unserviceable. When the clearance becomes too great to allow control of speed, torque, and air-fuel ratio, discard the throttle body.

  - 8.6 Engine Assembly:

  - 8.6.1 Assemble the engine according to the 2.0 L Ecoboost assembly procedures in the 2012 Explorer Shop Manual, except as noted in Section 7.  Ensure all components (that is, pistons, rings, bearings, etc.) are replaced in the same positions used originally when assembled at the factory.

    - Sealing Compounds—Use a silicon-based sealer, as needed, on the contact surfaces between the rear-seal housing and oil pan and the front cover and cylinder block, cylinder head and oil pan.  Use Motorcraft Gasket Maker (TA-16)9,6 or equivalent between the 6th intake and exhaust camshaft cap and the cylinder head. Use silicon-based sealer sparingly since it can elevate the indicated silicon content of the used oil.

Note 3—Non-silicon liquid or tape thread sealers may be used on bolts and plugs.

    - Gaskets and Seals—Install new gaskets and seals during engine assembly.

  - 8.7  Cylinder Head Assembly:

    - 8.7.1 Cylinder heads may be used as long as they remain within service specifications. Refer to the 2012 Explorer Service Manual.

    - 8.7.2 Replace the valves on cylinder heads reused on another engine block.

    - 8.7.3 If a cylinder head is removed from an engine block ahead of schedule due to broken pistons, short-block failure, or lack of test severity, the laboratory may reuse the cylinder head without replacing the valves provided they are within service limit.

    - 8.7.4 Assemble the cylinder heads in accordance with the service manual.  Lap the valves before installation and install new intake- and exhaust-valve seals. Set the valve lash in accordance with the procedure in the workshop manual and record the valve lash.

    - 8.7.5 Vacuum check the valve ports before use.

  - 8.8 Engine Installation on Test Stand—Install the engine onto the stand as described in 7.6.2. Install all engine components external to the long block according to the 2.0L Ecoboost assembly procedures in the 2012 Explorer Shop Manual, where applicable. Connect the engine to all external laboratory systems identified in Section 6, in accordance with laboratory procedures.

  - 8.9 Pressure-Sensor Installation—Once the sensor tubes and modified valve cover are installed (see 7.4.4 and 7.4.5), install pressure sensors into the pressure-sensor tube using the AVL type TT21 sensor-installation mounting tool (P/N TIWG0214A.01). Torque the sensors to 1.5 N·m.

  - 8.10 New-Engine Break In—Once a new engine has been installed on the test stand, perform the eight-hour break-in procedure shown in Table 2 using oil TMC 220.

# TABLE 2 Sequence IX Eight-Hour, Break-In Procedure

| Step | Engine speed, r/min | Engine torque, N•m | Time per stage, h:min | Total Time, h:min |
| --- | --- | --- | --- | --- |
| Install new oil filter and charge engine with 4.2 kg of new oil |  |  |  |  |
| 1 | 1000A | 0 | 0:30 | 0:30 |
| Oil change 1: Shut engine down, drain used oil, and remove oil filter. Allow oil to drain for 20 min. Install new oil filter and add 4.2 kg of new oil. |  |  |  |  |
| Start engine and idle for 5 min |  |  |  |  |
| 2 | 1500 | 38 | 0:30 | 1:00 |
| 3 | 2000 | 72 | 0:30 | 1:30 |
| 4 | 2500 | 111 | 0:30 | 2:00 |
| 5 | 3000 | 135 | 0:30 | 2:30 |
| 6 | 3000 | 150 | 3:15 | 5:45 |
| 7 | 2000 | 72 | 0:15 | 6:00 |
| 8 | 3250 | 155 | 0:15 | 6:15 |
| 9 | 3500 | 155 | 0:15 | 6:30 |
| 10 | 3750 | 155 | 0:15 | 6:45 |
| 11 | 4000 | 155 | 1:15 | 8:00 |
| Bring engine to idle speed for 5 min, then shut down |  |  |  |  |
| Oil change 2: Drain used oil and remove oil filter. Allow oil to drain for 20 min. Install new oil filter and add 4.2 kg new oil. |  |  |  |  |

A Idle speed.

  - 8.10.1 The controlled quantities during the break-in are listed in Table 3. All other controls are left wide open or free flowing. The engine does not produce enough heat in the early steps to reach all target temperatures. All controlled quantities shall be on target at the beginning of Step 4.

# TABLE 3  Sequence IX Controlled Quantities for the Eight-Hour Break-in

| Quantity, unit | Controlled value |
| --- | --- |
| Coolant-out temperature, °C | 85 |
| Oil-gallery temperature, °C | 100 |
| Inlet-air pressure, kPa (gauge) | 0.05 |
| Air-charge temperature, °C | 37 |
| Inlet-air temperature, °C | 30 |
| Humidity, g/kg | 11.4 |
| Fuel pressure, kPa | 450 ± 37 |
| Coolant flow rate | Valve wide open |

8.11 Temperature Measurements:

8.11.1 General:

8.11.1.1 Temperature measurement locations are specified in 8.11.4.

8.11.1.2 Use thermocouples that can be calibrated with an accuracy of ± 0.5 °C. Use Ford-specified temperature sensors for PCM inputs.

8.11.2  Equipment:

8.11.2.1 Use premium, sheathed thermocouples in all cases except the intake-air thermocouple which may be an open-tip type. Use thermocouples with a diameter of 3 mm.  Locate all thermocouples in the center of the stream.

8.11.2.2 Thermocouples, wires, and extension wires shall be matched to perform in accordance with the special limits of error as defined in ANSI MC96.1.

8.11.3 Calibration—Refer to Table 4 for calibration interval of thermocouples. The temperature-measurement system shall indicate within ± 0.5 °C of the laboratory calibration standard. The calibration standard shall be traceable to NIST.

8.11.4 Locations for Engine-Temperature Sensors:

8.11.4.1 Engine-Coolant Inlet—Install the sensor in the coolant inlet on the engine (P/N OHTVH-008-17,6) perpendicular to the run. Install sensor with the tip in the center of the stream of flow (see Fig. A6.2).

8.11.4.2 Engine-Coolant Outlet—Install the sensor in the coolant outlet on the engine (P/N OHTVH-009-17,6) perpendicular to the run. Install sensor with the tip in the center of the stream of flow (see Fig. A6.2).

8.11.4.3  Engine-Oil Gallery—Install the tip of the sensor at the center of the flow stream in the external, oil-filter adapter (see Fig. A6.12) through the hole for the oil-pressure switch (which is not used). Install a tee to accept this temperature sensor and attach the oil-pressure line.

8.11.4.4 Engine-Oil-Filter In—Install the tip of the sensor at the center of the cross fitting attached to the side opposite from the engine-oil-inlet temperature sensor on the oil-filter adaptor. Modify the adapter with a 1/8 in. NPT hole to access the oil passage (see Fig. A6.12).

8.11.4.5  Inlet Air—Install the tip of the thermocouple midstream in the air-cleaner box downstream of the filter (see Fig. A6.8). Insertion depth shall be 37 mm ± 2 mm.

8.11.4.6 Fuel—Install the sensor in the low-pressure fuel line no more than 155 mm from the high-pressure pump.  Use an appropriate size “T” fitting to ensure the sensor and fitting do not interfere with the fuel flow (see Fig A6.7).

8.11.4.7 Air Charge—Install the sensor in the intercooler outlet tube 25 mm ± 2 mm downstream from the MAPT sensor (see Fig A6.9).

8.11.4.8 Exhaust—Install a sensor 140 mm ± 12 mm downstream on the exhaust flange (see Fig. A6.6).

8.11.4.9 Oil Sump—Measurement of oil-sump temperature is optional.

8.12 Pressure Measurements:

8.12.1 General—Pressure measurement locations are specified in 8.12.4.

8.12.2  Equipment—The accuracy and resolution of the pressure-measurement sensors and the complete pressure-measurement system shall meet the requirements of the Data Acquisition and Control Automation II (DACA-II) Task Force Report21.  Replace pressure sensors that are part of the PCM system with Ford-specified equipment.

Note 4—Tubing between the pressure-tap locations and the final pressure sensors should incorporate condensate traps, as indicated by good engineering practice. This is particularly important in applications where low, air pressures are transmitted by means of lines which pass through low-lying trenches between the test stand and the instrument console.

8.12.3 Calibration—Refer to Table 4 for calibration interval for pressure sensors. Pressure- measurement systems shall conform to the guidelines in DACA-II Task Force Report21. The calibration standard shall be traceable to NIST22.

8.12.4 Locations for Pressure-Measurement Sensors:

8.12.4.1 Intake Manifold—Measure intake-manifold pressure (MAP) at the port downstream of the throttle body on the intake manifold (see Fig. A6.9)

8.12.4.2 Engine-Oil Gallery—Measure oil-pump pressure in the external oil-filter adapter (see Fig. A6.11) through the hole for the oil-pressure switch (not used). Install a tee to accept the temperature sensor and attach the oil-pressure line.

8.12.4.3 Coolant Pressure—Measure engine-coolant-out pressure at the top of the coolant reservoir as shown in Fig. A6.18. Control to 70 kPa ± 2 kPa.

8.12.4.4 Fuel—Measure fuel pressure in the lower pressure fuel line at the exit of the stand fuel pump.

8.12.4.5 Crankcase—Measure crankcase pressure at the dummy positive crankcase ventilation (PCV) valve in the cylinder-block oil separator.

8.12.4.6 Exhaust Back-Pressure—Measure the exhaust back-pressure with the exhaust-gas sampling probe located 76 mm ± 12 mm downstream of the exhaust flange (see Fig. A6.6). A sensor capable of absolute or gauge measurement corrected with barometric pressure reading is recommended. Install a condensate trap between the probe and sensor to accumulate water present in the exhaust gas.

8.12.4.7 Inlet Air—Measure inlet-air pressure in the air-cleaner box downstream of the air filter (see Fig A6.8).

8.12.4.8 Pre-Intercooler—Measure the pre-intercooler pressure with the sampling probe located 155 mm ± 50 mm downstream of the turbocharger flange (see Fig A6.9).

8.12.4.9 Boost Pressure (Post-Intercooler)—Measure the boost pressure with the sampling probe located downstream of the intercooler and at least 305 mm upstream of the MAPT sensor (see Fig A6.9).

8.12.4.10. Cylinder Head Oil—Measure cylinder-head oil pressure at the oil-gallery plug on the left side of the cylinder head next to the belt tensioner (see Fig A6.19).

8.13  Flow-Rate Measurements:

8.13.1 General—With the exception of engine coolant, equipment for measuring the flow rate for the four required quantities is not specified. This provides opportunity for adaptation of existing test-stand instrumentation (see X1.4.5 for suitable mass-flow meters).

8.13.2  Engine Coolant—Determine coolant flow rate using a flowmeter with an accuracy of ± 1 % (see Fig. A6.3). A suitable flowmeter is available from Micromotion (Emerson),6, model Number R200SA418NCAMEZZZZ.    Take precautions to prevent air pockets from forming in the lines to the flow meter. Transparent lines or bleed lines, or both, are beneficial in this application. Ensure that the manufacturer’s requirement for orientation and straight sections of pipe are installed immediately up- and down-stream of the flowmeter.

8.13.3  Calibration— Refer to Table 4 for the calibration interval of flow-rate measurements. Calibrate the engine-coolant flowmeters at 55 L/min and 95 ºC coolant-outlet temperature.

8.13.4 Locations for Flow-Rate Measurements:

8.13.4.1  Engine Coolant—Install the flowmeter at either the coolant inlet or outlet sides of the engine.

8.13.4.2 Fuel—Measure fuel flow rate in kg/h on the low-pressure, fuel system before the high-pressure, engine-fuel pump.

8.14 Humidity Measurement—Condition the intake air to 11.4 g/kg ± 0.8 g/kg humidity.  The test stand intake-air duct system is not specified.

8.15 Lambda  Sensor Calibration—Use the manufacturer’s calibration requirements for the O2 sensor.

8.16 In-cylinder Pressure Measurement—Use the manufacturer’s calibration requirements for the in-cylinder pressure sensors. Refer to Table 4 for the calibration interval.

8.17  Crank-angle Measurement—Use the manufacturer’s calibration requirements for the crankangle encoder. Refer to Table 4 for the calibration interval.

8.18  Charge Amplifier—Use the manufacturer’s calibration requirements for the charge amplifier. Refer to Table 4 for the calibration interval.

8.19  Load Cell—Calibrate the load cell before every reference test.

# TABLE 4 Instrumentation Calibration Periods

| Instrument Type | Section | Calibration Period |
| --- | --- | --- |
| Load cell | 8.19 | Prior to every reference test |
| Thermocouples | 8.11 | Every 3 mo Every 3 mo Every 3 mo |
| Pressure sensors | 8.12 |  |
| Flow meters | 8.13 |  |
| In-cylinder pressure sensors | 8.16 | Every 300 h |
| Charge amplifier | 8.18 | Manufacturer’s recommendation |

9. Reagents and Materials

9.1 Solvents and Cleaners Required—No substitutions are allowed. (Warning—Use adequate safety provisions with all solvents and cleaners.)

9.1.1 Solvent—Use only mineral spirits (for example, Stoddard Solvent) meeting the requirements of Specification D235, Type II, Class C for volume fraction of aromatics 0 % to 2 %, flash point 61 °C minimum, and color not darker than +25 on Saybolt Scale or 25 on Pt-Co Scale. (Warning—Combustible. Health hazard.) Obtain a Certificate of Analysis for each batch of solvent from the supplier.

9.1.2 Organic Solvent—Use solvent conforming to 9.1.1.

9.1.3 Ultrasonic Cleaner—Use only Brulin AquaVantage 815 GD and 815 QR-NF19,6.

9.1.4 Carburetor Cleaner—Use Berryman Chemtool B1220,6.

    - 9.2 Test Fuel—Approximately 340 L of Haltermann HF2021 EPA Tier 3 EEE Lube Cert test fuel12,6 are required for each test. (Warning—Flammable, health hazard.)

9.3 Sealing Compound—Loctite 565,6 or Motorcraft gasket maker TA-16 silicon-based sealer.

9.4 Parts Cleaning Soap—Commercial laundry detergent. Tide,6 has been found suitable for this purpose.

10. Calibration and Standardization

10.1 General:

10.1.1 Annex A2 describes calibration procedures using the TMC reference oils, including their storage and conditions of use, the conducting of tests, and the reporting of results. Determine the acceptability of a reference oil according to the Lubricant Test Monitoring System (LTMS).

10.1.2 Annex A3 describes general maintenance activities involving TMC reference oils, including special reference oil tests, special use of the reference oil calibration system, donated reference oil test programs, introducing new reference oils, and TMC information letters and memoranda.

10.1.3 Annex A4 provides general information regarding new laboratories, the role of the TMC regarding precision data, and the calibration of test stands used for non-standard tests.

10.2 Activities specific to the Sequence IX :

10.2.1 Verify the calibration of test stands with reference oils supplied by the TMC (see 10.2.2). Consult Annex A2 prior to attempting calibration of a new stand. Stand calibration tests are normally conducted upon expiration of either the 90 d calibration time period, after completing five non-reference oil tests, or 150 engine hours at the start of the test. Calibration time periods may, however, be adjusted by the TMC. Any non-reference oil test started within 90 d of the previous calibration test and with less than 150 engine hours at the start of test is considered within the calibration period, provided the 5 allowed non-reference oil tests that have been completed since the previous calibration test in the stand are not exceeded.

10.2.2  The TMC provides a reference oil sample of 22.4 L for each stand calibration test.

10.3  Unacceptable Calibration Results:

10.3.1  It is recognized that a certain percentage of calibration tests fall outside the acceptance limits because of the application of statistics in the development of the acceptance limits. Failure of a reference oil test to meet ei (prediction error) or Zi (exponentially weighted moving average) control chart limits can be indicative of a false alarm or a stand, laboratory, or industry problem. When this occurs, the laboratory, in conjunction with the TMC, shall attempt to determine the problem source. The TMC may solicit input from industry expertise (other testing laboratories, the test sponsor, ASTM Technical Guidance Committee, Sequence IX Surveillance Panel, and so on) to help determine the cause and extent of a problem. The Sequence IX Surveillance Panel adjudicates industry problems.

10.3.2  If the TMC determines the problem is a false alarm and is stand-related, there is no impact on other non-reference tests running in other stands within the laboratory. If the TMC determines the problem is laboratory-related, non-reference tests run during the problem period shall be considered invalid, unless there is specific evidence to the contrary for each individual test.

10.3.3  The TMC reschedules a calibration test once it is satisfied that no particular problem exists or the problem has been resolved. The laboratory shall provide adequate documentation to support conclusions reached during this process. Attach this documentation to the acceptable calibration test report. It shall provide sufficient information to show how the problem related to other tests operated during the same period.

10.4  Test Stand Modifications—A nonstandard test includes any test completed under a modified procedure requiring hardware or controller modifications to the test stand. The TMC determines whether another calibration test is necessary after the modifications have been completed.

10.5  Test Numbering System:

10.5.1  Acceptable Tests—The test number shall follow the format AAA-BB-CCCC-DDD where AAA represents the test stand number, BB represents the number of tests on the stand, CCCC represents the engine number, and DDD represents of tests on the engine. As an example, 6-102-32-5 represents the 102nd test on Stand 6 and the 5th test on engine number 32. Consecutively number all tests on a given stand and engine.

10.5.2  Unacceptable or Aborted Tests—If a calibration test is aborted or the results are outside the acceptance limits, the DDD portion of the test number for subsequent calibration test(s) shall include a letter suffix. The completion of any amount of operational time on tests will cause the test number to increase by one.

10.5.3  Re-reference the engines once removed from the test stand and re-installed, even if the test number and time criteria are met by the engine. Laboratories shall inform the TMC with a written explanation when a test engine is removed from a test stand and installed onto another test stand. Calibrate engines moved from one stand into another test stand as a new stand/engine.

11.  Test Procedure

11.1 Oil- Flush Procedure—For each new test, use the test oil to perform two oil flushes as follows:

11.1.1 Install a new oil filter, charge engine with 4.2 kg of new oil, and carry out the steps shown in Table 5.

# TABLE 5  Oil-Flush Procedure

| Step | Time per stage, h:min | Total Time, h:min | Ramp Time, h:min | Engine speed, r/min | Engine torque, Nm |
| --- | --- | --- | --- | --- | --- |
| 1 | 0:02 | 0:02 | - | Idle | 0 |
| 2 | 0:15 | 0:17 | 0:02 | 2000 | 70 |
| 3 | 0:02 | 0:19 | 0:02 | Ramp to idle | 0 |

11.1.2 Repeat 11.1.1.

11.1.3 During the whole of the oil-flush procedure, control to the conditions shown in Table 6.

11.1.3.1 The oil-gallery temperature shall reach 95 ºC within 30 min.

# TABLE 6 Oil-Flush-Procedure Conditions

| Controlled Quantity, unit | Set Point |
| --- | --- |
| Coolant-out temperature, °C | 95 |
| Oil-gallery temperature, °CA | 95 |
| Air-charge temperature, °C | 43 |
| Inlet-air temperature, °C | 30 |
| Inlet-air pressure, kPa (gauge) | 0.05 |
| Exhaust back pressure, kPa (absolute) | 104 |
| Humidity, g/kg | 11.4 |
| Fuel pressure, kPa | 450 ± 37 |

A See 11.1.3.1

11.2 Oil-Conditioning Procedure:

11.2.1 General—Prior to initiating the test cycle, condition the test oil as described in this section.

11.2.2 Install a new oil filter, charge engine with 4.2 kg of new oil, and carry out the steps shown in Table 7.

# TABLE 7. Oil-Conditioning Procedure

| Step | Time per stage, h:min | Total itme, h:min | Ramp time, min | Engine speed, r/min | Engine torque, Nm | Coolant temp., °C | Oil-gallery temp., °C | Air-charge temp., °C |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1A | 0:02 | 0:02 | - | idle | 0 | 95 | 95 | 43 |
| 2 | 0:15 | 0:17 | 1B | 2000 | 100 | 95 | 95 | 43 |
| 3 | 1:00 | 1:17 | 1 | 1750 | 269 | 95 | 95 | 43 |
| 4 | 0:15 | 1:32 | 1B | 1750 | 50 | 45 | 45 | 30 |
| B | 0:02 | 1:34 | 1 | idle | 0 | 45 | 45 | 30 |

A Targets are not expected to be reached during step.

B For coolant and oil-gallery temperatures, the ramp times amount to 15 min.

11.2.3 At the end of Step 5, shut-down the engine for a minimum of 10 min.

11.2.4 Take oil dip and inspect the engine and the test stand for oil leaks and any obvious damage.  If the level on the stock dipstick is at the minimum level or below, investigate the cause and rectify.

11.2.5 During the whole of the oil-conditioning procedure, control to the conditions shown in Table 8.

# TABLE 8 Oil-Conditioning Procedure and Test Cycle Conditions

| Controlled Quantity, unit | Set Point |
| --- | --- |
| Inlet-air temperature, °C | 30 ± 0.5 |
| Inlet-air pressure, kPa (gauge) | 0.05 ± 0.02 |
| Exhaust back pressure, kPa (absolute) | 104 ± 2 |
| Humidity, g/kg | 11.4 ± 0.5 |
| Fuel pressure, kPa | 450 ± 37 |
| Coolant flow, L/min | 55 ± 2 |
| Coolant Pressure, kPa | 70 ± 2 |
| Fuel temperature, °C | 30 ± 0.5 |

11.3 Test Cycle—For one complete test, carry out the test cycle shown in Table 9 until four valid iterations have been recorded (see 11.3.5). Each cycle is referred to as one iteration, the four cycles being denoted as iterations A, B, C and D.

11.3.1 Step 3 consists of two parts: 20 min to reach the conditions shown in Step 3a and 5 min to stabilize at the conditions shown in Step 3b.

# TABLE 9 Test Cycle

| Step | Time per stage, h:min | Total time, h:min | Ramp time, min | Engine speed, r/min | Engine torque, Nm | Coolant temp., °C | Oil-gallery temp., °C | Air-charge temp., °C |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0:02 | 0:02 | - | idle | 0 | (95)E | (95)E | (43)E |
| 2 | 0:15 | 0:17 | 1A | 2000 | 100 | 95 | 95 | 43 |
| 3aB | 0:20 | 0:37 | 1 | 1750 | 269 | 95 | 95 | 43 |
| 3bB | 0.05 | 0.42 | 0 | 1750 | 369 | 95 | 95 | 43 |
| 4C | ~3:20 | 4:02 | 1 | 1750 | 269 | 95 | 95 | 43 |
| 5 | 0:15 | 4:17 | 1A | 2000 | 50 | 45 | 45 | 30 |
| 6D | 0:02 | 4:19 | 1 | idle | 0 | 45 | 45 | 30 |

A For coolant and oil-gallery temperatures the ramp times amount to 15 min.

B See 11.3.1

C See 11.3.2.

D See 11.3.3.

E values in parentheses are targets but likely unreachable during the step indicated.

11.3.2 Record in Step 4 the combustion analysis data using AVL IndiCom for 175,000 combustion cycles (see Annex A11 for combustion analysis settings).

11.3.3  During the idle Step 6 take oil sample as follows:

11.3.3.1 Take a 150 mL purge sample followed by a 60 mL sample.

11.3.3.2 Retain the 30 mL oil sample for analysis.

11.3.3.3 Shut-down the engine and return the 150 mL purge sample.

11.3.3.4 Leave engine down for a minimum of 10 min.

11.3.3.5 Take oil dip and inspect engine and stand for oil leaks and any obvious damage.

11.3.3.6 Oil level should be above the minimum indicator on the dip stick.  If the oil is below the minimum indicator, troubleshoot the cause, and document the cause in final test report.

    - During the whole of the test cycle, control to the conditions shown in Tables 8 and 9.

    - Carry out the whole test cycle until four valid iterations have been recorded.  If 27 h of test time have been reached before four valid iterations have been obtained, the test is invalid.  Test time is accumulated at test conditions only (Step 4 in Table 9).

    - If 48 h of downtime have been reached before four valid iterations have been obtained, the test is invalid.  Downtime begins to accumulate 2 h after an iteration has finished (Step 4 in Table 9).  Outside of this 2 h window, downtime accumulates any time the test is not in Step 4 of Table 9.

11.3.7 Iteration Validity Requirements—for an iteration to be valid, the following conditions shall be met:

- at least 170,000 valid engine cycles per cylinder;

- all controlled parameters in Table A5.2 have a positive final QI.

11.3.8 Record the operational summary for each iteration A through D on Forms 5 to 8 of the Report Forms (see Annex A12). Enter the number of valid cycles, up to 175,000, run during the iteration.  Enter the number of invalid cycles.  The number of valid cycles minus the number of invalid cycles shall be greater than or equal to 170,000 for the iteration to be valid.  If the number of valid cycles is greater than 170,000, use only the first 170,000 cycles to calculate the number of events for that iteration.

  - End of Test:

11.4.1 Engine shut-down—Shut-down the engine as follows:

11.4.1.1 Turn-off the fuel supply.

11.4.1.2 Turn-off the chilled and process water.

11.4.1.3 Shut-off or remove air-intake supply.

11.4.1.4 Once the engine-oil temperature is less than 80 °C, drain the oil from the engine for at least 20 min.

- 12. Determination of Test Results

12.1 Steps for Calculating Low-Speed Preignition (LSPI) Cycles:

12.1.1 General:

12.1.1.1 The AVL combustion analysis equipment and the AVL IndiCom software are used to identify preignition events.

12.1.1.2 The procedure described in this section is intended to be used to evaluate complete test iterations between 170,000 and 175,000 valid engine cycles. If the test iteration does not contain at least 170,000 engine cycles, the iteration is invalid – see 12.2.2.4.

12.2 Removal of Invalid Cycles:

12.2.1 General—To determine combustion cycle validity, each cylinder is evaluated separately. Invalid combustion cycles are removed from each cylinder’s data set prior to performing the LSPI calculations for peak pressure (denoted by PP or PMAX – see Note 5) and mass fraction burn at 2 % (MFP2).

Note 5—The symbols PP and PMAX are used interchangeably throughout this method to denote the peak pressure. PMAX is used by AVL (see A11.2) and PP is used in section 12 and Forms 11 to 15 of the Report Forms (see Annex A12).

Note 6—MFB2 is the engine crankshaft angle, in , measured when 2 % of the mass fraction of fuel has been burned during a combustion cycle.

12.2.2 Use the following criteria to identify invalid cycles:

12.2.2.1. Remove all cycles with a MFB2 < -30°.

12.2.2.2 Remove all cycles with a PP < 2 MPa.

12.2.2.3 After all invalid MFB2 and PP cycles have been removed (see 12.2.2.1 and 12.2.2.2), remove all cycles with a pressure minimum voltage (PMINV) less than the mean of remaining PMINV - 0.5 V. For example, if the mean PMINV of the remaining engine cycles on cylinder 1 is -8.02 V, remove all cycles with PMINV < -8.52 V.

12.2.2.4 Once all invalid cycles are removed, proceed to 12.3 using only the first 170,000 valid cycles on any cylinder. If there are fewer than 170,000 valid engine cycles on any one cylinder, the iteration is considered invalid. Record the iteration as invalid and report the number of engine cycles run, along with the total number of invalid engine cycles in the test report.

12.3 Abnormal PP Cycles—Remove abnormal PP cycles individually for each cylinder as follows:

12.3.1 Remove obvious outliers.

Note 7—The mathematical method of estimating quantiles decreases in accuracy the further from normality so obvious outliers should be eliminated prior to proceeding.

# 12.3.1.1 Remove PP > 9 MPa (it is assumed that any cycle with PP > 9 MPa is an outlier).

12.3.2 Calculate the following quantities for the remaining results:

12.3.2.1 Mean (M).

12.3.2.2 Standard deviation (S).

12.3.2.3 Skewness (G), defined as:

G=nn-1n-2i=1nxi-xS3                                         (1)

12.3.2.4 Kurtosis (K), defined as:

K=nn+1n-1n-2n-3i=1nxi-xS4-3n-12n-2n-3                   (2)

12.3.3 Determine the number of standard deviations for the distributions subject to skewness and kurtosis corresponding to the 5 standard deviations that are appropriate for a valid normal distribution.

12.3.3.1 Simultaneously solve for B, C and D in Eqs (3), (4), and (5) using the values for G and K determined in 12.3.2.3 and 12.3.2.4, respectively:

1 = B2 + 2C2 + 6BD + 15D2						(3)

G = 8C3 + 6B2C + 72BCD + 270CD2 				 (4)

K = 3B4 + 60 B2C2 + 60C4 + 60B3D + 936BC2D + 630B2D2 + 4500C2D2 + 3780BD3 + 10395D4 – 3 	      (5)

Of the multiple solution sets possible for B, C, and D, only the set which has monotonically increasingly quantile mapping is acceptable [as Eq (9a) shows, F increases as Z increases]. Values of G and K that satisfy the following two inequalities lead to acceptable solutions:

K ≥ 1.4207293092995221G2 + 0.4563229601239591G + -0.2875094732604543         (7)

K ≥ 1.4180657316954324G2 + -0.4579764479129402G + -0.2886544863701676     (8)

# 12.3.3.2 Then calculate F, an estimate of the quantile corresponding to Z = 5:

F = -C +BZ +CZ2 + DZ3                                     (9a)

= -C +B(5) + C(52) + D(53)                             (9b)

Note 8—F will generally be on the order of 5 to 10 on the first iteration and 5 to 7 on the last iteration.

12.3.4 Omit those cycles with PP > M + FS, which are outliers.

12.3.5 If no outliers are found in 12.3.4, the process is complete. If outliers are found in 12.3.4, repeat steps 12.3.3.1 through 12.3.4 until no new outliers are found.

12.3.6 Record the total number of outliers from 12.3.1.1 and 12.3.4.

12.4 Abnormal MFB2 Cycles—Remove abnormal MFB2 cycles individually for each cylinder as follows:

12.4.1 Remove obvious outliers (see Note 7).

12.4.1.1 Remove MFB2 < 0. (It is assumed that any cycle with a MFB2 < 0 is an outlier.)

12.4.2 Calculate M, S, G, and K (see 12.3.2) for the remaining results.

12.4.3 Determine the number of standard deviations for the distributions subject to skewness and kurtosis corresponding to the -5 standard deviations that are appropriate for a valid normal distribution.

# 12.4.3.1 Simultaneously solve for B, C and D in Eqs (3), (4), and (5) using the values for G and K determined in 12.4.2.

12.4.3.2 Then calculate F, an estimate of the quantile function corresponding to Z = -5.

F = -C +BZ +CZ2 + DZ3                                      (10a)

= -C +B(-5) + C(-52) + D(-53)                           (10b)

Note 9—F will generally be on the order of -4 to -10 on the first iteration and -4 to -7 on the last iteration.

Of the multiple solution sets possible for B, C, and D, only the set which has monotonically increasingly quantile mapping is acceptable (as Eq (10a) shows, F increases as Z increases). Values of G and K that satisfy the inequalities in Eqs (7) and (8) lead to acceptable solutions.

12.4.4 Omit those cycles with MFB2 < M + FS which are outliers.

12.4.5 If no outliers are found in 12.4.4, the process is complete. If outliers are found in 12.4.4, repeat steps 12.4.3.1 through 12.4.4 until no new outliers are found.

12.4.6 Record the total number of outliers from 12.4.1.1 and 12.4.4.

12.5 Report LSPI Cycles:

12.5.1 On Form 11 of the Report Forms (see Annex A12), report the following data for each cylinder for each iteration A through D:

12.5.1.1 Total number of combined LSPI cycles. An LSPI cycle is defined as any combustion event containing both PP and MFB2 outliers.

# 12.5.1.2 Total number of combustion cycles containing only a PP outlier.

12.5.1.3 Total number of combustion cycles containing only a MFB2 outlier.

# 12.5.1.4 Number of invalid cycles.

12.6 Record the controlled, monitored and controller area network (CAN) bus data listed in Table 11 at a rate of 1/sec. See Annex A10 for data acquisition addresses for the CAN bus data.

12.6.1 Report CAN bus data for the four iterations A through D (see 11.3), on Forms 9 and 10 of the Report Forms (see Annex A12).

12.7 Calculation of LSPI Events—At the end of each 175,000 cycle run, calculate the number of LSPI events as described in this section using the following data from the AVL IndiCom combustion software to determine iteration validity:

a) PP (see Note 5);

b) MFB2;

- Pressure minimum voltage (PMINV).

12.7.1 For each iteration A through D, on Forms 12 through 15 of the Report Forms, report cylinder number, cycle number, PP, MFB2 and type of combustion event for each abnormal combustion cycle identified in sections 12.3 and 12.4.

12.7.1.1 An abnormal combustion event is defined as follows:

a) PP only;

b) MFB2 only;

c) both PP and MFB2 (this is defined as an LSPI event).

12.8 Calculation of Average Number of Preignition Events (AvPIE)—Report on Form 4 of the Report Form (see Annex A12) the total number of LSPI events for each iteration A through D (see 11.3). Calculate the average number of events for these four iterations and report as AvPIE.

12.8.1 If Severity Adjusted or Industry Corrected final AvPIE values are less than zero, report the final AvPIE as zero.

# Table 11. Recorded Test Points

|  | Test Point | Units |
| --- | --- | --- |
|  | Engine speed | r/min |
|  | Engine torque | N•m |
|  | Coolant-out temperature | ° C |
|  | Oil-gallery temperature | ° C |
|  | Air-charge temperature | ° C |
| Controlled | Inlet-air temperature | ° C |
|  | Inlet-air pressure (gauge) | kPa |
|  | Exhaust back pressure (absolute) | kPa |
|  | Fuel temperature | ° C |
|  | Inlet-air humidity | g/kg |
|  | Coolant flow rate | L/m in |

|  | Fuel flow rate | kg/h |
| --- | --- | --- |
|  | Intake-manifold press ure (absolute) | kPa |
|  | Air-charge pressure (absolute) | kPa |
|  | Barometric pressure (absolute) | kPa |
|  | Oil-gallery pressure (gauge) | kPa |
|  | Oil-head pressure (gauge) | kPa |
|  | Oil-filter-In temperature | ° C |
| Monitored | Exhaust temperature | ° C |
|  | Crankcase pressure (gauge) | kPa |
|  | Fuel pressure (gauge) | kPa |
|  | Power | kW |
|  | Pre-intercooler air pressure (absolute) | kPa |
|  | Ambient temperature | ° C |
|  | Coolant-in temperature | ° C |
|  | Oil-Sump Temperature | ° C |
|  | Equivalence ratio () | dimensionless |

|  | Ignition timing advance for #1 cylinder | ° |
| --- | --- | --- |
|  | Absolute throttle position | % |
|  | Engine-coolant temperature | ° C |
|  | Inlet-air temperature | ° C |
|  | Equivalence ratio () | dimensionless |
| PCM CAN bus | Absolute load value | % |
| channels | Intake-manifold pressure (absolute) | kPa |
|  | Fuel-rail pressure (gauge) | kPa |
|  | Accelerator-pedal position | % |
|  | Boost pressure - raw value (absolute) | kPa |
|  | Turbocharger wastegate duty cycle | % |
|  | Actual intake (A) camshaft position | ° |
|  | Actual exhaust (B) camshaft position | ° |
|  | Intake (A) camshaft position actuator duty cycle | % |
|  | Exhaust (B) camshaft position actuator duty cycle | % |
|  | Charge-air-cooler temperature | ° C |
|  | Cylinder 1 knock/combustion performance count | count |
|  | Cylinder 2 knock/combustion performance count | count |
|  | Cylinder 3 knock/combustion performance count | count |
|  | Cylinder 4 knock/combustion performance count | count |

13.  Report

13.1  For reference oil results, use the standardized report form set available from the ASTM TMC21 and data dictionary for reporting test results and for summarizing operational data (see Annex A12).

Note 10—Report the non-reference oil test results on these same forms if the results are intended to be submitted as candidate oil results against a specification.

13.1.1  Fill out the report forms according to the formats shown in the data dictionary.

13.1.2  Transmit results to the TMC within 5 working days of test completion.

13.1.3  Transmit the results electronically as described in the ASTM Data Communications Committee Test Report Transmission Model (Section 2 — Flat File Transmission Format) available from the ASTM TMC. Upload files via the TMC’s website.

13.2  Report all reference oil test results, whether aborted, invalidated, or successfully completed, to the TMC.

13.3  Precision of Reported Units—Use the Practice E29 rounding-off method for critical pass/fail test result data. Report the data to the same precision as indicated in data dictionary.

13.4  In the space provided, note the time, date, test hour, and duration of any shutdown or off-test condition. Start counting downtime at one hour after the end of an iteration or any time a test comes down in the middle of an iteration. The maximum allowable downtime is 48 h.

13.5  If a calibration period is extended beyond the normal calibration period length, make a note in the comment section and attach a written confirmation of the granted extension from the TMC to the test report. List the outcomes of previous runs that may need to be considered as part of the extension in the comment section.

14.  Precision and Bias

14.1  Precision:

14.1.1  Test precision is established on the basis of operationally valid reference-oil test results monitored by the TMC.

14.1.2  Intermediate Precision Conditions—Conditions where test results are obtained with the same test method using the same test oil, with changing conditions such as operators, measuring equipment, test stands, test engines, and time.

Note 11—Intermediate precision is the appropriate term for this test method, rather than repeatability, which defines more rigorous within-laboratory conditions.

14.1.2.1  Intermediate Precision Limit (ip)—The difference between two results obtained under intermediate precision conditions that in the long run, in the normal and correct conduct of the test method, exceed the value shown in Table 12 in only one case in twenty. When only a single test result is available, the intermediate precision limit can be used to calculate a range (test result ± intermediate precision limit) outside of which a second test result would be expected to fall about one time in twenty.

14.1.3  Reproducibility Conditions—Conditions where test results are obtained with the same test method using the same test oil in different laboratories with different operators using different equipment.

14.1.3.1  Reproducibility Limit (R)—The difference between two results obtained under reproducibility conditions that would, in the long run, in the normal and correct conduct of the test method, exceed the values in Table 12 in only one case in twenty. When only a single test result is available, the reproducibility limit can be used to calculate a range (test result ± reproducibility limit) outside of which a second test result would be expected to fall about one time in twenty.

TABLE 12  Sequence IX Test PrecisionA

| Quantity | Intermediate PrecisionB |  | ReproducibilityC |  |
| --- | --- | --- | --- | --- |
|  | SipD | ip | SRD | R |
| Average number of preignition events, AvPIE+0.5 | 0.2856 | 0.7997 | 0.2856 | 0.7997 |

A These statistics are based on 34 tests conducted on eight stand/engine combinations at three laboratories on ASTM reference oils 220, 221, and 223. They were calculated on March 29, 2017.

B See 14.1.2.

C See 14.1.3.

D S is the standard deviation.

14.2  Bias—No estimate of bias for this test method is possible because the performance results for an oil are determined only under specific conditions of the test and no absolute standards exist.

# aNNEXES

(Mandatory Information)

A1.  ASTM TEST MONITORING CENTER ORGANIZATION

A1.1  Nature and Functions of the ASTM Test Monitoring Center (TMC)—The TMC is a non-profit organization located in Pittsburgh, Pennsylvania and is staffed to: administer engineering studies; conduct laboratory inspections; perform statistical analyses of reference oil test data; blend, store, and ship reference oils; and provide the associated administrative functions to maintain the referencing calibration program for various lubricant tests as directed by ASTM Subcommittee D02.B0 and the ASTM Executive Committee. The TMC coordinates its activities with the test sponsors, the test developers, the surveillance panels, and the testing laboratories. Contact TMC through the TMC Director at:

ASTM Test Monitoring Center

6555 Penn Avenue

Pittsburgh, PA 15206-4489

www.astmtmc.cmu.edu

A1.2  Rules of Operation of the ASTM TMC—The TMC operates in accordance with the ASTM Charter, the ASTM Bylaws, the Regulations Governing ASTM Technical Committees, the Bylaws Governing ASTM Committee D02, and the Rules and Regulations Governing the ASTM Test Monitoring System.

A1.3  Management of the ASTM TMC—The management of the Test Monitoring System is vested in the Executive Committee elected by Subcommittee D02.B0. The Executive Committee selects the TMC Director who is responsible for directing the activities of the TMC.

A1.4  Operating Income of the ASTM TMC—The TMC operating income is obtained from fees levied on the reference oils supplied and on the calibration tests conducted. Fee schedules are established by the Executive Committee and reviewed by Subcommittee D02.B0.

# A2. ASTM TEST MONITORING CENTER: CALIBRATION PROCEDURES

A2.1  Reference Oils—These oils are formulated or selected to represent specific chemical, or performance levels, or both. They are usually supplied directly to a testing laboratory under code numbers to ensure that the laboratory is not influenced by prior knowledge of acceptable results in assessing test results. The TMC determines the specific reference oil the laboratory shall test.

A2.1.1  Reference Oil Data Reporting—Test laboratories that receive reference oils for stand calibration shall submit data to the TMC on every sample of reference oil they receive.  If a shipment contains any missing or damaged samples, the laboratory shall notify the TMC immediately.

A2.2  Calibration Testing:

A2.2.1  Full-scale calibration testing shall be conducted at regular intervals. These full-scale tests are conducted using coded reference oils supplied by the TMC. It is a laboratory's responsibility to keep the on-site reference oil inventory at or above the minimum level specified by the TMC test engineers.

A2.2.2  Test Stands Used for Non-Standard Tests—If a non-standard test is conducted on a previously calibrated test stand, the laboratory shall conduct a reference oil test on that stand to demonstrate that it continues to be calibrated, prior to running standard tests.

A2.3  Reference Oil Storage—Store reference oils under cover in locations where the ambient temperature is between -10 °C and +50 °C.

A2.4  Analysis of Reference Oil—Unless specifically authorized by the TMC, do not analyze TMC reference oils, either physically or chemically. Do not resell ASTM reference oils or supply them to other laboratories without the approval of the TMC. The reference oils are supplied only for the intended purpose of obtaining calibration under the ASTM Test Monitoring System. Any unauthorized use is strictly forbidden. The testing laboratory tacitly agrees to use the TMC reference oils exclusively in accordance with the TMC’s published Policies for Use and Analysis of ASTM Reference Oils, and to run and report the reference oil test results according to TMC guidelines. Additional policies for the use and analysis of ASTM Reference Oils are available from the TMC.

A2.5  Conducting a Reference Oil Test—When laboratory personnel are ready to run a reference calibration test, they shall request an oil code via the TMC website.

A2.6  Reporting Reference Oil Test Results—Upon completion of the reference oil test, the test laboratory transmits the data electronically to the TMC, as described in Section 13. The TMC reviews the data and contacts the laboratory engineer to report the laboratory's calibration status. All reference oil test results, whether aborted, invalidated, or successfully completed, shall be reported to the TMC.

A2.6.1 All deviations from the specified test method shall be reported.

# A3. ASTM TEST MONITORING CENTER: MAINTENANCE ACTIVITIES

A3.1  Special Reference Oil Tests—To ensure continuous severity and precision monitoring, calibration tests are conducted periodically throughout the year. Occasionally, the majority or even all of the industry’s test stands will conduct calibration tests at roughly the same time. This could result in an unacceptably large time frame when very few calibration tests are conducted. The TMC can shorten or extend calibration periods as needed to provide a consistent flow of reference oil test data. Adjustments to calibration periods are made such that laboratories incur no net loss or gain in calibration status.

A3.2  Special Use of the Reference Oil Calibration System—The surveillance panel has the option to use the reference oil system to evaluate changes that have potential impact on test severity and precision. This option is only taken when a program of donated tests is not feasible. The surveillance panel and the TMC shall develop a detailed plan for the test program. This plan requires all reference oil tests in the program to be completed as close to the same time as possible, so that no laboratory/stand calibration status is left pending for an excessive length of time. In order to maintain the integrity of the reference oil monitoring system, each reference oil test is conducted so as to be interpretable for stand calibration. To facilitate the required test scheduling, the surveillance panel may direct the TMC to lengthen and shorten reference oil calibration periods within laboratories such that the laboratories incur no net loss or gain in calibration status. To ensure accurate stand, or laboratory, or both severity assessments, conduct non-reference oil tests the same as reference oil tests.

A3.3  Donated Reference Oil Test Programs—The surveillance panel is charged with maintaining effective reference oil test severity and precision monitoring. During times of new parts introductions, new or re-blended reference oil additions, and procedural revisions, it may be necessary to evaluate the possible effects on severity and precision levels. The surveillance panel may choose to conduct a program of donated reference oil tests in those laboratories participating in the monitoring system, in order to quantify the effect of a particular change on severity and precision. Typically, the surveillance panel requests its panel members to volunteer enough reference oil test results to create a robust data set. Broad laboratory participation is needed to provide a representative sampling of the industry. To ensure the quality of the data obtained, donated tests are conducted on calibrated test stands. The surveillance panel shall arrange an appropriate number of donated tests and ensure completion of the test program in a timely manner.

A3.4  Intervals Between Reference Oil Tests—Under special circumstances, such as extended downtime caused by industry-wide parts or fuel shortages, the TMC may extend the intervals between reference oil tests.

A3.5  Introducing New Reference Oils—Reference oils produce various results. When new reference oils are selected, participating laboratories will be requested to conduct their share of tests to enable the TMC to recommend industry test targets. ASTM surveillance panels require a minimum number of tests to establish the industry test targets for new reference oils.

A3.6  TMC Information Letters—Occasionally it is necessary to revise the test method, and notify the test laboratories of the change, prior to consideration of the revision by Subcommittee D02.B0. In such a case, the TMC issues an Information Letter. Information Letters are balloted semi-annually by Subcommittee D02.B0, and subsequently by D02. By this means, the Society due process procedures are applied to these Information Letters.

A3.6.1   Issuing Authority—The authority to issue an Information Letter differs according to its nature. In the case of an Information Letter concerning a part number change which does not affect test results, the TMC is authorized to issue such a letter. Long-term studies by the surveillance panel to improve the test procedure through improved operation and hardware control may result in the issuance of an Information Letter. If obvious procedural items affecting test results need immediate attention, the test sponsor and the TMC issue an Information Letter and present the background and data supporting that action to the surveillance panel for approval prior to the semiannual Subcommittee D02.B0 meeting.

A3.7  TMC Memoranda—In addition to the Information Letters, supplementary memoranda are issued. These are developed by the TMC and distributed to the appropriate surveillance panel and participating laboratories. They convey such information as batch approvals for test parts or materials, clarification of the test procedure, notes and suggestions of the collection and analysis of special data that the TMC may request, or for any other pertinent matters having no direct effect on the test performance, results, or precision and bias.

# A4. ASTM TEST MONITORING CENTER: RELATED INFORMATION

A4.1  New Laboratories—Laboratories wishing to become part of the ASTM Test Monitoring System will be requested to conduct reference oil tests to ensure that the laboratory is using the proper testing techniques. Information concerning fees, laboratory inspection, reagents, testing practices, appropriate committee membership, and rater training can be obtained by contacting the TMC Director.

A4.2  Information Letters: COTCO Approval—Authority for the issuance of Information Letters was given by the committee on Technical Committee Operations in 1984, as follows: “COTCO recognizes that D02 has a unique and complex situation. The use of Information Letters is approved providing each letter contains a disclaimer to the affect that such has not obtained ASTM consensus. These Information Letters should be moved to such consensus as rapidly as possible.”

A4.3  Precision Data—The TMC determines the precision of test methods by analyzing results of calibration tests conducted on reference oils. Precision data are updated regularly. Current precision data can be obtained from the TMC.

# A5.  CONTROL AND DATA ACQUISITION REQUIREMENTS

A5.1  General Description:

A5.1.1  The data acquisition system shall be capable of logging the operational data in digital format. It is to the advantage of the laboratory that the system be capable of real time plotting of controlled quantities to help assess test validity. The systems shall be capable of calculating real time quality index as this will be monitored throughout the test as designated in A5.4.

A5.1.2  Control capability is not dictated by this procedure. The control system shall be capable of keeping the controlled quantities within the limits specified in Table 8 and maintain the quality index shown in A5.4.

A5.1.3  Design the control and data acquisition system to meet the requirements listed below. Use the recommendations laid out in the Instrumentation Task Force Report and Data Acquisition Task Force Report for any items not addressed in Annex A3.

A5.2  Digital Recording Frequency—The maximum allowable time period over which data can be accumulated is 1 s. This data can be filtered, as described in A5.5, and will be considered a reading.

A5.3  Steady State Operation:

A5.3.1  Each test interval of 175,000 engine cycles is conducted at steady state operation Calculate the Quality Index (QI), as described in A5.4, using values reported to the accuracy levels in Table A5.1.

# TABLE A5.1 Accuracy Levels of Data Points to be Used in QI Calculations

| ##### Quantity | Field Length |
| --- | --- |
| Speed | XXXX. |
| Humidity | XX.X |
| Temperature | XX.X |
| ##### Load | XXX.X |
| Inlet Air Pressure | XX.XXX |
| Exhaust Backpressure | XX.X |

A5.3.2  The time intervals between recorded readings shall not exceed 1 s. Data shall be recorded throughout the length of each test iteration.

A5.4  QI Calculation:

A5.4.1  In accordance with the DACA II Report II, calculate the QI for all controlled quantities for the steady state portion of each test stage throughout the entire test. Ensure missing or bad quality data are accounted for in accordance with the DACA II Report.

A5.4.2  Update the QI periodically throughout the test to determine the operational validity while the test is in progress. This could indicate if the test operational validity is in question before the test has completed.

A5.4.3  Use the Eq A5.1and the values listed in Table A5.2 to calculate the QIi:

QIi =  1- 1n1nU+L-2Xi U-L2                           			             (A5.1)

where:

i = the quantity measured in the test,

| Xi | = | the recorded value of the measured quantity i, |
| --- | --- | --- |
| U | = | the upper-specification limit for the measured quantity i, |
| L | = | the lower-specification limit for the measured quantity i, and |
| n | = | the total number of data points taken as determined from test length and procedural specified sampling rate. |

A5.4.4  Reset data that is greater than the over-range values listed in Table A5.2 with the over-range value listed in Table A5.2.

A5.4.5  Reset data that is lower than the under-range values listed in Table A5.2 with the under-range value listed in Table A5.2.

A5.4.6  Round the QI values to the nearest 0.001.

A5.4.7  Report the QI values on Forms 5 to 8  of the test report.

A5.4.8  If the end-of-test QI value is below 0.000 for reference oil tests, review the test operations with the TMC. The TMC issues a letter to the laboratory and the test sponsor on its opinion.

A5.4.8.1  The laboratory documents its comments regarding the end-of-test QI values less than 0.000 for non-reference oil tests. The laboratory or test sponsor might request TMC review of test operations for non-reference oil tests. The TMC issues a letter to document its opinion.

TABLE A5.2    L and U Limits and Over- and Under-Range Values

| Quantity, unit | L | U | Over-range | Under-range |
| --- | --- | --- | --- | --- |
| Speed, r/min | 1730 | 1770 | 3941 | 0 |
| Torque, N•m | 264 | 274 | 817 | 0 |
| Coolant out temperature, °C | 94.5 | 95.5 | 289 | 0 |
| Oil gallery temperature, °C | 94.5 | 95.5 | 150 | 40 |
| Air charge temperature, °C | 42.5 | 43.5 | 98 | 0 |
| Inlet air temperature, °C | 29.5 | 30.5 | 85 | 0 |
| Fuel temperature, °C | 29.5 | 30.5 | 1190 | 0 |
| Back pressure, kPa (absolute) | 102 | 106 | 323 | 0 |
| Inlet air pressure, kPa (absolute) | 0.03 | 0.07 | 2.2 | -2.1 |
| Humidity, g/kg | 10.9 | 11.9 | 66 | 0 |
| Coolant pressure, kPa (gauge) | 68 | 72 | 290 | 0 |
| Coolant flow rate, L/min | 53 | 57 | 274 | 0 |

A5.5  Time Constants:

A5.5.1  Filtering can be applied to all control quantities. The amount of filtering applied shall not allow time constants to exceed the values listed in Table A5.3. This time constant shall pertain to the entire system, running from the sensor to the display and data acquisition.

A5.5.2  Maximum allowable system time constants for the controlled quantities are shown in Table A5.3.

# TABLE A5.3 Maximum Allowable Time Constants

| Control quantity, unit | Time constant, s |
| --- | --- |
| Engine speed, r/min | 0.5 |
| Torque, Nm | 0.7 |
| Engine-oil-in temperature °C | 2.4 |
| Engine-coolant-out temperature, °C | 2.4 |
| Engine-coolant flowrate, L/min | 8.0 |
| Inlet-air temperature, °C | 2.4 |
| Inlet-air pressure, kPa | 1.2 |
| Exhaust back pressure, kPa | 1.2 |
| Engine-coolant pressure, kPa | 1.2 |

# Annex A6. TEMPERATURE, PRESSURE AND OTHER CONTROL SYSTEMS

# A6.1  See Figs. A6.1 to A6.17.

FIG. A6.1 Oil Pan Drain Locations

# Locate the temperature sensors in the thermostat housing and at water pump inlet as shown in 1 and 12 respectively.

(1) Thermostat housing, coolant out with temperature sensor (P/N OHTVH-009-1)

(2) Sight glass

(3) Flowmeter (can be installed on the inlet or outlet sides of the engine, outlet installation shown here)

(4) Flow-control valve

(5) Optional temperature sensor

(6) Fabricated coolant reservoir

(7) Constant full expansion tank

(8) Pressure radiator cap (MOTORCRAFT RS40 P/N D2YY-8100-A)

(9) Process-water control valve (regulated by temperature controller with three remote set points)

(10) Heat exchanger (ITT Standard P/N 5-030-06-048-001 TYP.) (Run engine coolant through the tube side)

(11) Process water supply (shell side)

(12) Water-pump inlet with temperature sensor (OHTVH-008-1)

(13) Turbocharger-coolant return

(14) Engine coolant (tube side)

(15) Coolant system drain valve

(16) Coolant-pressure regulator

(17) Coolant pressure

# FIG. A6.3  Schematic Showing Components of a Typical Engine Cooling System

# FIG. A6.4 Motor Mount, Front (Two Options Shown)

# FIG. A6.5 Motor Mount, Rear

# FIG. A6.6 Exhaust Measurements and Instrumentation

# FIG. A6.7 Location of Fuel-Temperature Sensor

# FIG. A6.8 Typical Air Inlet System

# FIG. A6.9: Intercooler Tubing Measurements and Instrumentation

# FIG. A6.10 Typical Intercooler Installation

# Fig. A6.11 Oil Cooler Showing Oil Gallery Pressure Sensor Location

# Oil Out temperature location in oil filter adapter

# FIG. A6.12  Oil Cooler Showing Oil Temperature Locations

52.8

# Fig. A6.13 Piston Diameter Measurements

# NOTE: All dimensions in mm.

# A6.14. Bore Ladder

# FIG. A6.15  Vacuum System

# FIG. A6.16 Dynamometer Wiring Harness

# FIG. A6.17 Engine Wiring Harness

# Fig A6.18 Engine-Coolant-Out Pressure Measurement Location

# Fig A6.19 Cylinder Head Pressure Measurement Location

# ANNEX A7  TEST FUEL SPECIFICATION

# A7.1 See Table A7.1

# Table A7.1 Test Fuel Specification

| Quantity, units | Test method | Specification |
| --- | --- | --- |
| Research octane number | D2699 | 96.0 to 98.5 |
| Octane number sensitivity | D2700 | 7.5 to 10.5 |
| Lead concentration, mg/L | D3237 | ≤ 2.5 |
| Total sulfur mass fraction, mg/kg | D2622, D3120, D5453 | ≤ 15 |
| Phosphorus concentration, mg/L | D3231 | ≤ 1.3 |
| Copper corrosion (3 h at 50 °C) (dark orange) | D130 | ≤ 1b |
| Oxidation stability, min | D525 | ≥ 1000 |
| Specific gravity, kg/L | D1298 | 0.734 to 0.744 |
| Hydrocarbon Composition | D1319 |  |
| Aromatics, volume fraction, % |  | 25 to 35 |
| Olefins, volume fraction, % |  | ≤ 10 |
| Saturates, volume fraction, % |  | remainder |
| Gum concentration (washed), mg/100 mL | D381 | ≤ 4 |
| Gum concentration (unwashed), mg/100 mL | D381 | ≤ 10 |
| Reid Vapor Pressure, kPa | D323 | 60 to 63 |
| Distillation % to be evaporated within temperatures shown below: | D86 |  |
| IBPA, °C |  | 24 to 35 |
| 10 %, °C |  | 49 to 57 |
| 50 %, °C |  | 93 to 110 |
| 90 %, °C |  | 149 to 163 |
| End Point, °C |  | ≤ 213 |
| Residue volume fraction, % |  | ≤ 2 |
| Water and sediment, % | D2709 | ≤ 0.01 |
| Odor |  | Shall have the usual characteristic odor of gasoline with no pronounced foreign odor. Shall have the usual characteristic odor of gasoline with no pronounced foreign odor. Shall have the usual characteristic odor of gasoline with no pronounced foreign odor |
| Color |  | Red |

A Initial boiling point

Annex A8. PART NUMBERS FOR ENGINE ASSEMBLY, ENGINE PARTS, FASTENERS,  GASKETS,  TEST STAND SETUP PARTS, AND SPECIAL PARTS

# A8.1 See Tables A8.1 to A8.8.

# TABLE A8.1 Engine Assembly Part Numbers

| Current Ford Service P/N | Current Ford Engineering P/N | Description |
| --- | --- | --- |
| BB5Z-6006-A | BB5E-6006-AD | 2.0L ENGINE ASY LB |
|  | DA8E-6006-BB | 2.0L ENGINE ASY LB |

# TABLE A8.2 Reusable Engine Parts

| Current Ford Service P/N | Current Ford Engineering P/N | Description |
| --- | --- | --- |
| BB5Z9F593B | BB5E9F593BA | INJECTOR ASY |
| CJ5Z9D280A | CJ5E9D280BF | MANIFOLD ASY - FUEL SUPPLY |
| CJ5Z9D440A | CJ5E9B374BC | COVER - FUEL PUMP |

# TABLE A8.3 Part Numbers for Fasteners

| Current Ford Service P/N | Current Ford Engineering P/N | Description |
| --- | --- | --- |
| W500033S437 | W500033S437 | BOLT - FLANGED HEX. |
| W500114S442 | W500114S442 | BOLT |
| W500212S437 | W500212S437 | SCREW |
| W500214S437 | W500214S437 | BOLT ‐ HEX.HEAD |
| W500221S437 | W500221S437 | BOLT - HEX.HEAD |
| W500224S437 | W500224S437 | BOLT |
| W500300S437 | W500300S437 | BOLT |
| W500301S437 | W500301S437 | BOLT |
| W500310S437 | W500310S437 | BOLT - HEX.HEAD |
| W500313S437 | W500313S437 | BOLT |
| W500328S437 | W500328S437 | BOLT |
| W500414S442 | W500414S442 | BOLT |
| W503275S437 | W503275S437 | BOLT - HEX. HEAD - FLANGED |
| W505531S442 | W505531S442 | SCREW |
| W506976S442 | W506976S442 | SCREW |
| W520214S440 | W520214S440 | NUT |
| W700115S437 | W700115S437 | SCREW AND WASHER ASY |
| W701183S300 | W701183S300 | DOWEL - BUS H |
| W701219S437 | W701219S437 | BOLT |
| W702426S303 | W702426S303 | BOLT - HEX.HEAD |
| W702492S437 | W702492S437 | STUD |
| W702700S437 | W702700S437 | STUD |
| W703383S437 | W703383S437 | BOLT |
| W703643S430 | W703643S430 | BOLT |
| W703649S300 | W703649S300 | PIN |
| W704474S437 | W704474S437 | STUD |
| W706282S430 | W706282S430 | BOLT |
| W706284S437 | W706284S437 | BOLT |
| W706487S437 | W706487S437 | BOLT‐OIL COOLER FILTER |
| W711261S437 | W711261S437 | BOLT |
| W711574S439 | W711574S439 | STUD |
| W712022S430A | W712022S430 | BOLT ‐ HEX.HEAD |
| W713095S403 | W713095S403 | NUT |
| W715323S300 | W715323S300 | WAS HER - COPPER, T/C OIL LINE |
| W715638S443 | W715638S443 | STUD |
| W716137S437 | W716137S437 | BOLT |
| W716735S437 | W716735S437 | BOLT |
| W716841S900 | W716841S900 | PIN, BELL HOUSING |
| 1L5Z6379AA | W706161S300 | BOLT |
| 1S7Z6A340AA | 1S7G6K340BC | BOLT, CRK S HFT PULLEY |
| 1S7Z6K282AA | 1S7G6K282AB | BOLT, CHAIN TEN |
| AG9Z6065A | AG9G6065BA | BOLT - HEX.HEAD, CYL HEAD |
| AG9Z6345A | AG9G6345AC | BOLT - BEARING CAP - HEX. HEAD |
| BB5Z6214A | BB5E6214CA | BOLT - CONNECTING ROD |
| CV6Z6279A | CV6E6279AA | BOLT, CAMSHAFT |

# TABLE A8.4 Part Numbers for Test Parts

| Current Ford Service P/N | Current Ford Engineering P/N | Des cription |
| --- | --- | --- |
| 7T4Z9601A | 7T439601AA | ELEMENT ASY - AIR CLEANER |
| 1S7Z6378AA | 1S7G6378AB | WAS HER,CRK DIAMOND CRUSH |
| 6M8Z6278A | 6M8G6278AA | WAS HER, CAM, DIAMOND CRUS H |

# TABLE A8.5 Part Numbers for Gaskets

| Current Ford S ervice P/N | Current Ford Engineering P/N | Description |
| --- | --- | --- |
| CJ5Z6079D | CJ5E6079AC | KIT - GASKET |
| 1S7Z6571EA | 1S7G6A517BG | SEAL - VALVE STEM EX |
| 1S7Z6840AA | 1S7G6A636AD | GASKET, OIL FILTER ADPT |
| 1S7Z6K301BA | 1S7G6A321AA | SEAL - CRANKSHAFT REAR OIL |
| 1S7Z8507AE | 1S7G8507AF | GASKET - WATER PUMP |
| 3M4Z6625AA | 3M4G6625AA | GASKET, OIL PMP P/U TUBE |
| 3M4Z8255A | 3M4G8K530AB | GASKET, T/STAT HSG |
| 3S4Z6571AA | 3S4G6A517AA | SEAL - VALVE STEM INT |
| 9L8Z9E936A | 9L8E9E936AA | GASKET, T/B |
| AA5Z9E583A | AA5E9E583AA | SEAL, FU PUMP |
| AG9Z9P431A | AG9G9P431AA | GASKET, T/C COOL LINE |
| BB5Z2A572B | BB5E2D224BB | GASKET - VACUUM PUMP |
| BB5Z6584A | BB5E6K260AB | GASKET, CAM COVER |
| BB5Z6L612A | BB536L612AA | GASKET, EXHAUST |
| BG9Z9229A | BG9E9U509AB | KIT - "O" RING, FU INJ |
| BR3Z6C535B | BR3E6P251BA | SEAL - VALVE VCT |
| CB5Z9276A | CJ5E9A420BA | GASKET, FU PUMP CVR |
| CJ5Z6051A | CJ5E6051EC | GASKET - CYLINDER HEAD |
| CJ5Z6N652A | CJ5E6N652AA | GASKET, T/C OIL DRAIN LINE |
| CJ5Z8255A | CJ5E8255AA | SEAL - THERMOSTAT |
| CJ5Z9439A | CJ5E9439AA | GASKET - INTAKE MANIFOLD |
| CJ5Z9448A | CJ5E9448BA | GASKET, EX MANIFOLD |
| CM5Z6700A | CM5E6700AB | SEAL AS Y - CRKS HAFT OIL - FRT |

# Table A8.6 Test Stand Setup Part Numbers

| Current Ford S ervice P/N | Current Ford Engineering P/N | Des cription |
| --- | --- | --- |
| AG9Z9D930B | AG9T9H589BE | WIRE ASY, FE INJ |
| 1S7Z12A699BB | 1S7A12A699BB | SENS OR - ENGINE KNOCK |
| 6M8Z6C315AA | 6M8G6C315AB | SENS OR - CRANKSHAFT POSITION - CPS |
| 8F9Z9F472A | 8F9A9Y460AB | SENS OR ASY, O2 |
| 8V2Z12B579A | 8V2112B579AA | SENS OR ASY, MAF |
| 9L8Z6G004E | 9L8A6G004BC | SENS OR ASY, CYL HD TMP |
| AA5Z9A600B | AA539A600AD | CLEANER ASY - AIR |
| AE5Z6A228A | AE5Q6A228AA | PULLEY ASY - TENSION BELT |
| AE5Z8620A | AE5Q6C301AA | V-BELT |
| AG9Z6K679A | AG9G6K679BC | PIPE - OIL FEED, T/C |
| AG9Z6K868A | CJ5E6K868AA | VALVE ASY, ENG PST OIL COOL |
| AG9Z6L092A | AG9G6K677BC | HOSE - T/C OIL DRAIN |
| AG9Z8555A | AG9G8A506BB | HOSE - WATER INLET, T/C |
| AG9Z9F479A | AG919F479AB | SENS OR ASY, MAP |
| BV6Z9F479A | BV619F479AA | SENS OR ASY, MAPT |
| AS 7Z6B288A | AS7112K073AA | SENS OR - CAMS HAFT POS ITION |
| BB3Z6A642A | BB3E6A810AA | KIT ENGINE OIL COOLER |
| BB5Z11002C | BB5T11000AA | STARTER MOTOR AS Y |
| BB5Z5A231A | BB535A281AA | CLAMP - HOSE, T/C TO EXH |
| BB5Z6C640A | BB536K863CE | CONNECTION - AIR INLET T/B END |
| BB5Z6C640B | BB536K863DF | CONNECTION - AIR INLET, I/C END |
| BB5Z6C646C | BB536C646CD | DUCT - AIR, TURBO END |
| BB5Z6C646D | BB536C646DF | DUCT - AIR, INTERCOOLER END |
| BB5Z6C683A | BB5E6L663AA | FILTER AS Y (T/C SCREEN) |
| BB5Z9647A | BB539647AB | BRACKET, AIRBOX |
| BB5Z9661A | BB539643AA | COVER, AIRBOX |
| BB5Z9B659B | BB539F805DE | HOSE - AIR, TURBO END |
| BB5Z9B659E | BB539F805CG | HOSE - AIR, AIR BOX END |
| BM5Z9F972A | BM5G9F972BA | SENS OR - FUEL INJECTOR PRES SURE |
| BR2Z9E499A | BR2E9E499AA | CONNECTOR, VAC CONTRL, T/C |
| CB5Z6K682F | CB5E6K682BF | TURBO CHARGER |
| CB5Z8592A | CB5E8592AB | CONNECTION - WATER OUT, T/C |
| CB5Z8K153B | CB5E8B535AC | TUBE - WATER OUTLET |
| CB5Z9424D | CB5E9424AF | MANIFOLD AS Y - INTAKE |
| CB5Z9S 468C | CB5E9S468AF | HOSE, EMS (VAC HARNESS) |
| CJ5Z9J323B | CJ5E9J323BC | TUBE AS Y FE PMP TO FE MAN |
| CM5Z12029A | CM5E12A366CA | COIL ASY - IGNITION |
| CP9Z9E926A | CM5E9F991AD | THROTTLE BODY AND MOTOR ASY |
| D4ZZ7600A | D4ZA7120AB | SLEEVE, PILOT BEARING |
| DU5Z12A581U | DU5T12C508UE | WIRE ASY, ENGINE MAIN |
| YS 4Z6766A | YS4G6766DA | CAP ASY - OIL FILLER |
| 5M6Z8509AE | 5M6Q8509AE | PULLEY - WATER PUMP |
| AG9Z6312B | AG9E6D334AA | PULLEY - CRANKSHAFT |

# TABLE A8.7 Part Numbers for Special Parts

| DescriptionA | P/N |
| --- | --- |
| Housing, flywheel | OHTVH-005-1 |
| Flywheel, modified, 2.0l | OHTVH-006-1 |
| Clutch (Sachs) | K0047-07 |
| Plate, Pressure | VH006-8-2 |
| Harness, Dyno, 2.0l | OHTVH-007-1 |
| Inlet, Coolant | OHTVH-008-1 |
| Clip, Retainer, Sensor, Coolant Inlet | VH008-1 |
| Seal, Coolant Inlet | VH008-2 |
| Outlet, Coolant | OHTVH-009-1 |
| Seal, Coolant Outlet | VH009-6 |
| Spacer (Shim), Clutch Pressure Plate | OHTVH-011-1 |
| Cylinder Head, Instrumented | TEIB |
| Mount, Front, Ford 2.0l | OHTVH-004-1 |
| Rubber Isolator, Front Mount | 85 ESCORT |
| Rubber Isolator, Rear Mount | 6628-A |
| Pressure Transducer, | AVL GH15DK |

A All parts are available from OH Technologies, 9300 Progress Pkwy, Mentor, OH 44060.

B Test Engineering Inc.

# Table A8.8 Service Tools

| Tool name |  | Supplier | P/N |
| --- | --- | --- | --- |
| Camshaft alignment tool |  | Ford, OTC | 303-1565 |
| Crankshaft TDC timing peg |  | Ford, OTC | - 303-507 |
| Crankshaft position sensor alignment tool |  | Ford, OTC | 303-1521 |
| Pressure sensor installation tool |  | AVL | TT21 type mounting tool (PN TIWG0214A.01 |

# A9.2 Cylinder Head Measurements—see Table A9.2.

# Table A9.2 Cylinder Head Measurements Record

Head #								Engine #

Head Run #								Test #

DATE:									Instrument Cntrl # (Valve Guide)

# Instrument Cntrl # (Valve Stem)

|  | Valve guide diameterA, mm | Valve stem diameterB, mm | ClearanceC, mm |  |  | Valve guide diameterA, mm | Valve stem diameterB, mm | ClearanceC, mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1A intake |  |  |  |  | 1A exhaust |  |  |  |
| 1B intake |  |  |  |  | 1B exhaust |  |  |  |
| 2A intake |  |  |  |  | 2A exhaust |  |  |  |
| 2B intake |  |  |  |  | 2B exhaust |  |  |  |
| 3A intake |  |  |  |  | 3A exhaust |  |  |  |
| 3B intake |  |  |  |  | 3B exhaust |  |  |  |
| 4A intake |  |  |  |  | 4A exhaust |  |  |  |
| 4B intake |  |  |  |  | 4B exhaust |  |  |  |

# A Target 5.51 mm

B Target 5.5 mm

C Target 0.03 mm to 0.07 mm

Instrument cntrl # (length)						Instrument cntrl # (tension)

|  | Spring free lengthA, mm | Spring tension, kg @ 28.5 mm |  |  |  | Spring free lengthA, mm | Spring tension, kg @ 28.5 mm |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1A intake |  |  |  |  | 1A exhaust |  |  |
| 1B intake |  |  |  |  | 1B exhaust |  |  |
| 2A intake |  |  |  |  | 2A exhaust |  |  |
| 2B intake |  |  |  |  | 2B exhaust |  |  |
| 3A intake |  |  |  |  | 3A exhaust |  |  |
| 3B intake |  |  |  |  | 3B exhaust |  |  |
| 4A intake |  |  |  |  | 4A exhaust |  |  |
| 4B intake |  |  |  |  | 4B exhaust |  |  |

# A Target 47 mm

# Instrument cntrl # (lash)

| Intake valve lash measurementA, mm |  |  |  |  | Exhaust valve lash measurementB, mm |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1F |  |  |  |  | 1F |  |
| 1R |  |  |  |  | 1R |  |
| 2F |  |  |  |  | 2F |  |
| 2R |  |  |  |  | 2R |  |
| 3F |  |  |  |  | 3F |  |
| 3R |  |  |  |  | 3R |  |
| 4F |  |  |  |  | 4F |  |
| 4R |  |  |  |  | 4R |  |

A Target 0.19 mm to 0.31 mm							B Target 0.30 mm to 0.42 mm

# Head flatness:								      Initials:

- A10 PCM CANBUS PARAMETER ADDRESSES

- A10.1 CAN Bus Data—Set up the data acquisition software to record the parameter addresses, as shown in Table A10.1, from the engine’s PCM.

# Table A10.1 PCM CANBUS Parameter Identification (PID)

| Mode | PID Number (Hex) | Parameter Description | Type | Bytes | Scale | Offset | Minimum | Maximum | Units |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0E | Ignition timing advance for #1 cylinder | Unsigned numeric | 1 | 0.5 | -64 | -64 | 63.5 | ° |
| 1 | 11 | Absolute throttle position | Unsigned numeric | 1 | 0.392156862745 | 0 | 0 | 100 | % |
| 1 | 05 | Engine-coolant temperature | Unsigned numeric | 1 | 1 | -40 | -40 | 215 | ° C |
| 1 | 0F | Intake-air temperature | Unsigned numeric | 1 | 1 | -40 | -40 | 215 | º C |
| 1 | 34 | Equivalence ratio () | Unsigned numeric | 2 | 0.000030518044 | 0 | 0 | 2 | dimensionless |
| 1 | 43 | Absolute load value | Unsigned numeric | 2 | 0.392156862745 | 0 | 0 | 25700 | % |
| 1 | 0B | Intake-manifold pressure (absolute) | Unsigned numeric | 1 | 1 | 0 | 0 | 255 | kPa |
| 1 | 23 | Fuel-rail pressure (gauge) | Unsigned numeric | 2 | 10 | 0 | 0 | 655350 | kPa |
| 1 | 49 | Accelerator-pedal position | Unsigned numeric | 1 | 0.392156862745 | 0 | 0 | 100 | % |
| 22 | 033E | Boost pressure (absolute) - raw value | Unsigned numeric | 2 | 0.007629394531 | 0 | 0 | 499.992370605469 | kPa |
| 22 | 0462 | Turbocharger wastegate duty cycle | Unsigned numeric | 2 | 0.003051757813 | 0 | 0 | 199.996948274955 | % |
| 22 | 0318 | Actual intake (A) camshaft position | Signed numeric | 2 | 0.0625 | 0 | -2048 | 2047.9375 | ° |
| 22 | 0319 | Actual exhaust (B) camshaft position | Signed numeric | 2 | 0.0625 | 0 | -2048 | 2047.9375 | ° |
| 22 | 0316 | Intake (A) camshaft position actuator duty cycle | Unsigned numeric | 2 | 0.003051757813 | 0 | 0 | 199.996948242188 | % |
| 22 | 0317 | Exhaust (B) camshaft position actuator duty cycle | Unsigned numeric | 2 | 0.003051757813 | 0 | 0 | 199.996948242188 | % |
| 22 | 0461 | Charge air-cooler temperature | Signed numeric | 2 | 0.015625 | 0 | -512 | 511.984375 | ° C |
| 22 | 05AC | Cylinder 1 pre-ignition counter | Unsigned numeric | 1 | 1 | 0 | 0 | 255 | count |
| 22 | 05AD | Cylinder 2 pre-ignition counter | Unsigned numeric | 1 | 1 | 0 | 0 | 255 | count |
| 22 | 05AE | Cylinder 3 pre-ignition counter | Unsigned numeric | 1 | 1 | 0 | 0 | 255 | count |
| 22 | 05AF | Cylinder 4 pre-ignition counter | Unsigned numeric | 1 | 1 | 0 | 0 | 255 | count |

- A11. SETTINGS FOR THE AVL INDICOM COMBUSTION ANALYSIS SYSTEM

A11.1 General—The AVL IndiCom is a combustion analysis software package that combines data acquisition and evaluation for graphical presentation.  The settings applicable to the Sequence IX test are provided below.

# A11.1.1 Amplifier and Pressure Sensor Settings (accessed through the “Sensor” menu):

| Amplifier Settings | Pressure Sensor Settings |
| --- | --- |

Pressure Sensor Settings

# A11.1.2 Standard Results Settings:

| PCYL MAX Settings |  |
| --- | --- |

| PCYL MIN Settings |  |
| --- | --- |

| PCYL Max Rise Settings |  |
| --- | --- |

| PCYL IMEP Settings |  |
| --- | --- |

| PCYL Heat Release Settings |  |
| --- | --- |

| PCYL Heat Release Settings |  |
| --- | --- |

PCYL Single Value Settings

| PCYL Knock (Cylinder Pressure) Settings |  |
| --- | --- |

PCYL Knock (Cylinder Pressure) Settings

| PCYL Polytrophic Coefficient Settings |  |
| --- | --- |

| IGN1 MAX Settings |  |
| --- | --- |

| IGN1 Edge Detection Settings |  |
| --- | --- |

| IGN1 Timing Settings |  |
| --- | --- |

Speed Settings

A11.2 Channels To Record—Record the following channels:

- PMAX* (see Note 5)

- PMAXV*

- PMINV*

# A12. SEQUENCE IX REPORT FORMS AND DATA DICTIONARY

A12.1 Download the standardized report form set and data dictionary from the ASTM Test Monitoring Center21 or obtain them in hardcopy format from the TMC. The contents of the report form set are as follows:

- Title / Validity Declaration Page					Form 1

- Table of Contents							Form 2

- Test Results Summary						Form 3

- Summary of LSPI Iterations 					Form 4

- Operational Summary – Iteration A  				Form 5

- Operational Summary – Iteration B  				Form 6

- Operational Summary – Iteration C  				Form 7

- Operational Summary – Iteration D  				Form 8

- Operational Summary – CAN BUS, Iterations A and B 		Form 9

- Operational Summary – CAN BUS, Iterations C and D  	Form 10

- LSPI Cycle Count and Type Summary  				Form 11

- LSPI Events Summary-Iteration A  				Form 12

- LSPI Events Summary-Iteration B  				Form 13

- LSPI Events Summary-Iteration C  				Form 14

15  LSPI Events Summary-Iteration D  				Form 15

16  Chemical Analysis  						Form 16

17. Hardware Information 						Form 17

- Downtime Record						Form 18

- Comment Record							Form 19

- ACC Conformance 						Form 20

# APPENDIX

(Nonmandatory Information)

# X1. SOURCES OF INFORMATION, PARTS, AND MATERIALS

X1.1 General:

X1.1.1 The following sources are provided for convenience only. This does not represent an exclusive or complete listing of required materials or information sources.

X1.2  Engine Measurement Record Forms:

X1.2.1  The necessary engine measurement record forms are shown in tables A9.1 to A9.3.

X1.3  Sources Of Information:

X1.3.1  ASTM Test Monitoring Center—Direct all communications to the TMC to:

ASTM Test Monitoring Center,

6555 Penn Ave.,

Pittsburgh, PA 15206-4489.

X1.3.2  Test Sponsor—Direct all communications with the test sponsor (Ford Motor Co.) to:

Ford Motor Company,

17225 Federal Drive,

Allen Park, MI 48101

X1.3.3 Fuel Information and Availability—Obtain general information concerning EEE Lube Cert fuel, including availability, from:

Haltermann Products,

1201 S. Sheldon Rd.,

P.O. Box 249,

Channelview, TX 79530-0429.

X1.4 Sources of Materials:

X1.4.1 Aeroquip Hose and Fittings—Obtain from:

Aeroquip Corp.,

1225 W. Main,

Van Wert, OH 45891.

X1.4.2  Intake-Air Humidity Instruments—Dewpoint meters from the following sources are suitable for measurement of the intake-air specific humidity:

- Alnor (the Dewpointer)

- EG & G

- Foxboro

- Hy-Cal

- General Eastern

- Protimeter.

X1.4.3  Heat Exchangers—Obtain ITT Standard Heat Exchangers from:

Kinetics Engineering Corp.,

2055 Silber Road, Suite 101,

Houston, TX 77055.

X1.4.4 Fuel Flow Measurement—Mass fuel flowmeters are available from:

Micro Motion Corp.,

7070 Winchester Circle,

Boulder, CO 80301.

X1.4.5 Parts Washer and Chemicals—A dishwasher type parts cleaner and associated chemicals can be obtained from:

Better Engineering Manufacturing,

8361 Town Court Center,

Baltimore, MD 21236-4964.

X1.4.6  Crankcase and Intake-Air Pressure Gauges—Obtain from:

Dwyer Instrument Co.,

Junction of Indiana State Highway 212 and U.S. Highway 12,

P.O. Box 373,

Michigan City, IN 46360.

X1.4.7  Tygon Hose—Tygon hose is available through local Cadillac Plastic Co. distributors or the following supplier:

The Norton Co.,

12 East Avenue,

Tallmadge, OH 44278.

X1.4.8  Special Tools for the Test Engine—Special tools to facilitate assembly and disassembly of the engine are available from:

Any Ford dealership

or

Owatonna Tool Co.,

2013 4th St.,

NW Owatonna, MN 55060.

X1.4.9 Ultrasonic Parts Cleaner—Obtain TierraTech model MOT500NS ultrasonic parts cleaner or similar from:

TierraTech,

Draper Business Park,

12227 South Business Park Drive,

Suite 100,

Draper, UT 84020.

sales@tierratech.com.

X1.4.10 Ultrasonic Cleaner—Obtain Brulin 815 GD and 815 QR-NF from:

BHC (Formerly Brulin & Co, Inc.),

2920 Dr Andrew J Brown Ave,

Indianapolis, IN 46205.

www.bhcinc.com.

X1.4.12 Parts Cleaning Soap—Commercially available soap.  Tide has been found suitable for this purpose. It is manufactured by:

Proctor and Gamble Company,

1 P&G Plaza,

Cincinnati, OH 45202,

USA.

www.pg.com.

X1.4.13 Ford camshaft alignment tool—Obtain Ford P/N 303-1565 from a Ford or Lincoln dealer.

X1.4.14 Crankshaft TDC timing peg—Obtain Ford P/N 303-507 from a Ford or Lincoln dealer.

X1.4.15 Dynamometer—Obtain Midwest dynamometer model MW-1014A from: OHT (see X1.5.2);

or

Dyne Systems, Inc.,

W209 N17391 Industrial Drive,

Jackson, WI 53037 USA, tel:800-657-0726;

or

Dyno One Inc.,

14671 N 250 W Edinburgh,

IN 46124.

info@dyno-one.com; Tel 812-526-0500.

X1.4.16 Rear Motor Mount—manufactured by Quicksilver, P/N 6628-A. www.quicksilver-products.com.

X1.4.17 Carburetor Cleaner—Obtain Chemtool B12 from:

Berryman Products, Inc,

3800 E. Randol Mill Rd,

Arlington, TX 76011.

Tel: +1 800 433 1704; www.berrymanproducts.com.

X1.5 Sources of Engine Parts:

X1.5.1 Test Engine Parts—Procure the required engine parts (including the PCM calibration number U502-HBBJ0-v1-7-VEP-371.VBF) from the test sponsor (Ford Motor Co.):

Ford Motor Co.,

Ford Component Sales,

290 Town Center Dr.,

Dearborn, MI 48126.

X1.5.2  Various Parts:

X1.5.2.1 Obtain the following parts from:

OH Technologies,

9300 Progress Pkwy.,

Mentor, OH 44060.

- Coolant inlet and outlet

- Flywheel

- Bellhousing

- Engine wire harnesses.

A1.5.2.2 Obtain the following parts from:

Test Engineering, Inc.,

12758 Cimarron Path, Ste. 102,

San Antonio, TX 78249-3417.

- Modified cylinder head

- Piston ring tension measurement.

A1.5.3 Type 5 or Type 52 Intercooler: Obtain from FrozenBoost Inc., www.frozenboost.com.

ASTM Test Monitoring Center, 6555 Penn Avenue, Pittsburgh, PA 15206-4489. www.astmtmc.cmu.edu.

Until the next revision of this test method, the ASTM TMC will update changes to this method by means of Information Letters. Information Letters may be obtained from the TMC.

For referenced ASTM standards, visit the ASTM website, www.astm.org, or contact ASTM Customer Service at service@astm.org. For Annual Book of ASTM Standards volume information, refer to the standard’s Document Summary page on the ASTM website.

Available from ANSI, 1899 L Street, NW, 11th Floor, Washington, DC 20036. Tel: +1 202 293 89020; www.ansi.org.

The sole source of supply of this component known to the committee at this time is Ford Motor Co., 290 Town Center Dr, Dearborn, MI 48126.

If you are aware of alternative suppliers, please provide the information to ASTM International Headquarters. Your comments will receive careful consideration at a meeting of the responsible technical committee which you may attend.

The sole source of supply of this part known to the committee at this time is OH Technologies, 9300 Progress Pkwy., Mentor, O 44060, USA.. Tel: +1 440 354 7007. www.ohtech.com.

The sole source of supply of this part known to the committee at this time is Kinetics Engineering Corp., 2055 Silber Road, Suite 101, Houston, TX 77055.

Available from Ford dealership as well as select auto parts stores.

Available from OH Technologies, 9300 Progress Pkwy., Mentor, OH 44060, or from Dyne Systems, Inc. W209 N17391 Industrial Drive, Jackson, WI 53037 USA 800-657-0726; dtnesystems.com, or from Dyno One, Inc. 14671 N 250 W Edinburgh, IN 46124, info@dyno-one.com. Tel 812-526-0500.

The sole source of supply of this system known to the committee at this time is AVL Gmbh, Platz 1, A-8020, Graz, Austria. www avl.com.

The sole source of supply of this fuel known to the committee at this time is Haltermann Products, 1201 Sheldon Road, P.O. Box 429, Channeview, TX 777530, USA. www.haltermansolutions.com.

Test Engineering Inc., 12758 Cimmaron Path, Ste. 102, San Antonio, TX 78249-3417.

Available from any Ford dealership or from Owatonna Tools Co., 2013 4th St., NW Owatonna, MN 55060.

The sole source of supply of this bracket known to the committee at this time is Quicksilver. www.quicksilver-products.com.

Available from retailers and autopart stores.

FrozenBoost Inc., www.frozenboost.com.

The sole source of supply of this product known to the committee at this time is TierraTech, Draper Business Park, 12227 South Business Park Drive, Suite 100, Draper, UT 84020. sales@tierratech.com.

The sole source of supply of this product known to the committee at this time is Brulin Holding Company, 2920 Dr Andrew J Brown Ave, Indianapolis, IN 46205. www.bhcinc.com.

The sole source of supply of this product known to the committee at this time is Berryman Products, Inc, 3800 E. Randol Mill Rd, Arlington, TX 76011. Tel: +1 800 433 1704; www.berrymanproducts.com.

Available from the ASTM Test Monitoring Center, 6555 Penn Avenue, Pittsburg, PA 15206-4489, Attention: Administrator.

National Institute of Standards and Technology, 100 Bureau Drive, Stop 2300, Gaithersburg, MD 20899-2300. Email: calibrations@nist.gov. Phone: +1 301 975 2200.

Emerson Automotive Solutions, Micro Motion Corp., 7070 Winchester Circle, Boulder, CO 80301. www3.emersonprocess.com.

Loctite is a registered trademark of Henkel Corporation.

Available from Henkel. Corporation, One Henkel Way, Rocky Hill, CT 06067, USA. www henkelna.com.

The sole source of supply of this detergent known to the committee at this time is Proctor and Gamble Company, 1 P&G Plaza, Cincinnati, OH 45202, USA. Tel.  +1-513-983-1100. www.pg.com.

see LTMS document available from TMC at www.astmtmc.cmu.edu/ftp/docs/ltms/ltms.pdf.