Date:

To: Subcommittee D02.B0 members

Technical Contact: Lyle Bowman, lbowman@namwobl.com, 415- 479 -3004

Work Item: WK49675

Ballot Action: New engine oil test method

Rationale: This test method is expected be in a new engine oil specification

Standard Test Method for

Determination of Timing Chain Wear in a Turbocharged, Direct Injection, Spark Ignition, Four-Cylinder Engine

This standard is issued under the fixed designation X XXXX; the number immediately following the designation indicates the year of original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A superscript epsilon () indicates an editorial change since the last revision or reapproval.

INTRODUCTION

Portions of this test method are written for use by laboratories that make use of ASTM Test Monitoring Center (TMC) services (see Annex A1-A4).

The TMC provides reference oils, and engineering and statistical services to laboratories that desire to produce test results that are statistically similar to those produced by laboratories previously calibrated by the TMC.

In general, the Test Purchaser decides if a calibrated test stand is to be used. Organizations such as the American Chemistry Council require that a laboratory utilize the TMC services as part of their test registration process. In addition, the American Petroleum Institute and the Gear Lubricant Review Committee of the Lubricant Review Institute (SAE International) require that a laboratory use the TMC services in seeking qualification of oils against their specifications.

The advantage of using the TMC services to calibrate test stands is that the test laboratory (and hence the Test Purchaser) has an assurance that the test stand was operating at the proper level of test severity. It should also be borne in mind that results obtained in a non-calibrated test stand may not be the same as those obtained in a test stand participating in the ASTM TMC services process.

Laboratories that choose not to use the TMC services may simply disregard these portions.

  - Scope

1.1 Undesirable timing chain wear has been observed with gasoline turbocharged direct injection (GTDI) engines in field service, and data from a correlating laboratory engine test have shown that appropriately formulated engine lubricating oil minimizes that wear. A refined version of the correlative laboratory engine test has been developed to provide a means for screening lubricating oils for that specific purpose. The laboratory engine test is 216 h in length, conducted under varying conditions, and the increase in timing chain length determined at the end of test is the primary result.

1.2 The values stated in SI units are to be regarded as the standard. (Values in parentheses are provided for information.)

1.2.1 Exception—Where there is no direct SI equivalent such as screw threads, national pipe threads/diameters, tubing size, or specified single source equipment.

1.3 This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use. See Annex A6 for general safety precautions.

1.4 Table of Contents:                       	                                     		     Section

Scope                                                                                        	1

Referenced Documents	2

Terminology 	3

Summary of Test Method	4

Significance and Use	5

Apparatus	6

Test Engine	6.1

Reagents	7

Preparation of Apparatus 	8

Chain and Camshaft Installation	8.20.6

Timing Chain Measurement	8.21.5

Electronic Throttle controller	8.18

Measurement Instrumentation	8.24

Test Procedure	9

Break-in Procedure	9.1.1

Engine Operation Procedure	9.2

Cycling Schedule	9.2.4

Stages and Ramps	9.2.4.3

Oil Level Check and Sampling	9.4.1

Blowby Flow Rate Adjustment	9.7

Diagnostic Data review	10			 Test Results	11

Primary Result – Timing Chain Elongation	11.1.1

Report	12

Precision and Bias	13

Test Precision	13.1

Keywords	14

ANNEXES

ASTM TMC - Organization	A1

ASTM TMC - Calibration Procedures	A2

ASTM TMC – Maintenance Activities	A3

ASTM TMC – Related Information	A4

Engine Parts	A5

Assembled Test Engine	A5.1

Safety Precautions	A6

Engine Rebuild Templates	A7

Cylinder Head Measurements	A8.1

Cylinder Bore Measurements	A8.2

Bearing Journal Measurements	A8.3

Various Engine Part Photographs and Figures	A9

Typical Ramps (temperature, torque, blowby)	A9.23

Control and Data Acquisition Requirements	A10

APPENDIXES

Sources of Materials and Information	X1.

Engine Brackets - Schematics	X2.

2. Referenced Documents

2.1 ASTM Standards :

D235  Specification for Mineral Spirits (Petroleum Spirits) (Hydrocarbon Dry Cleaning Solvent)

D4175 Terminology Relating to Petroleum, Petroleum Products, and Lubricants

2.2 American National Standards Institute

ANSI MC96.1

3. Terminology

3.1 Definitions:

3.1.1 blowby, n—in internal  combustion engines, the combustion products and unburned air-and-fuel  mixture that enter the crankcase. D4175

3.1.2 engine oil, n—a liquid that reduces  friction or wear, or both, between the moving parts within an engine; removes  heat, particularly from the underside of pistons; and serves as a combustion  gas sealant for piston rings.

3.1.2.1 Discussion—It may contain additives to enhance certain properties.  Inhibition of engine rusting, deposit formation, valve train wear, oil oxidation, and foaming are examples. D4175

3.1.3 wear, n—the loss of material from a surface, generally occurring between two surfaces in relative motion, and resulting from mechanical or chemical action or a combination of both. D4175

3.2 Definitions of terms Specific to This Standard:

3.2.1 timing chain, n--the part of an internal combustion engine that synchronizes the rotation of the crankshaft and the camshaft(s) so that the engine's valves open and close at the proper times during each cylinder's intake and exhaust strokes; in this engine, the timing chain is a roller chain configuration.

3.2.2 PCM, n--an engine control unit, most commonly called the powertrain control module (PCM), is an electronic device that instantaneously controls a series of actuators on an internal combustion engine to ensure optimal engine performance.

4.  Summary of  CW (Chain Wear) Test Method

4.1 The test engine is completely rebuilt before each test.

4.2 The timing chain length is measured before and after engine break in, and at the end of test (216 h). The test is conducted for 54 cycles, each 4 h cycle consisting of operation at two stages with differing operating conditions.

4.3 The increase in timing chain length, determined at the end of test, is the primary test result.

5. Significance and Use

5.1 This test method evaluates an automotive engine oil's lubricating efficiency in inhibiting timing chain lengthening under operating conditions selected to accelerate timing chain deformation. Varying quality reference oils were used in developing the operating conditions of the test procedure.

5.2 The test method can be used to screen lubricants for satisfactory lubrication of an engine timing chain, and has application in automotive engine oil specification

6. Apparatus – General Description

6.1 Timing Chain Test Engine

(1) The test engine is a Ford 2.0 L, spark ignition, four stroke, four-cylinder, GTDI engine4,7, with dual overhead camshafts driven by a timing chain, four valves per cylinder and electronic fuel injection.

(2) Assembled test engine part number and description (Table A5.1).

(3) Configure a test stand to accept the test engine. (Suggested arrangement (X2.1)

6.2 Reusable Engine Parts and Fasteners

(1) All other engine parts, than the ‘Required New Engine Parts’, can be used for six maximum tests as long as they remain serviceable (see Tables A5.2 and A5.3).

(2) Crankshaft and bearings, connecting rods and bearings, pistons, camshafts, timing chain covers, cylinder blocks , cylinder head assemblies, turbocharger, PCV valve and fuel injectors may be used for a maximum of 6 tests as long as they remain serviceable.

(3) The PCV valve is flow tested before each test to ensure it meets the required flow. These parts should be kept together as a set for all 6 tests.

(4) Damaged threads in the block can be corrected with commercially available thread inserts.

6.3 Required New Engine Parts for each test (the “Test Parts”)

(1) The Test Parts and Gaskets Lists (Tables A5.4 and A5.5) describe these parts.

(2) Use new valve train drive parts and piston rings for each test.

(3) Do not modify or alter test parts without the approval of the CW Test Surveillance Panel.

6.4 Additional Related Parts and Tools

(1) The Test Stand Setup Parts and Special Parts Lists (Tables A5.6 and A5.7, respectively), with a few noted exceptions, can be reused for numerous tests as long as they remain serviceable.

(2) Engine parts other than valve train and drive parts can be replaced during the test, provided the reason for  replacement was not oil related.

6.5 Special service tools

(1) A complete list of special tools for the test engine is shown in (Table A5.8)

(2) The tools are available from a Ford dealership.

(3) These are designed to aid in performing several service items, in addition to the following specific service items that require special tools to perform the functions indicated (if not self-explanatory).

6.6 Specially Fabricated Engine Parts

(1) The following subsections detail the specially fabricated engine parts required in this test method:

(2) Intake Air System can be fabricated but must use the stock 2012 Explorer air cleaner assembly (Table A5.6, X1.2) and MAF.

(3) Use a modified oil pan with dipstick, fill port and pick up tube listed in (Table A5.7, X1.28)

Note 1 – Sources for some materials and information provided in Appendix X1.

6.7 Other Special Equipment

(1) Use an appropriate air conditioning system to control the temperature and pressure of the intake air to meet the requirements listed in Tables 3 and 4.

(2) An appropriate fuel supply system is necessary.

(3)  The control and data acquisition system requirements are listed in Annex A10.

6.8 Driveline

(1) Use the flywheel, clutch, pressure plate, bell housing, clutch spacer listed in Table A5.7  (X1.28)

6.9 Special Engine Measurement and Assembly Equipment

(1) Items routinely used in laboratory and workshop are not included.

(2) Use any special tools or equipment shown in the 2012 Explorer service manual for assembly.

(3) A list of these tools is provided in Table A5.8.

(4) Complete any assembly instructions not detailed in Section 7 according to the instructions in the 2012 Explorer Service Manual.

6.9.1 Piston ring positioner

(1) Use the piston ring positioner to locate the piston rings from the cylinder block deck surface by 38 mm.

(2) This allows the compression rings to be positioned in a consistent location in the cylinder bore for the ring gap measurement.

6.9.2  Piston Ring Grinder

(1) A ring grinder is required for adjusting ring gaps.

(2) A suitable ring grinder is suggested in See 8.18.2.

7. Reagents and Materials

7.1 Degreasing Solvent

7.1.1 Use only mineral spirits meeting the requirements of Specification D235, Type II, Class C for Aromatic Content (0 % to 2 % by volume), Flash Point (61 °C, min) and Color (not darker than +25 on Saybolt Scale or 25 on Pt-Co Scale). (Warning—Combustible. Health hazard.) Obtain a Certificate of Analysis for each batch of solvent from the supplier.

7.2 Organic Solvent

7.2.1 Penmul L460-- (Warning—Combustible. Health hazard.)5,7  (X1.20)

7.3 Test Fuel

7.3.1 Use only EEE unleaded fuel6,7 (Warning—Flammable. Health Hazard.) (X1.6)

7.4 Test Oil

7.4.1 A minimum quantity of 23 L (6 gal) required.

7.5 Engine Coolant

7.5.1 Shell Zone Dex-Cool concentrate mixed 50/50 with deionized water  (X.1.33)

7.6  Ultrasonic Cleaner

7.6.1 Tierra Tech ultrasonic solution 7 and B  (X1.17).

7.7 Parts Cleaning Soap

7.7.1 NAT-50 or PDN-50 are acceptable. (Warning—Health hazard.) (X1.21)

5 Penmul L460 can be obtained from Penetone Corp., P.O. Box 22006, Los Angeles, CA 90022

6 General information concerning EEE fuel, including availability, can be obtained from the following: Haltermann Products, 1201 S. Sheldon Rd., P.O. Box 249  Channelview, TX 79530-0429

7 If you are aware of alternative suppliers, please provide this information to ASTM International Headquarters. Your comments will receive careful consideration at a meeting of the responsible technical committee, which you may attend.

8. Preparation of Apparatus

8.1  Engine Parts Cleaning

8.1.1 Rinse parts with parts cleaning soap, NAT-50 or PDN-50 before putting into ultrasonic cleaner.

8.1.2 Clean the cylinder block, cylinder heads, pistons, oil pan and front cover using Tierra Tech model MOT500NS ultrasonic parts cleaner or similar apparatus. (X1.16).

8.1.3The ultrasonic parts cleaner solution, Ultrasonic solution 7 and B, is also available from Tierra Tech,.

8.1.4 Put all of the following components into the ultrasonic parts cleaner for 30 min:

(1) Cylinder block with main bearings. Oil jets are removed.

(2) Bare pistons without wristpins (The piston compression and oil rings are removed from each piston prior to going into the ultrasonic cleaner; they will get replaced with a new set)

(3) Bare cylinder head (No valve train components)

(4) OHT oil pan

(5) Front cover

8.1.5 Ultrasonic parts cleaner details

(1) Add solution once that in the ultrasonic cleaner reaches a minimum of 60 ºC (140 °F).

(2) DO NOT add the degreasers until the ultrasonic mixture has reached a temperature of 60 ºC (140 °F).

(3) Add 20.82 L (5 .5 gal) of ultrasonic solution 7

(4) Add 1.83 L  (0.5( gal) of ultrasonic solution B

(5) Change the soap and water solution at least after every 25 h of use.

Note 2: The solution shown above is based upon the MOT-500NS model (1900 L capacity). Quantities will be different for a different size unit.

8.1.6 Cleaning procedure details

8.1.6.1 After 30 min, the parts are removed and immediately sprayed with hot water, then solvent and left to air dry.

8.1.6.2 The remaining components are spray-cleaned with degreasing solvent then blown out with pressurized air and left to air dry:

(1) Camshafts and all valve train.

(2) Intake manifold/ Throttle body (not being separated)

(3) Fuel pump housing with piston.

(4) Vacuum pump and oil screen.

(5) Intake and outlet of the turbocharger are lightly wiped down with solvent.

(6) The oil screen is also cleaned. (We don’t clean the inside of the turbocharger)

(7) The carbon build up on the injectors is wiped of

(8) Oil Pump

(9) VCT solenoids are sprayed with solvent.

(10) Valve Cover

(11) Turbo charger oil lines

(12) Oil separator (PCV housing on the cylinder block)

(13) Oil pick up tube

(14) Oil squirters/jets

(15) Crankshaft

(16) Rods and pins

(17) All valvetrain

(18)The test batch camshaft sprockets and crankshaft gear.

(19) The test batch timing chain is cleaned as described in the Timing Chain Cleaning Procedure (See 8.21.1).

8.2  Cylinder Deglazing

8.2.1 Use a flexible cylinder hone Flex Hone Model: GB33432 and Pneumatic Honing Drill, Westward 1/2 Reversible Air Drill, Model: 5ZL26G to deglaze the cylinder walls. (X1.18 and X.1.19)

8.3  PCV Valve Flow Rate Device

(1) Use this device to verify the flow rate of the PCV valve before the test and measure the degree of clogging after the test.

(2) Fabricate the device according to the details shown in Fig. 1.

(3) The device shall have a full scale accuracy of 5 % and a resolution of 0.05 L/s.

NOTE 1—The inlet flow meter must calibrate to within 5 % of the standard (pre-calibrated) orifices at the pressure differentials stamped on the orifices.

FIG. 1  PCV Valve Flow Test Apparatus

8.4  Miscellaneous Engine Components-Preparation

8.4.1 Engine Build-Up and Measurement Area-Environment

(1) The ambient atmosphere of the engine buildup and measurement areas shall be reasonably free of contaminants.

(2) A relatively constant temperature (within ± 3 °C) is necessary to ensure acceptable repeatability in the measurement of parts dimensions.

(3) To prevent moisture forming on cold engine parts that are brought into the buildup or measurement areas, maintain the relative humidity at a nominal maximum of 50 %.

8.5  Throttle Body:

8.5.1  Clean the butterfly and bore of the throttle body with carburetor cleaner (Chemtool B12, X1.34) and air-dry before each test.

(1) Do not disassemble the throttle body as this will cause excessive wear on the components.

(2) The idle air screw can be removed for the cleaning process.

(3) Fully close the idle air screw during test operation.

(4) There is no specific life for the throttle body. However, the clearance between the bore and the butterfly will eventually increase and render the body unserviceable.

(5) When the clearance becomes too great to allow control of speed, torque, and air-fuel ratio, discard the throttle body.

8.6  PCV Valve—Measure and record the flow rates of the PCV valve with the calibrated flow device described in Fig. A8.19.

(1) Measure the flow rate at 27 kPa and 60 kPa vacuum.

(2) Because of the hysteresis in the PCV valve spring, make the vacuum adjustments in one direction only.

(3) Measure the flow rate twice and average the readings.

(4) Reject any PCV valve that does not exhibit an average flow rate of 36 L/min to 54 L/min at 27 kPa and 19 L/min to 21 L/min at 60 kPa

8.7  Water Pump Drive System—Use only the pulleys and belt provided in the test stand set-up parts list (Table A5.6), crankshaft pulley, water pump and pulley, tensioner, and six groove belt shown in Fig. 2.

FIG. 2  Water Pump Drive Arrangement

8.8  Oil Separators—Clean with degreasing solvent (See 7.1) and allow to air-dry.

8.9  Assembling the Test Engine-Preparations—Use the long block obtained from the supplier (X1.1).

(1) If this is the first test on a new engine, disassemble the long block in accordance with the 2012 Explorer workshop manual.

(2) Required new parts and reusable parts are listed in Table A5.

8.10  Parts Selection—Instructions concerning the use of new or used parts are detailed in See 6.2 - 6.6.

8.11  Sealing Compounds—Use a silicon-based sealer as needed  on the contact surfaces between the rear seal housing and oil pan and  the front cover and cylinder block, cylinder head and oil pan.

(1) Use Motorcraft Gasket Maker (TA-16) or equivalent between the  6th intake and exhaust camshaft cap and the cylinder head.

(2)   Use silicon-based sealer sparingly since it can elevate the indicated silicon content of the used oil.

NOTE 3—Non-silicon liquid or tape thread sealers can be used on bolts and plugs.

8.12  Gaskets and Seals—Install new gaskets and seals during engine assembly.

8.13  Block Preparations—Inspect block, including oil galleries for debris and rust.

(1) Remove any debris or rust that is found.

(2) Remove oil gallery plugs.

(3) Removal of coolant jacket plugs is left to the discretion of the laboratory.

8.14  Deglazing Procedure: Deglazing is performed after ultrasonic cleaning under the following conditions to achieve a 9 µm (Ra) to 13 µm (Ra) surface finish and 30º ± 5º degree crosshatch:

(1) Mount the engine block in an engine stand or suitable fixture so it is secure and will not move during    deglazing operation.

(2) Rinse cylinder bores with degreasing solvent.

(3) Deglaze cylinder bores using drill and hone shown in Figs. 3 and 4

(4) Run the drill at 500 r/min horizontal drill speed for 25 to 35 vertical strokes over elapsed time of 20 s to 25 s. There should be a steady supply of lubricant supplied during each stroke.

(5) Use a 50/50 ratio of degreasing solvent and EF411, as the hone lubricant.

(6) Clean cylinders after honing deglazing with warm/hot water or hot water and detergent (Tide is suitable) using a brush, then oil cylinders with EF411.

(7) Replace ball hone after deglazing 24 engine blocks

Fig. 3: Pneumatic Honing Drill

Pneumatic Honing Drill

Brand: Westward

1/2 Reversible Air Drill

Model: 5ZL26G

Speed: 500 r/min

620 kPa (90 psig), max

Fig. 4: Cylinder Hone

Flexible Cylinder Hone

Flex, Model: GB33432

Bore Diam.: 95.25 mm (3.75 in.)

Abrasive material: Silicon Carbide Grit

8.15 Crosshatch Procedure:

8.15.1 Apparatus

(1) HatchView Software

(2) USB microscope.

(3) Computer System Requirements: Windows XP, Vista or Windows 7 (32 or 64 bit), an available USB 2.0 port is required for live “video” viewing.

8.15.2 Preparation:

(1) Cylinder should be clean of any oil or residue from honing to maintain consistency of measurements.

(2) Adjust focus of camera while face of the camera is placed against the cylinder wall.

(3) Set camera resolution to 640x480 and 30 fps.

(4) Use the identification feature available in the program to title the image with cylinder number and test number.

8.15.3 Measurement:

(1) The measurement is taken at the rear most longitudinal position of each cylinder.

(2) The measurement is taken at 38.1 mm (1.5 in.) down from the top of the cylinder deck. A ruler is used to measure.

(3) The measurement is to range for 25° to 35° with a target of 30°

8.16 Crankshaft preparation

(1)  Clean the crankshaft (See 8.1)

(2)  Spray the crankshaft with degreasing solvent.

(3)  Measure the main journals and connecting rods journals (horizontal diameter, vertical diameter) bearing inside diameter and clearance and verify that they meet the service limits.

(4) The crankshaft is polished with 400 grit 3M utility cloth while it is still lightly coated in degreasing solvent.

(5)A final finish is given using 600 grit crocus cloth. The crankshaft is cleaned with degreasing solvent for the final time.

8.17  Piston and rod assembly

(1) Clean the pistons according to See 8.1.

(2)Measure piston, piston pin and pin rod hole diameters to ensure they meet service limits.

(3)Install the pistons on the connecting rods per the procedure in the 2012 Explorer workshop manual.

8.18  Piston Rings

8.18.1 Ring Gap Adjustment:

(1) The piston rings are cleaned and wiped with EF411 to get the factory coating off.

(2) The first ring is gapped to 1.651 mm (0.065 in.) and the second ring is gapped to 1.778 mm (0.070 in.).

(2a) Typically, these gaps have been shown to produce acceptable blowby levels with the surface finish and crosshatch pattern achieved in See 8.14.

(3) However, to achieve an average blowby of 65 L/min to 75 L/min, an adjustment may be necessary immediately before or after the 24 h measurement

(4) A 24 h blowby value of at least 70 L/min is recommended to produce an average blowby of 65 L/min to 75 L/min for the remainder of the test.

(5) Ring gap adjustments are not allowed once the test has resumed after the 24 h blowby reading. This recommendation is included because the test will be invalid if the blowby drops below 65 L/min after the 24 h reading.

(6) The ring placement is 38 mm (1.5 in.) from the deck, using piston ring setter (Fig. A7.1).

8.18.2 Piston Ring Cutting Procedure:

(1) Cut the top and second compression ring gaps to the required gap using the Sanford Piston Ring Grinder. (X1.22)  ring cutting burr (X1.24) rotated at a rated speed of 3450 r/min.

(2) Remove equal amounts from both sides of the gap. Make final cuts on the down stroke only.

(3) The ring is cut with a maximum increment of 0.125 mm until the desired ring gap is achieved.

(4) After the rings are cut remove the ring from the cutting tool, debur using a Sunnen soft stone (X1.24) and wipe with a dry towel.

8.18.3 Installation:

(1) Install the oil control rings and the compression rings on the pistons with the gaps located over the piston pin.

(2) Position the gaps at approximately 180° intervals, with the top compression ring gap toward the rear.

(3) Install the rings using a ring spreader tool, keeping the rings' surfaces parallel to the ring groove in the piston.

(4) If any rings require replacement, then measure and record the new ring gap(s)

8.19 Cylinder Bore Measurements

(1) Measure the cylinder bores with the bearing caps in place.

(2) Clean the bores with a dry rag. The bores shall be clean and dry when they are measured.

(3) Use a bore gage micrometer, along with the bore ladder (Fig. A.7.2), to determine the diameter of cylinders at the top, middle and bottom.

8.20  Assembling the Test Engine

8.20.1 Assemble the engine according to the instructions in the 2012 Explorer service manual unless specified herein.

8.20.2 Cylinder block

(1) The heater hose tube is removed from the block as shown in Fig. 5 and plugged with a 3.2 mm (5/8 in.) freeze plug coated in RTV.

Figure 5: Cylinder Block Heater Hose Tube

8.20.3 Piston Installation

(1) Install piston and rod assemblies in proper cylinders, taking care to ensure rings are not damaged during installation.

(2) Wipe the cylinders with EF-411 (X1.13).

(3) Install the pistons and connecting rods with the notches facing the rear.

(4) Install the rod bearing caps and torque according to the procedure in the 2012 Explorer workshop manual.

8.20.4 Oil System Components

(1) All oil system components in the engine are production configuration with the exception of the oil pan and the oil pickup tube, shown in Fig. 6.

8.20.5 Cylinder Head Installation

(1) Obtain cylinder heads from a supplier listed in X1.28.

(2) Heads may be used for up to six tests, as long as they remain serviceable.

(3)  Disassemble heads and inspect for any debris or other deleterious materials and remove as necessary.

(4)  Clean the cylinder head in the Ultrasonic cleaner as described in See 8.1.

(5)  Determine valve guide clearance at the top and middle of the heads on the transverse side of the guide.

(6) Reject any heads that exceed the service limits shown in the 2012 Explorer work shop manual.

(7) Measure and record intake and exhaust valve springs, spring free length, and spring load at a compressed height of 28.7 mm.

(8) Verify the compressed spring load is 460 N ± 21 N. Reject any springs not meeting this criteria.

(9) Assemble the cylinder heads in accordance with the service manual.  The valves are lapped before installation and new intake and exhaust valve seals are installed.

(10) Set the valve lash per the procedure in the workshop manual and record the valve lash.

8.20.6 Chain and Camshaft Installation Procedure

(1) Measure the test chain according to the Timing Chain Measurement Procedure  (See 8.21.5) prior to installing it in the engine.

(2) Install camshaft and timing chain according to the procedure in the 2012 Explorer workshop manual.

(3) If using the Ford camshaft alignment tool (Ford P/N 303-1565) (X1.25) be sure not to let it bind in slots at the rear of the camshafts. It should be loose after the timing chain installation is complete.

(3a) Be sure camshaft positioning tool is flat before installing.

(4) Use a spanner on the harmonic balancer or a flywheel lock to hold the crankshaft.

(4a) Alternate method, the crankshaft positioning crankshaft TDC timing peg (Ford P/N 303-507) (X1.26) can be used to hold the crankshaft in place while performing this installation.

(5) Install the timing chain with the lettering on the black link facing forward. This will ensure the chain is installed in the same orientation if/when it is removed and reinstalled during the test.

(6) Coat the timing chain with test oil every time it is installed in the engine other than the pre break in installation.

(6a) Coat the timing chain with EF-411 when it is first installed before break in.

(7) Install the chain tensioner and guides according to the 2012 Explorer workshop manual.

(8) After the tensioner is installed and the pin is pulled from the tensioner to release the tensioner arm, do not move or apply any force to the tensioner arm.

8.20.7  Balance Shaft Housing

(1) Do not install the balance shaft housing; it cannot be used with the test oil pan.

(2) Remove the balancer and plug the oil passage with a CFM Balance Shaft Delete Kit (Part number 1-0180).

8.20.8  Oil Pan and Baffle

(1) Install oil pan baffle to the oil pan as shown in Fig. 6.

(2) Install the oil pan according to the procedure in the 2012 Explorer service manual.

Oil Pan

Fig. 6

8.20.9 Water Pump, Water Pump Drive

(1) Install the water pump and pulley, the crankshaft pulley, and tensioner according to the 2012 Explorer service manual.

(1a) These are the only components needed to drive the water pump. All other production front end accessory drive components do not need to be installed.

(2) Do not use the engine to drive any external engine accessory other than the water pump.

(3) Pull back tensioner and install water pump drive belt as shown in Fig. 7.

(4) Ensure that there is a minimum contact angle of 20° between the drive belt and the water pump pulley.

FIG. 7 Water Pump Drive Arrangement

8.20.10 Engine cooling system

(1) Coolant inlet and outlet available from the supplier listed in X1.28.

(2) Do not install the thermostat.

(3) Plumb the external coolant system, see Figs. A9.1 and A9.2.

(4) Use coolant flow meter with and accuracy of ±1 %.

(5) A radiator cap is used to limit system pressure to 105 kPa.

(6) Pressurize the coolant system to 70 kPa ± 10 kPa at the top of the coolant reservoir

(7) Control the engine coolant flow rate and outlet temperature in accordance with the specifications listed in Table 4.

(8) Cyclic ramping specifications are detailed in Table 5.

(9) Prior to running each reference calibration test, inspect the engine coolant system components, external to the engine, and clean as needed.

(10) The coolant side of the system typically doesn’t needed cleaning, but the process water side may need routine cleaning.

(10a) While a specific flushing technique is not specified, the process should include use of a commercial descaling cleaner .

8.20.11 Cylinder block oil separator

(1) Install a dummy PCV valve (PCV valve with the internal components removed) in the oil separator on the side of the engine block.

(2) A functional PCV is located at the stand in the external ventilation system, and crankcase pressure is measured in this location.

8.20.12 Oil cooling system

(1) Use the production oil cooler (BB3Z-6A642-A) attached to the oil filter adapter.

(2) Use process water on the coolant side to control the oil temperature.

(3) Control oil temperature by a valve on the process water inlet line to adjust the flow of process water through a feedback loop from the ‘oil in’ thermocouple location.

8.21 Timing Chain

8.21.1 New chain preparation

(1) Place a new timing chain into an ultrasonic bath with degreasing solvent for 20 min.

(2) Remove the chain from the ultrasonic cleaner and dip into room temperature degreasing solvent to cool chain.

(3) Dip the chain in heptane or solvent 142 to prevent rust.

(4) Oil chain by dipping in EF-411.

(5) Install the chain in the engine for engine break in

8.21.2 After break in

(1) After break in remove the chain from the engine.

(2) Place the chain into an ultrasonic bath with degreasing solvent for 20 min.

(3) Remove the chain from the ultrasonic cleaner and dip into room temperature degreasing solvent to cool chain.

(4) Dip the chain in heptane or solvent 142 to prevent rust.

(5) Oil chain by dipping in EF-411.

(6) Hang the chain to let excess oil run off and let the chain cool off for a minimum of 2 h in the metrology lab before starting the after break in measurement procedure. This will allow the temperature of the chain to stabilize.

8.21.3 Chain measurement after break in

(1) Dip the chain in degreasing solvent to remove EF-411 then dip the chain in new test oil.

(2) Install the chain in the engine for the start of test.

(Note: Do not clean the timing chain if it is removed during the test for an engine repair)

8.21.4 End of test

(1) At the end of test, remove the timing chain from the engine.

(2) Place the timing chain into an ultrasonic bath with degreasing solvent for 20 min.

(3) Remove the chain from the ultrasonic cleaner and dip into room temperature degreasing solvent to cool chain.

(4) Dip the chain in heptane or solvent 142 to prevent rust.

(6) Oil chain by dipping in EF-411.

(7) Hang the chain to let excess oil run off and let the chain cool off for a minimum of 2 h in the metrology lab before starting the measurement procedure. This will allow the temperature of the chain to stabilize

8.21.5 Chain measurement - general

(1) The timing chain is measured two times during the test; after the 8 h engine break in and at the end of the test.

(2) Use the Motorized chain measurement apparatus, MCMR 1000 (X1.31) shown in Fig. 8

(3) Parts list show in A5.8

Fig.8: Chain Measurement Apparatus

8.21.6 Chain measurement - rig calibration

(1) Check calibration on the measurement apparatus before every test chain measurement using a reference

chain and ensure the reference chain measurement is within ± 25.4 µm (± 0.001 in.) of the previous

measurement then proceed to next step.

(2) If reading is larger, then investigate source of error.

(3) Adjust the rig to achieve a measurement within 25.4 µm (0.001 in.) of the last correct reading.

(4) The lab needs to have a single new unused chain that is used as a reference chain and this chain is only

used for calibrating the measurement apparatus.

8.21.7 Chain measurement - procedure

(3) Orient the sprockets of the measurement apparatus such that they are aligned with their alignment orientation marks.

(4) Install chain on measurement apparatus with the “key” link in the standard (aligned) location.

(5) Ensure that the USB digital interface cable between the indicator and the computer is connected and that the first cell of the spreadsheet is selected into which the data will begin being entered.

(6) Energize the drive motor on the chain measurement apparatus and run until a minimum of 30 chain lengths worth of reading have been captured (207 sprocket revolutions)

(7) When complete, examine the averages for the three measurement ranges and verify the total range does not exceed ± 0.008 mm (± 0.0003 in.); if it does, repeat the measurement by overwriting the data.

8.21.8 Chain measurement – results (see 11.1.1)

(1) Determine the averages for the three measurement ranges

(2) Determine the average of those three subset average measurements

(3) This average is used as the final chain measurement in the calculation below:

Chain elongation = 2 x (final average measurement-initial average measurement)/nominal chain length. The nominal chain length is 43.125 in.

8.22 Test stand installation

8.22.1 Functions that are to be performed in a specific manner or at a specific time in the assembly process are noted.

8.22.2 Test engine

(1) Mount the engine on the test stand so that the flywheel friction face is 0.0° ± 0.5° from vertical.

(2) Four motor mounts are used (Quicksilver part# 6628-A) as shown in Fig. A9.3, Fig. A9.4, and Fig. A9.5.

(3) Drawings of the mount brackets are shown in X2.1 and X2.2.

(4) The engine must be at 0.0° ± 0.5° role angle.

8.22.3 Flywheel

(1) The flywheel bolts get lightly coated with Loctite 565 to prevent any oil from seeping out of the holes.

(2) Torque the flywheel 108 N.m to 115 N.m.

(3) Obtain the flywheel from the supplier (see X.1.28).

8.22.4 Clutch and pressure plate

(1) Obtain the clutch, pressure plate and spacer from the supplier (see X1.28).

(2) Put the flat side on the clutch toward the engine.

(3) The spacer goes between the flywheel and pressure plate.

(4) Torque the pressure plate bolts to 25 N.m to 33 N.m.

(5) Each clutch gets replaced every 6 runs.

8.22.5 Driveline

(1) The driveline is greased every test.

(2) Driveline specifications:

(2a) Driveline Degree: 1.5° ±  0.5°

(2b) 595 mm ± 13 mm installed length from flange-to-flange

(2c) 1410 series flanges

(2d) 69.9 mm (2.75 in.) pilot

(2e) 95.25 mm (3.75 in.) bolt circle

(2f) 88.9 mm (3.50 in.) by 2.11 mm (0.083 in.) stub and slip

8.22.6 Dynamometer: Use Midwest dynamometer model 1014A.

(1) Dynamometer can be purchased from the vendor listed in X1.27

8.22.7  Exhaust System and Gas Sampling Fittings:

(1) A typical exhaust system, and fittings for backpressure probes, O2 sensors and thermocouple are illustrated in Fig. A9.8.

(2) Exhaust components should be constructed of either solid or bellows pipe/tubing.

(3) Other type flexible pipe is not acceptable.

(4) The backpressure probes can be used until they become unserviceable.

(5) If the existing probes are not cracked, brittle, or deformed, clean the outer surface and clear all port holes.

(6) Check the probes for possible internal obstruction and reinstall the probes in the exhaust pipe.

(7) Stainless steel probes are generally serviceable for several tests; mild steel probes tend to become brittle after one test.

(8) Exhaust gas is noxious.

(9) (Warning—Any leaks in the connections to the sample probe will result in erroneous readings and incorrect air-fuel ratio adjustment.)

8.22.8 Fuel Management System

(1) The fuel injectors can be used for 6 tests.

(2) Inspect the O-rings to ensure they are in good condition and will not allow fuel leaks, replace if necessary.

(3) Install the fuel injectors into the fuel rail and into the cylinder head.

(4) Fuel system schematic shown in Fig. 9

Fig. 9

Fuel System Schematic

8.22.9 Powertrain Control Module

(1) The engine uses a PCM provided by Ford Motor Company to run this test.

(2) The PCM contains a calibration developed for this test

(3)  Use a PCM that contains calibration U5J0110D1VEPfn13_78_2.

(4) The PCM module is available from the supplier listed in X1.32.

(5) The PCM power shall come from a battery 13.5 V ± 1.5 V or a power supply that does not interrupt/interfere with proper PCM operation.

(6) Connect the PCM battery/power supply to the engine wire harness with an appropriate gage wire of the shortest practical length so as to maintain a dc voltage of 12 V to 15 V and minimize PCM electrical noise problems.

(7) Ground the PCM ground wire to the engine.

(8) From the same ground point, run a minimum two gage wire back to the battery negative to prevent interruption/interference of the PCM operation.

(9) The power supply can also be used for the Lambda measuring devices.

8.22.10 Spark Plugs

(1) Install new Motorcraft CYFS-12-Y2 spark plugs.

(2) Spark plugs come pre-gapped.

(3) Torque the spark plugs to 9 N·m to 12 N·m.

(4) Do not use anti-seize compounds on spark plug threads.

8.22.11 Crankcase Ventilation System

(1) The crankcase ventilation system is a closed system allowing blowby to be vented from the crankcase and drawn into the intake manifold.

(2) The metal parts of the crankcase ventilation system get flushed with carburetor cleaner (Chemtool B12) or any equivalent solvent after every test, then blown out with pressurized air and are left to air dry.

(3) All the hoses (i.e. tygon) get replaced every test.

(4) If using a smooth bore Teflon braided stainless steel hose, these can be reused after cleaning in an organic degreaser (Penmul L460).

(5) A schematic of the crankcase ventilation system (Fig. 10), and a photograph (Fig. 11) are shown.

3-way valve connection

2-way valve connection

Fig. 10: Schematic - Crankcase Ventilation System

Fig. 11 Crankcase Ventilation System

8.22.11.1 System description

(1) Blowby flows through the oil drain back passages in cylinder block and head and through the front cover and out through the camshaft cover.

(2) The blowby heat exchanger and oil separator prevents loss of oil, fuel and water into PCV system.

(3) A typical heat exchanger cooling system is shown in Fig. A9.6.

(4) The PCV valve flows approximately 120 L/min. Blowby flowrate is 65 L/min to 75 L/min.

(5) When excessive plugging of the PCV valve occurs or there is excess blowby, the blowby is vented to the fresh air tube after the mass air flow sensor.

(6) A dummy PCV valve (PCV valve with the internal components removed) placed in the stock PCV valve location in the block-mounted oil separator is used for crankcase pressure measurement.

8.22.12 Blowby Heat Exchanger and Oil Separator

(1) Use ITT Heater exchanger S-160-02-008-002 (X1.8) and Moroso oil separator, Part number 85487 (X1.29).

(2) Disassemble and soak both in Penmul L460 (X1.20) for 24 h.

(3) Rinse with hot water, then rinse a final time with degreasing solvent and let air dry.

8.22.13 Intake Air Components

(1) Install the  fresh air tube, air cleaner assembly, and new air filter.

(2) Modify the air cleaner assembly to accept fittings for inlet air temperature thermocouple and pressure tap as shown in Fig. A2.12.

(3) The excessive blowby tube is shown connected to the fresh air tube after the MAF sensor.

(4) Use the 2012 Explorer fresh air tubes, or fresh air tubes can be fabricated but must be 1040 mm ± 25 mm from the MAF sensor to the turbocharger inlet.

8.22.14 Water to Air Turbocharger Intercooler

(1) Use water to air intercooler (A9.5) capable of achieving the required air charge temperature (Table 4) and an

average system pressure loss less than 3 kPa in both stages

(2) The intercooler accumulates significant amounts of  blowby condensate during each test.

(3) The air side of the intercooler must be spray cleaned with degreasing solvent, rinsed with hot water and left to air dry before each test.

(4) Use commercial Aqua Safe descaler to clean the water side.

8.22.14.1 Intercooler Tubing

(1) Fabricate the intake air system with 51 mm ID stainless steel tubing from the turbocharger to the intercooler and 64 mm ID stainless steel tubing from the intercooler to the throttle body.

(2) The tubing length is not specified but should be the appropriate length to achieve the required air charge temperature and system pressure loss.

(3) Locate the MAPT sensor 305 mm ± 25 mm from the intake surface of the throttle body and the intake air charge temperature thermocouple 25 mm downstream from the MAPT sensor.

(4) The post-intercooler turbo boost pressure measurement probe should be placed a minimum of 25.4 mm (12 in.) upstream from the MAPT sensor.

(5) The pre- intercooler turbo boost pressure measurement probe should be placed a minimum of 25.4 mm (12 in.) downstream from the turbocharger outlet.

(6) Typical installation is shown in Fig. 12, the measurements can be seen in Fig. A2.13.

Figure 12, Typical Intercooler Installation

8.22.15  External Hose Replacement

(1) Inspect all external hoses used on the test stand and replace any hoses that have become unserviceable.

(2) Check for internal wall separations that could cause flow restrictions.

(3) Check all connections to ensure security.

8.22.16  Wiring Harness

(1) There are two wiring harnesses used on the test stand, a dynamometer harness that connects to the stand power and PCM and an engine harness.

(2) Obtain the dynamometer wiring harness and engine wiring harness from the supplier listed in X1.28, A9.2.

8.22.17 Electronic Throttle Controller

(1) Throttle is controlled using simulated accelerator pedal position signals.

(2) The dynamometer wiring harness is supplied with an Accelerator Pedal Position jumper cable with un-terminated pigtail leads.

(3) The test laboratory must connect two voltage command signals, Acc Pos Sensor 1 and Acc Pos Sensor 2, to the Accelerator Pedal Position jumper cable.

(4) The voltage control ranges for each signal are shown in Table 1.

(5) The wiring schematic and pin-out description for this connection is shown in Fig. 13.

(6) The voltage signals must be run through a voltage isolator otherwise interference will occur between the lab DAC system and the engine ECU and throttle control will be erratic.

Table 1: Accelerator Position Sensor Control Ranges

| Command Signal | Operating Range | Min Signal (Idle) | Max Signal (WOT) |
| --- | --- | --- | --- |
| Acc Pos Sensor 1 | 0 Vdc to 5.0 Vdc | 0.75 Vdc (15 %) | 4.25 Vdc (85 %) |
| Acc Pos Sensor 2 | 0 Vdc to 2.5 Vdc | 0.375 Vdc (15 %) | 2.125 Vdc (85 %) |
| Note: Acc Pos Senor 2 should always equal 50 % of Acc Pos Sensor 1 |  |  |  |

Figure 13: Accelerator Position Wiring Schematic

8.23  Engine Fluids (Supply/Discharge Systems)

8.23.1 Air supply system

(1)  Condition the intake air to 32 °C ± 0.5 °C, 11.4 g/kg ± 0.8 g/kg humidity, and pressurized to 0.05 kPa ± 0.02 kPa.

(2) 8.1.1 The supply system shall be capable of delivering 110 L/s of conditioned air, while maintaining the intake/air parameters detailed in Table 4.

(3) The test stand intake air duct system is not specified.

8.23.2 Dew Point

(1) The dew point may be measured in the main system duct or at the test stand.

(2) If the dew point is measured in the main system duct, verify the dew point periodically at the test stand.

(3) Maintain the duct surface temperature above the dew point temperature at all points downstream of the humidity measurement point to prevent condensation and loss of humidity level.

8.23.3 Fuel System

(1) A schematic diagram of a typical fuel supply system is shown in Fig. 9.

(2) Supply an excess volume of fuel to the fuel rail at all times.

(3) The engine has a closed loop fuel system so excess fuel goes into the loop back to the heat exchanger.

(4) Deliver the fuel to a high-pressure engine driven pump that boosts the pressure and supplies the fuel to the fuel rail.

(5) Maintain the fuel temperature to the fuel rail below 50 °C.

(6) To ensure good atomization of the fuel, maintain the fuel pressure to the high pressure fuel pump above 413 kPa.

(7) In addition, the fuel pressure should be constant at all steady-state conditions to ensure good speed, power, and air-fuel ratio control.

8.23.4 Fuel details

(1) Approximately 1600 L of EEE Lube cert fuel are required for each test.

(2) Obtain EEE lube cert fuel from the supplier listed in X1.6.

(3) Laboratory storage tank may be filled with subsequent batches of fuel. A new batch of fuel may be added to existing fuel in the tank

(4) The fuel batch that is reported for a test is the last fuel batch that was added to the tank before the test started.

(5) A certificate of analysis accompanies each batch.

8.23.5  Engine Oil:

(1) The test oil sample shall be uncontaminated and representative of the lubricant formulation being evaluated.

(2) A minimum of 7.5 L of new oil is required to complete the test.

(3) A 20 L sample of new oil is normally provided to allow for inadvertent losses.

8.24 Measurement Instrumentation

8.24.1 Temperatures - general

(1) Temperature measurement locations for the six required temperatures are specified.

(2) Use thermocouples that are calibrated to 0.5 °C.

(3) Use only OEM temperature sensors for EEC inputs. (4) All thermocouples, except the intake-air thermocouple, shall be premium and sheathed.

(5) The intake-air thermocouple may be an open-tip type.

(6) The diameter and length of the thermocouples shall be 3 mm by 100 mm.

(7) Thermocouples, wires, and extension wires should be matched to perform in accordance with the special limits of error as defined in ANSI MC96.1.

8.24.1.1Temperature measurement locations

(1) Coolant inlet - Install the sensor in the coolant inlet on the engine (OHTVH-008-1) perpendicular to the run. Install sensor with the tip in the center of the stream of flow. (See Fig. A9.1).

(2) Coolant outlet - Install the sensor in the coolant outlet on the engine (OHTVH-009-1) perpendicular to the run. Install sensor with the tip in the center of the stream of flow. (See Fig. A9.1).

(3) Engine oil inlet- Install the tip of the sensor at the center of the flow stream in the external oil filter adapter (see Fig. A9.3) through the hole for the oil pressure switch (not used). Install a tee to accept this temperature sensor and attach the oil pressure line.

(4) Engine oil outlet - Install the tip of the sensor at the center of the cross fitting attached to the side opposite from the engine oil inlet temperature sensor on the oil filter adaptor. The adapter needs to be modified with a 1/8 NPT hole to access the oil passage (see Fig. A9.3).

(5) Intake air -  Install the tip of the thermocouple midstream in the air cleaner box downstream of the filter (see Fig. A9.16). Insertion depth shall be 37 mm ± 2 mm.

(6) Fuel – Install the sensor in the fuel line before the high pressure pump.

(7) Air Charge – Install the sensor in the intercooler outlet tube 25 mm ± 2 mm downstream from the MAPT sensor. Locate the tip at the center of the flow. (See Fig. A9.4)

(8) Pre-intercooler – Install a sensor in the tube between the turbocharger and the intercooler (See Fig A9.4).  PAUSE

(9) Exhaust – Install a sensor 140 mm ± 12 mm downstream on the exhaust flange (see Fig. 2.8)

(10) Blowby gas – Install a sensor at the gas outlet of the blowby heat exchanger

8.24.1.2 Thermocouple calibration

(1) Calibrate all thermocouples prior to a reference oil test.

(2) The temperature measurement system shall indicate within ± 0.5 °C of the laboratory calibration standard.

(3) The calibration standard shall be traceable to NIST.

Figure A2.15 Oil cooler showing oil gallery pressure location

8.24.2 Pressures - general

(1) Pressure measurement for each of the eight required parameters is detailed in the following sections, allowing reasonable opportunity for adaptation of existing test stand instrumentation.

(2) However, the accuracy and resolution of the pressure measurement sensors and the complete pressure measurement system shall meet the requirements of the DACA-II document.

(3) Replace pressure sensors that are part of the EEC system with only Ford specified equipment.

NOTE 5—Tubing between the pressure tap locations and the final pressure sensors should incorporate condensate traps, as indicated by good engineering practice. This is particularly important in applications where low air pressures are transmitted by means of lines that pass through low-lying trenches between the test stand and the instrument console.

8.24.2.1 Pressure measurement locations

(1) Manifold Absolute Pressure (MAP) – Measure the manifold absolute pressure at the port downstream of the throttle-body on the front side of the intake manifold (See Fig 2.13)

(2) Engine oil -  Measure oil pump pressure in the external oil filter adapter (see Fig. A2.16) through the hole for the oil pressure switch (not used). Install a tee to accept the temperature sensor and attach the oil pressure line.

(3) Coolant—Measure engine coolant pressure at the top of the coolant reservoir as shown in Fig. A2.3.

(4)  Fuel – Measure fuel pressure in the lower pressure fuel line at the exit of the stand fuel pump.

(5) Crankcase oil – Measure crankcase oil pressure at the dummy PCV valve in the cylinder block oil separator.

(6) Exhaust gas - Measure the exhaust back pressure with the exhaust gas sampling probe located 76 mm ± 12 mm downstream of the exhaust flange (see Fig. A2.8).

(6a) A sensor capable of absolute or gage measurement corrected with barometric pressure reading is recommended.

(6b) Install a condensate trap between the probe and sensor to accumulate water present in the exhaust gas.

(7) Inlet air – Measure inlet air pressure in the air cleaner downstream of the air filter. (See Fig A2.12)

(8) Pre-intercooler gas – Measure the pre-intercooler pressure with the exhaust gas sampling probe located 155 mm ± 25 mm downstream of the turbocharger flange (See Fig 2.13)

(9) Boost (post-intercooler) Measure the post-intercooler pressure with the exhaust gas sampling probe located downstream of the intercooler and at least 305 mm upstream of the MAPT sensor. (See Fig 2.13)

(10) Cylinder head oil– Measure cylinder head pressure at the oil gallery plug on the left side of the cylinder head next to the belt tensioner.

8.24.2.2 Pressure sensor calibration

(1) Calibrate all pressure measurement sensors prior to a reference oil test.

(2) The MAP pressure measurement system shall indicate within 0.1 kPa of the laboratory calibration standard.

(3) All other pressure measurement systems shall conform to the guidelines in ASTM Research Report RR:D02-1218.22

(4) The calibration standard shall be traceable to NIST

8.24.3  Flow rates – general

(1) Flow rate measurement for each of the four required parameters is detailed in the following subsections.

(2) With the exception of the engine coolant and blowby flow rates, measurement equipment is not specified for a given parameter.

(3) This allows reasonable opportunity for adaptation of existing test stand instrumentation.

8.24.3.1 Flow rates - measurement

(1) Engine coolant - Determine the engine coolant flow rate using a flowmeter with an accuracy of ±1 % (see Fig. A2.3)

(1a) Flowmeter is available from the supplier in X2.1.6.

(2a) Take precautions to prevent air pockets from forming in the lines to the pressure sensor.

(3a) Transparent lines or bleed lines, or both, are beneficial in this application.

(4a) Ensure that the manufacturer’s requirements for orientation and straight sections of pipe are installed immediately up and down stream of the flowmeter.

(2) Blowby heat exchanger  coolant—Measure the total volumetric coolant flow rate through the blowby heat exchanger  system as shown in (See Fig. A2.11).

(3) Fuel – Measure fuel flow in kg/hr on the low pressure fuel system before the high pressure engine fuel pump.

8.24.3.2  Flow devices – calibration

(1) Calibrate the flowmeters used in the measurement of both the engine coolant flow rate and blowby heat exchanger  coolant flow prior to a reference oil test.

(2) Calibrate the flowmeters as installed in the system at the test stand with test fluid.

(3) Calibrate the flowmeters with a turbine flowmeter or by a volume/time method at Stage 1 and 2 operating conditions.

8.24.4  Blowby

(1) Measure the blowby flow rate using the apparatus shown in Fig. 9.

(1a) The measurement system routes the blowby through an external, sharp-edged orifice and into the atmosphere.

(1b) Maintain crankcase pressure during operation of the system at 0.0 Pa ± 25 Pa to minimize the potential for crankcase leakage.

(1c) Mount the orifice plate in a vertical position.

(2) Determine the blowby flow rate by measuring the differential pressure drop across the sharp-edged orifice

(3) An inclined manometer or differential pressure sensor is required for measurement of the differential pressure drop.

(3a) The differential pressure drop sensor shall have a range from 0 kPa to 1 kPa.

(4) Fabricate the sharp-edged orifice assembly that is specifically designed for blowby flow rate measurement in strict compliance with the specifications that are available from the TMC.

(5) Additional information on the orifice system can be obtained from the source listed in X2.1.8

(6) The assembly contains five orifices.

(6a) The 9.525 mm orifice is generally satisfactory for the range of blowby flow rate encountered.

(7) The complete orifice assembly can also be purchased from the supplier listed in X2.1.11.

9.  Test Procedure

9.1  Pre-test Procedure:

9.1.1  Engine Break-In Procedure—Run break-in schedule listed in Table 2.

(1) Conduct the break-in before each test using the test oil.

(2) The break-in procedure has 12 steps and is 8.25 h long.

(3) There are 30 s ramps between steps that are counted as part of the 8.25 h.

(4) Flush the engine during the break-in procedure.

(4a) There are a total of 3 oil flushes as shown in Table 2; drain the oil for 15 min after each flush.

9.1.1.2 Install a pre-measured timing chain in the engine as listed in section 8.20.6 Chain and Camshaft Installation Procedure.

(1) Coat the timing chain with EF-411 oil before break-in installation.

9.1.1.3 Charge the engine with 3600 g of test oil.

(1) Prime and install a new oil filter.

9.1.1.4 The engine is now ready to start Step 1 of the break-in as listed in Table 2.

# TABLE 2 Sequence CW Break-in Schedule

| Step | Speed (r/min) | Load (N·m) | Time per stage (h:min) | Total Time (h:min) |
| --- | --- | --- | --- | --- |
| Charge engine with 3600 g of new test oil and new oil filter |  |  |  |  |
| 1 | Idle | 0 | 0:30 | 0:30 |
| Oil Flush 1 -Shut engine down and drain used test oil and remove oil filter. Add 3600 g of new test oil and install new oil filter |  |  |  |  |
| Start engine and let idle for 5 min |  |  |  |  |
| 2 | 1500 | 38 | 0:30 | 1:00 |
| 3 | 2000 | 72 | 0:30 | 1:30 |
| 4 | 2500 | 111 | 0:30 | 2:00 |
| 5 | 3000 | 135 | 0:30 | 2:30 |
| 6 | 3000 | 150 | 3:15 | 5:45 |
| 7 | 2000 | 72 | 0:15 | 6:00 |
| 8 | 3250 | 155 | 0:15 | 6:15 |
| 9 | 3500 | 155 | 0:15 | 6:30 |
| 10 | 3750 | 155 | 0:15 | 6:45 |
| 11 | 4000 | 155 | 1:15 | 8:00 |
| Bring engine to idle for 5 min and shut down. |  |  |  |  |
| Oil Flush 2- Shut engine down and drain used test oil and remove oil filter. Add 3600 g of new test oil and install new oil filter. |  |  |  |  |
| 12 | Idle | 0 | 0:15 | 8:15 |
| Oil Flush 3- Shut engine down, drain used test oil and remove oil filter. |  |  |  |  |

9.1.1.5 The controlled parameters during break-in are listed in Table 3.

(1) All other controls are left wide open/free flowing.

(2) The engine does not produce enough heat in the early steps to reach all target temperatures.

(3) All controlled parameters are expected to be on target at the beginning of Step 4.

# TABLE 3 Sequence CW Break-in Controlled Parameters

| Break-in Controlled Parameters |  |
| --- | --- |
| Coolant Out Temp. | 85 oC |
| Oil Gallery Temp. | 100 oC |
| Inlet Air Pressure | 0.05 kPa |
| Air Charge Temp. | 37 oC |
| Inlet Air Temp. | 30 oC |

9.1.1.6 The laboratory ambient atmosphere shall be reasonably free of contaminants.

(1) The temperature and humidity levels of the operating area are not specified.

(2) A fan is allowed to divert air toward the turbocharger during break-in only.

9.1.1.7 The break-in allows an opportunity to check PCM system operation, check for leaks in the various systems and purge air from the cooling systems.

(1) Specifications concerning the break-in procedure are shown in Table 2 and Table 3.

(2) The engine start-up and shutdown procedures are detailed in 12.2.1 and 12.2.4 respectively.

9.1.1.8 The same test PCM calibration U5J0110D1VEPfn13_78_2 is used during break in.

(1) Step 2 is a good time to check if the Lambda enrichment in the PCM calibration is working properly.

9.1.1.9 Perform Oil Flush 1 at the end of Step 1.

(1) Drain the used oil and remove the used oil filter.

(2) Let the oil drain for 15 min.

(3) Charge the engine with 3600 g of new test oil.

(4) Prime a new oil filter with test oil and install.

(5) The engine is now ready to start Step 2 of the break-in.

(6) Continue to run the break-in until the end of Step 11 with the same oil charge.

9.1.1.10 Perform Oil Flush 2 at the end of Step 11 after the engine has idled for 5 min and shuts down.

(1) Drain the used test oil and remove the used oil filter.

(2) Let the oil drain for 15 min.

(3) Charge the engine with 3600 g of new test oil.

(4) Prime a new oil filter with test oil and install.

(5) The engine is now ready to start Step 12 of the break-in.

9.1.1.11 Oil Flush 3 is performed at the end of Step 12.

(1) Drain the used test oil and remove the used oil filter.

(2) Let the oil drain for 15 min.

9.1.1.12 Remove the timing chain for cleaning and 0 h measurement according to the Timing Chain Cleaning Procedure (see 8.21.2) and Timing Chain Measurement Procedure (see 8.21.7).

(1) After measuring the chain, coat the chain in new test oil and install it back into the engine using the procedure described in the Timing Chain and Camshaft Installation Procedure (see 8.20.6).

9.1.1.13 After the timing chain has been installed, measure 3600 g of test oil.

(1) With a portion of this 3600 g of new test oil, prime a new oil filter and install it on the engine.

(2) Charge the engine with the remaining new test oil for the final oil charge.

9.1.1.14 Start and run the engine at idle for 5 min, then shut down the engine.

(1) After the engine is shutdown for 20 min ± 2 min, record the dipstick level in millimeters.

(2) Rotate the calibrated dipstick 360 degrees while still in the oil pan to capture the oil level at the highest point.

(3) Remove the dipstick to view the reading.

(4) Break-in and the initial oil level measurement is now completed and test is ready to begin.

(5) No makeup oil is added.

9.2  Engine Operating Procedure:

9.2.1  Engine Start-up—Use the following detailed procedure each time the engine is started.

(1) Turn on the ignition, safety circuits, fuel management system, fuel pump, and the blowby coolant pump.

(2) Ensure  the intake-air supply duct is connected.

9.2.2 Crank The Engine—The engine should start within 4 s.

(1) Since the engine has a crankshaft-driven oil pump, cranking oil pressure might be low.

(2) If used, disable a low oil pressure ignition shutoff during engine starting to allow the engine to start even though the oil pressure is low.

(3) The inclusion of this type switch could lead to excessive cranking time to start the engine.

9.2.2.1 If starting difficulties are encountered, the laboratory should not continue to crank the engine excessively.

(1) Perform diagnostics to determine the reason the engine will not start (ignition problems, insufficient or excess fuel, and so forth).

(2) Warning— Excessive cranking times can promote additional fuel dilution of the test oil and can adversely affect the test. In addition to other precautions, do not attempt to pour gasoline into the intake-air horn.

9.2.3 Test Start —Conduct the test according to the operational parameters shown in Table 4.

(1) The test stage and ramp order are shown in Table 5.

# TABLE 4 Test Operational Parameters

| Parameter | Units | Stage 1 | Stage 2 |  |
| --- | --- | --- | --- | --- |
| Duration | min | 120 | 60 |  |
| Engine Speed | r/min | 1550 ± 5 | 2500 ± 5 |  |
| Torque | N·M | 50 ± 2 | 128 ± 2 |  |
| Oil Gallery Temperature | oC | 50 ± 0.5 | 100 ± 0.5 |  |
| Coolant Out Temperature | oC | 45 ± 0.5 | 85 ± 0.5 |  |
| Coolant Flow | L/min | 40 ± 2 | 70 ± 2 |  |
| Inlet Air Pressure | kPa | 0.05 ± 0.02 |  |  |
| Coolant Pressure | kPa | 70 ± 2 |  |  |
| Inlet Air Temperature | oC | 32 ± 0.5 |  |  |
| Exhaust Back Pressure | kPa | 104 ± 2 | 107 ± 2 |  |
| Air Charge Temperature | oC | 30 ± 0.5 |  |  |
| AFR | Lambda | 0.78 ± 0.05 | 1 ± 0.05 |  |
| Blowby outlet Temperature | oC | 23 ± 2 | 78 ± 2 |  |
| Humidity | g/kg | 11.4 ± 1.0 |  |  |
| Blowby | L/min | 65 - 75 |  |  |

9.2.3.1 Start the engine and let idle for 5 min then shut the engine down, these 5 min do not count toward test time.	(1)  Take a dip 20 min ± 2 min after the engine shutdown.

(2) Follow the procedure in section 9.4.1 on how to take the dip reading.

(2) Record the 0 h dip reading.

9.2.3.2 Start the engine and let idle for 5 min, these 5 min do not count toward total test time.

(1) Start the 30 min ramp to Stage 1 conditions.

(2) The test timer starts at the beginning of this ramp to Stage 1.

(3) Use the ramping conditions shown in Table 5.

9.2.4  Cyclic Schedule, General Description:

9.2.4.1 The test is composed of two stages as shown in Table 4 and 5.

(1) Together, the two stages and two ramps comprise one cycle. Each cycle lasts 4 h and is repeated 54 times for a total of 216 h.

(2) Six consecutive cycles are completed each 24 h period.

(3) Perform oil level measurement and sampling every 24 h.

(4) The oil level measurement and sampling procedure does not count toward test time and is described in section 9.4.1

9.2.4.2 Test Cycle: Each cycle is 4 h long and contains a Stage 2-1 ramp for 30 min (or start up/idle to Stage 1 at test start or after an oil dip), a Stage 1 for 120 min, a Stage 1-2 ramp for 30 min, and a Stage 2 for 60 min. This 4 h sequence is the only time that is counted as test time.

9.2.4.3 Ramps: The ramps between stages are 30 s (engine speed and coolant flow), 30 min (oil and coolant temperature) and 60 min (blowby temperature), to stabilize at stage conditions.

(1) The load ramps are different lengths.

(2) Ramp details are shown in Table 5.

(3) The ramps are considered complete after 30 min when the oil and coolant temperatures have reach stage conditions; at this time the stage timer starts.

(4) Note that half of the blowby temperature ramp occurs during stage operation.

(5) The coolant and oil temperature ramps are linear ramps between the steady state stage conditions, within ± 2 min, for the first 25 min to reach the next stage conditions.

(6) After the next stage, oil and coolant temperatures are achieved between 23 min and 27 min, with the last remaining minutes of the 30 min ramp used to stabilize at the stage conditions shown in Table 4.

(7) Figure A2.23 shows the desired shape of the ramps.

(8) The rate of speed, temperature, fuel and torque changes, as well as the amount of enrichment between stages, can influence test severity and engine component wear. Therefore, ramping rates are very important.

# TABLE 5 Stages Order and Ramp Description

| Stage | Description | Time (min) |
| --- | --- | --- |
| Stage 1 | Stage 1 conditions | 120 |
| Ramp 1 – 2 (or start up/idle to stage 2) | Linear 30 s speed and flow ramps. 3 min to 3.5 min torque ramp. Linear 30 min oil and coolant temperature ramp. 60 min blowby temperature ramp, to Stage 2 (Ramp 1-2 details below) | 30 |
| Stage 2 | Stage 2 conditions | 60 |
| Ramp 2 – 1 (or start up/idle to stage 1) | Linear 30 s speed and flow ramps. 3.5 min to 4.5 min torque ramp. Linear 30 min oil and coolant temperature ramp. 60 min blowby temperature ramp, to Stage 1 (Ramp details below) | 30 |
| Stage ramp | Ramp details |  |
| Stage 1-2 torque ramp | 30 s 95 N·m to 100 N·m 90 s 115 N·m to120 N·m 180 s to 240 s 126 N·m to 130 N·m |  |
| Stage 2-1 torque ramp | 30 s 75 N·m to 85 N·m 90 s 55 N·m to 60 N·m 150 s to 180 s 48 N·m to 52 N·m |  |
| Stage 1-2 oil temperature ramp | Linear ramp reach 75 oC by 12.5 min ± 2 min reach 100 oC ± 0.5 oC by 25 min ± 2 min remaining time used to stabilize at 100 oC± 0.5 oC | 30 |
| Stage 2-1 oil temperature ramp | Linear ramp reach 75 oC by 12.5 min ± 2 min reach 50 oC ± 0.5 oC by 25 min ± 2 min remaining time used to stabilize at 50 oC ± 0.5 oC | 30 |
| Stage 1-2 coolant temperature ramp | Linear ramp reach 65 oC by 12.5 min ± 2 min reach 85 oC± 0.5 oC by 25 min ± 2 min remaining time used to stabilize at 85 oC ± 0.5 oC | 30 |
| Stage 2-1 coolant temperature ramp | Linear ramp - reach 65 oC by 12.5 min ± 2 min - reach 45 oC ± 0.5 oC by 25 min ± 2 min remaining time used to stabilize at 45 oC ± 0.5 oC | 30 |
| Stage 1-2 blowby temperature ramp | Linear ramp from 23 oC to 73 oC reach 49 oC by 15 min ± 2 min reach 73 oC by 30 min ± 2 min Linear ramp from 73 oC to 78 oC, reach 78 oC ± 2 oC by 60 min (30 min of this ramp is run during Stage 2) | 60 |

| Stage 2-1 blowby temperature ramp | reach 55 oC by 15 min ± 2 min reach 32 oC by 30 min ± 2 min reach 23 oC ± 2 oC by 60 min (30 min of this ramp is run during Stage 1) | 60 |
| --- | --- | --- |

9.2.5 Engine Shutdown:

9.2.5.1  Scheduled Shutdown Procedure—Follow the procedure detailed below each time a scheduled shutdown is performed.

(1) Scheduled shutdowns include shutdowns that occur during engine break-in and oil leveling:

(2) Bring the engine speed to idle. Allow temperatures and flows to go free-flowing to cool the engine.

(3) Switch the ignition off.

(4) Turn off power to the ignition power source.

(5) Turn off fuel and coolant pumps.

(6) Reduce the intake-air pressure to atmospheric.

9.2.5.2 Unscheduled Engine Shutdown—Follow the procedure detailed below, each time an unscheduled engine shutdown is performed:

(1) Stop test timer when ramp down starts.

(2) 30 s ramp to idle and allow all temperatures and flows to go free-flowing to cool the engine down.

(3) Let the engine idle for a total of 2 min, the 30 s ramp down counts as part of the 2 min. Shut the engine down after 2 min.

(4) Switch the ignition off.

(5) Turn off fuel and coolant pumps.

(6) Reduce the intake-air pressure to atmospheric.

9.2.5.3 Start-Up After Oil Leveling Period—Follow the procedure detailed below each time an engine start-up is performed after an oil leveling period.

(1) Start—5 min in idle; then ramp to Stage 1 conditions for 30 min as shown in Table 5. The 5 min of idle does not count toward the total test time.

(2) The test timer starts at the beginning of the ramp to Stage 1 conditions.

9.2.6  Unscheduled Downtime—The oil leveling periods of 25 min ± 2 min are the only scheduled shutdowns allowed during the test.

(1) However, the test can be interrupted to perform necessary maintenance.

(2) Note all unscheduled downtime on the Supplemental Operational Data Form of the final test report.

9.2.7  Resumption of Test Time After Unscheduled Shutdown—After an unscheduled shutdown, test time does not begin until the engine has reached operating conditions for the stage at which the shutdown occurred.

(1) On start-up, idle for 5 min then use the ramp as shown in Table 5 for reaching the appropriate stage.

9.2.7.1 Start-Up After Unscheduled Shutdown—Follow the procedure detailed below, each time an engine start-up is performed after an unscheduled shutdown:

(1) Return to Stage 1—Engine idles for 5 min then ramp to Stage 1 conditions for 30 min using the ramp as described in Table 5.

(1a) The total test timer and stage timer resumes from where it left off before being shut down once Stage 1 conditions are reached.

(2) Return to Stage 2— Engine idles for 5 min then ramp to Stage 2 conditions for 30 min using the ramp as described in Table 5.

(2a) The total test timer and stage timer resumes from where it left off before being shut down once Stage 2 conditions are reached.

9.3 Periodic Measurements and Functions:

9.3.1  Blowby flow rate measurement - general

(1) Every sixth cycle, measure and record the blowby flow rate at 30 min to 45 min into Stage 2.

(1a) The engine shall be stable and operating at normal Stage 2 operating conditions.

(2) Measure blowby when the gas temperature is at least 32 °C.

(3) The installation of the blowby flow rate measurement apparatus is described in Fig. 9

(4) The procedure for measuring blowby flow rate is detailed in 9.3.1.1.

(5) Complete only one set (Stage 2) of blowby flow rate measurement during each six cycles.

(6) Under special circumstances additional blowby flow rate measurements can be performed to determine or verify a problem with the flow rate measurement apparatus or the engine.

(7) Record additional blowby flow rate measurements and an explanation of the reason for the additional measurements.

(7a) Include these data in the supplemental operational data in the final test report.

9.3.1.1 Blowby flow rate measurement - procedure

(1) Connect the blowby measurement device to the pressurized air source.

(2) Open the flow valve (bleeder valve) completely.

(3) Connect the blowby apparatus flow line to the 3-way valve located between the oil separator and intake tube.

(4) Position the 2-way valve to divert air to the monometer from the hollow PCV valve.

(5) Position the 2-way valve in between the PCV and throttle body to keep air from entering the throttle body.

(6) Position the 3-way valve to divert intake manifold vacuum from the engine PCV to the exhaust plumbing of the blowby apparatus meter.

(7) Adjust the flow valve (bleeder valve) to maintain crankcase pressure at 0 kPa to 0.025 kPa.

(8) Record the differential pressure across the blowby meter orifice, record the blowby gas temperature, and the barometric pressure.

(9) After completing the measurements, return the engine to normal operating configuration.

(9a) First, reposition the 3-way valve and both 2-way valves to ensure porting of the intake vacuum to the engine PCV; then,

(9b) disconnect the blowby apparatus hose from the closed port of the 3-way valve.

(10) Calculate the blowby flow rate and correct the value to standard conditions (38 °C, 100.3 kPa) using the calibration data for that orifice.

# Figure 9 Blowby Cart Connection

9.3.2 Parameter Logging

9.3.2.1 Refer to Table 6 for parameter logging information.

TABLE 6 Parameter Logging

|  | TEST POINT | UNITS |
| --- | --- | --- |
| Controlled | Engine Speed | r/min |
|  | Engine Torque | N•m |
|  | Coolant Out Temp | ºC |
|  | Oil Gallery Temp | ºC |
|  | Air Charge Temp | ºC |
|  | Inlet Air Temp | ºC |
|  | Inlet Air Press | kPaG |
|  | Exhaust Back Press | kPaA |
|  | Fuel Temp | ºC |
|  | Humidity | g/kg |
| Monitored | Fuel Flow | kg/hr |
|  | Manifold Absolute Pressure (MAP) | kPaA |
|  | Boost Pressure | kPaA |
|  | Barometric Pressure | kPaA |
|  | Oil Gallery Pressure | kPaG |
|  | Oil Head Pressure | kPaG |
|  | Oil Filter In Temp | ºC |
|  | Exhaust temp | ºC |
|  | Crank Case Pressure | kPaG |
|  | Fuel Pressure | kPaG |
|  | Power | kW |
|  | Pre-Intercooler Air Pressure | kPaA |
|  | Ambient Temperature | ºC |
|  | Coolant In Temperature | ºC |
|  | Coolant Pressure | kPaG |
|  | Coolant Flow | L/m |
|  | Blowby heat exchanger coolant | L/m |
|  | Lambda | unitless |
| PCM CAN BUS Channels | Ignition Timing Advance for #1 Cylinder | Deg CA |
|  | Absolute Throttle Position | % |
|  | Engine Coolant Temperature | ºC |
|  | Inlet Air Temperature | ºC |
|  | Equivalence Ratio (Lambda) | unitless |
|  | Absolute Load Value | % |
|  | Intake Manifold Absolute Pressure | kPa |
|  | Fuel Rail Pressure | kPa |
|  | Accelerator Pedal Position | % |
|  | Boost Absolute Pressure - Raw Value | kPa |
|  | Turbocharger Wastegate Duty Cycle | % |
|  | Actual Intake (A) Camshaft Position | Deg |
|  | Actual Exhaust (B) Camshaft Position | Deg |
|  | Intake (A) Camshaft Position Actuator Duty Cycle | % |
|  | Exhaust (B) Camshaft Position Actuator Duty Cycle | % |
|  | Charge Air Cooler Temperature | º C |

Table 7 PCM Parameter Logging Information

Table 8 Typical Uncontrolled Parameter Ranges

| Parameter | Stage 1 | Stage 2 |
| --- | --- | --- |
| Fuel Flow, kg/h | 3.2 – 3.5 | 8.0 – 8.5 |
| Exhaust Temperature, °C | 400 - 430 | 640-680 |

9.4 Oil Sampling:

9.4.1 Oil level Measurement and Sampling Procedure— Oil level measurement and sampling are scheduled at intervals of 24 h or 6 cycles.

(1) The procedure and sample times are listed in Table 9.

(2) The total test timer stops after every 6th cycle and Stage 2 has completed.

(3) Perform a 30 s (speed and load) ramp to idle and let the engine idle for 4.5 min.

(4) Take an oil sample during these 4.5 min of idle.

(5) Remove an oil sample from the valve attached to the T connected to the oil filter housing.

(5a) The location of the T where the oil is drawn is shown in Figure A9.15.

9.4.2 The minimum oil level allowed is indicated by the 100 mm mark on the calibrated oil dipstick.

(1) Rotate the calibrated dipstick 360 degrees while still in the oil pan to measure the highest mark.

(2) Remove the dipstick to view the mark.

# TABLE 9 Oil Level Measurements and Sampling

|  | Test Hours | 24 | 48 | 72 | 96 | 120 | 144 | 168 | 192 | 216 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Test Cycles | 6 | 12 | 18 | 24 | 30 | 36 | 42 | 48 | 54 |
| 1 | Remove a 120 mL to 150 mL purge sample while the engine is at idle. |  |  |  |  |  |  |  |  |  |
| 2 | Remove a 60 mL analysis sample while the engine is at idle. |  |  |  |  |  |  |  |  |  |
| 3 | Shut-down the engine 5 min after the start of oil sampling and leveling stage. |  |  |  |  |  |  |  |  |  |
| 4 | Immediately return the purge sample to the engine. |  |  |  |  |  |  |  |  |  |
| 5 | Record the dipstick level in millimeters 20 min ± 2 min after the engine is shutdown. |  |  |  |  |  |  |  |  |  |
| 6 | Log the oil level. The difference between the oil level and the Test Full mark is oil consumed or gained. Use the chart in Table 12 to determine the level. |  |  |  |  |  |  |  |  |  |
| 7 | Restart the engine after shutdown. |  |  |  |  |  |  |  |  |  |

9.5 General Maintenance

(1) The scheduled shutdown periods of 30 min during oil leveling allow limited opportunity for engine and stand maintenance.

(2) In addition, the test can be shut down at any convenient time to perform unscheduled maintenance; however, minimize the duration of a shutdown. Report any unscheduled shutdown on the Supplemental Operational Data Sheet.

9.6 Special Maintenance Procedures

(1) Functions that require special maintenance procedures are listed in this section.

(2) These maintenance procedures are specifically detailed because of the effect on test validity or because they require special care while being completed.

(3) Check the oil level before performing any maintenance requiring removal of the front cover or rear seal housing.

(3a) If the level is above 130 mm, the oil level is above the oil pan rail and a portion of the oil must be removed from the oil drain plug before performing the maintenance to ensure oil doesn’t leak over the pan rail.

(4) Use a clean container to catch the oil removed from the pan.

(5) Before restarting the test, return the oil to the engine after the maintenance is completed.

9.7 Blowby Flow Rate Adjustment—A blowby adjustment can only be done within the first 24 h of the test.

(1) Blowby measurement taken during the first test Stage 2 after break in (3.25 h to 3.45 h) provides a good indication how the blowby will perform for the rest of the test.

(2) If that blowby value is less than 70 L/min, a blowby adjustment should be made to achieve at least 70 L/min flow.

(3) Adjust the blowby by changing the ring gaps or replacing piston rings, if necessary.

(4) Ring gaps shown in Table 11 typically produce the above blowby levels. However, these can be adjusted as necessary to achieve the correct blowby level.

(5) Use the ring cutting procedure outlined in 8.18.2

(6) Stage 2 blowby for the test during the first 120 h of the test must fall within the range from 65 L/min to 75 L/min as listed in Table 10. The Stage 2 times are also listed in Table 10.

# TABLE 10, 2nd Stage Blowby Readings

| Stage 2 Blowby Readings |  |  |
| --- | --- | --- |
| Test Hours | Blowby Reading | Use these boxes for AVG. |
| 3.5-3.75 |  |  |
| 23.5-23.75 |  | 70 L/min Recommended |
| 47.5-47.75 |  |  |
| 71.5-71.75 |  |  |
| 95.5-95.75 |  |  |
| 119.5-119.75 |  |  |
| 143.5-143.75 |  | 23.5 h to 119.75 h Blowby average must be between 65 L/min to 75 L/min. |
| 167.5-167.75 |  |  |
| 191.5-191.75 |  |  |
| 215.5-215.75 |  |  |
| Test Average |  |  |

# TABLE 11, Suggested Piston Ring Gaps

| Top piston ring gap | 1.651 mm (0.065 in.) |
| --- | --- |
| 2nd piston ring gap | 1.778 mm (0.070 in.) |

9.7.1 High Blowby Flow Rate Adjustment—Reduce high blowby flow rate by replacing the compression rings with new rings that have smaller ring gaps.

9.7.2 Low Blowby Flow Rate Adjustment—Increase low blowby flow rate by increasing the ring gaps of the compression rings.

9.7.3 Engine Disassembly and Reassembly for Maintenance (Before End of Test):

9.7.3.1Engine assembly and disassembly shall adhere to the procedures in 8.9 and 9.7.4.2, respectively

(1) When the engine is disassembled for maintenance, drain as much test oil as possible from the oil pan into a clean container, and retain that oil for installation in the engine after reassembly.

(2) Take precautions to ensure the oil is not contaminated and to ensure that deposits are not disturbed on any parts.

(3) All parts should be placed in or over clean drain pans to collect oil that drains off while maintenance is being performed.

(4) The timing chain should be placed in a separate container to prevent it from getting contaminated.

9.7.3.2 During reassembly, used drained test oil may be utilized to lubricate the engine parts.

(1) Do not use EF-411 oil or new test oil during engine reassembly.

(2) After the engine has been reassembled, reinstall the used test oil removed from the oil pan and collected from the engine parts during disassembly and maintenance.

(2a) Do not add any new test oil to the pan.

10.  Diagnostic Data Review

10.1 This sub-section outlines significant characteristics of specific engine operating parameters. The following PCM parameters can directly influence the test or can be used to indicate normalcy of other parameters.

10.1.1 Engine Torque

(1) Engine torque is controlled in Stage 1 and 2 . It should remain relatively constant throughout a test and from test-to-test.

(2) Large differences in torque reading could be indicative of control or engine problems.

10.1.2 Fuel Consumption Rate

(1) The fuel consumption rate should remain relatively constant throughout the test. Fuel consumption rate is not a specifically controlled parameter but is used as a diagnostics tool.

10.1.3 Exhaust Gas Component Levels

(1) Use the Lambda levels in the exhaust gas to determine the characteristics of combustion that occur during    the test.

(2) Use this parameter to determine the normalcy of combustion and any significant changes in combustion that occur throughout a particular test.

(3) Lambda in all two stages is controlled by the program in the Powertrain Control Module. No adjustments can be made to change the exhaust gas Lambda.

(3a) If Lambda differs from what appears in Table 4, check the PCM and test cell control system. Correcting a fault in the PCM and test cell control system is the only way to achieve the correct Lambda value.

10.1.4 Crankcase Pressure

(1) Crankcase pressure is a function of blowby flow rate and PCV valve flow.

(2) High crankcase pressure is usually caused by high blowby flow rate or a significant loss of PCV valve flow. (3) Incorrect three-way valve plumbing or port plugging also promotes high crankcase pressure.

(4) Low or negative crankcase pressure might be caused by low blowby flow rate or a restriction of vent air to the PCV valve.

10.1.5 Oil Pressure

(1) The oil pressure is a function of oil viscosity and operating temperature. The oil pressure should remain consistent throughout the test, unless the oil exhibits a significant change in viscosity.

10.1.6 Oil Temperature Differential

(1) The oil temperature differential is primarily a function of oil flow rate and oil viscosity and is normally stable throughout the test.

(2) The differential can change if the oil viscosity changes significantly during the test.

10.1.7 Coolant Temperature Differential—The coolant temperature differential is primarily a function of the coolant flow rate and is normally stable throughout the test.

(1) Large variations in the differential can be caused by coolant flow rate or temperature measurement errors.

10.2  End of Test Procedures

10.2.1 Final Drain

(1) Drain the engine coolant after the completion of the last test cycle.

(2) Engine oil can be drained with the engine in or out of the engine stand.

10.2.2  Engine Disassembly

(1) During disassembly, ensure the original location of the parts can be identified with respect to either the cylinder number, valve location, bearings, etc.

10.2.3  Parts Layout for Measurement

(1) Lightly wipe down the timing chain of any excess oil and make sure to keep the chain free of any contaminants or debris.

(2) Prepare the timing chain for end of test measurement as listed in the Timing Chain Measurement and Cleaning Procedure.

11. Test Results

11.1 Primary test result

11.1.1 Calculate and record the change in timing chain length from Hour 0 to the end of test:

Chain elongation = 2 x (final average measurement-initial average measurement)/nominal chain length. The nominal chain length is 1095.375 mm (43.125 in.)

11.2 Used oil analyses

11.2.1

12. Report

12.1  For reference oil results, use the standardized report form set available from the ASTM TMC and

data dictionary for reporting test results and for summarizing operational data.

Note 10—Report the non-reference oil test results on these same forms if the results are intended to be submitted as candidate oil results against a specification.

12.1.1  Fill out the report forms according to the formats shown in the data dictionary.

12.1.2  Transmit results to the TMC within 5 working days of test completion.

12.1.3  Transmit the results electronically as described in the ASTM Data Communications Committee Test Report Transmission Model (Section 2 — Flat File Transmission Format) available from the ASTM TMC. Upload files via the TMC’s website.

12.2  Report all reference oil test results, whether aborted, invalidated, or successfully completed, to the TMC.

12.3  Deviations from Test Operational Limits—Report all deviations from specified test operational limits.

12.4  Precision of Reported Units—Use the Practice E29 rounding-off method for critical pass/fail test result data.

(1) Report the data to the same precision as indicated in data dictionary.

12.5  In the space provided, note the time, date, test hour, and duration of any shutdown or off-test condition.

(1) Document the outcome of all prior reference oil tests from the current calibration sequence that were operationally or statistically invalid.

12.6  If a calibration period is extended beyond the normal calibration period length, make a note in the comment section and attach a written confirmation of the granted extension from the TMC to the test report.

(1) List the outcomes of previous runs that may need to be considered as part of the extension in the comment section.

13.  Precision and Bias

13.1  Test Precision—Reference Oils:

13.1.1  Intermediate Precision Conditions—Conditions where test results are obtained with the same test method using the same test oil, with changing conditions such as operators, measuring equipment, test stands, test engines, and time.

Note 11—“Intermediate precision” is the appropriate term for this test method rather than “repeatability,” which defines more rigorous within-laboratory conditions.

13.1.1.1  Intermediate Precision Limit (i.p.)—The difference between two results obtained under intermediate precision conditions that would, in the long run, in the normal and correct conduct of the test method, exceed the values shown in Table 8 in only one case in twenty.

Table 8  Test PrecisionA

|  | Intermediate Precision |  | Reproducibility |  |
| --- | --- | --- | --- | --- |
| Test Result | Si.p. | i.p.B | SR | RB |

Change in timing chain length (mm)

_______________________________________________________

A These statistics are based on results obtained on Test Monitoring Center Reference Oils over the period from             through

B This value is obtained by multiplying the standard deviation by 2.8.

13.1.2  Reproducibility Conditions—Conditions where test results are obtained with the same test method using the same test oil in different laboratories with different operators using different equipment.

13.1.2.1  Reproducibility Limit (R)—The difference between two results obtained under reproducibility conditions that would, in the long run, in the normal and correct conduct of the test method, exceed the values in Table 8 in only one case in twenty.

13.2  Bias—Bias will be determined by applying an accepted statistical technique to reference oil test results, and when a significant bias is determined, a severity adjustment will be permitted for non-reference oil test results.

14. Keywords

14.1 timing chain; engine oil; turbocharger, ramp, blowby

ANNEXES

(Mandatory Information)

A1.  ASTM TEST MONITORING CENTER ORGANIZATION

A1.1  Nature and Functions of the ASTM Test Monitoring Center (TMC)—The TMC is a non-profit organization located in Pittsburgh, Pennsylvania and is staffed to: administer engineering studies; conduct laboratory inspections; perform statistical analyses of reference oil test data; blend, store, and ship reference oils; and provide the associated administrative functions to maintain the referencing calibration program for various lubricant tests as directed by ASTM Subcommittee D02.B0 and the ASTM Executive Committee. The TMC coordinates its activities with the test sponsors, the test developers, the surveillance panels, and the testing laboratories. Contact TMC through the TMC Director at:

ASTM Test Monitoring Center

6555 Penn Avenue

Pittsburgh, PA 15206-4489

www.astmtmc.cmu.edu

A1.2  Rules of Operation of the ASTM TMC—The TMC operates in accordance with the ASTM Charter, the ASTM Bylaws, the Regulations Governing ASTM Technical Committees, the Bylaws Governing ASTM Committee D02, and the Rules and Regulations Governing the ASTM Test Monitoring System.

A1.3  Management of the ASTM TMC—The management of the Test Monitoring System is vested in the Executive Committee elected by Subcommittee D02.B0. The Executive Committee selects the TMC Director who is responsible for directing the activities of the TMC.

A1.4  Operating Income of the ASTM TMC—The TMC operating income is obtained from fees levied on the reference oils supplied and on the calibration tests conducted. Fee schedules are established by the Executive Committee and reviewed by Subcommittee D02.B0.

A2. ASTM TEST MONITORING CENTER: CALIBRATION PROCEDURES

A2.1  Reference Oils—These oils are formulated or selected to represent specific chemical, or performance levels, or both. They are usually supplied directly to a testing laboratory under code numbers to ensure that the laboratory is not influenced by prior knowledge of acceptable results in assessing test results. The TMC determines the specific reference oil the laboratory shall test.

A2.1.1  Reference Oil Data Reporting – Test laboratories that receive reference oils for stand calibration shall submit data to the TMC on every sample of reference oil they receive.  If a shipment contains any missing or damaged samples, the laboratory shall notify the TMC immediately.

A2.2  Calibration Testing:

A2.2.1  Full-scale calibration testing shall be conducted at regular intervals. These full-scale tests are conducted using coded reference oils supplied by the TMC. It is a laboratory's responsibility to keep the on-site reference oil inventory at or above the minimum level specified by the TMC test engineers.

A2.2.2  Test Stands Used for Non-Standard Tests—If a non-standard test is conducted on a previously calibrated test stand, the laboratory shall conduct a reference oil test on that stand to demonstrate that it continues to be calibrated, prior to running standard tests.

A2.3  Reference Oil Storage—Store reference oils under cover in locations where the ambient temperature is between -10 °C and +50 °C.

A2.4  Analysis of Reference Oil—Unless specifically authorized by the TMC, do not analyze TMC reference oils, either physically or chemically. Do not resell ASTM reference oils or supply them to other laboratories without the approval of the TMC. The reference oils are supplied only for the intended purpose of obtaining calibration under the ASTM Test Monitoring System. Any unauthorized use is strictly forbidden. The testing laboratory tacitly agrees to use the TMC reference oils exclusively in accordance with the TMC’s published Policies for Use and Analysis of ASTM Reference Oils, and to run and report the reference oil test results according to TMC guidelines. Additional policies for the use and analysis of ASTM Reference Oils are available from the TMC.

A2.5  Conducting a Reference Oil Test—When laboratory personnel are ready to run a reference calibration test, they shall request an oil code via the TMC website.

A2.6  Reporting Reference Oil Test Results—Upon completion of the reference oil test, the test laboratory transmits the data electronically to the TMC, as described in Section ?. The TMC reviews the data and contacts the laboratory engineer to report the laboratory's calibration status. All reference oil test results, whether aborted, invalidated, or successfully completed, shall be reported to the TMC.

A2.6.1 All deviations from the specified test method shall be reported.

A3. ASTM TEST MONITORING CENTER: MAINTENANCE ACTIVITIES

A3.1  Special Reference Oil Tests—To ensure continuous severity and precision monitoring, calibration tests are conducted periodically throughout the year. Occasionally, the majority or even all of the industry’s test stands will conduct calibration tests at roughly the same time. This could result in an unacceptably large time frame when very few calibration tests are conducted. The TMC can shorten or extend calibration periods as needed to provide a consistent flow of reference oil test data. Adjustments to calibration periods are made such that laboratories incur no net loss or gain in calibration status.

A3.2  Special Use of the Reference Oil Calibration System—The surveillance panel has the option to use the reference oil system to evaluate changes that have potential impact on test severity and precision. This option is only taken when a program of donated tests is not feasible. The surveillance panel and the TMC shall develop a detailed plan for the test program. This plan requires all reference oil tests in the program to be completed as close to the same time as possible, so that no laboratory/stand calibration status is left pending for an excessive length of time. In order to maintain the integrity of the reference oil monitoring system, each reference oil test is conducted so as to be interpretable for stand calibration. To facilitate the required test scheduling, the surveillance panel may direct the TMC to lengthen and shorten reference oil calibration periods within laboratories such that the laboratories incur no net loss or gain in calibration status. To ensure accurate stand, or laboratory, or both severity assessments, conduct non-reference oil tests the same as reference oil tests.

A3.3  Donated Reference Oil Test Programs—The surveillance panel is charged with maintaining effective reference oil test severity and precision monitoring. During times of new parts introductions, new or re-blended reference oil additions, and procedural revisions, it may be necessary to evaluate the possible effects on severity and precision levels. The surveillance panel may choose to conduct a program of donated reference oil tests in those laboratories participating in the monitoring system, in order to quantify the effect of a particular change on severity and precision. Typically, the surveillance panel requests its panel members to volunteer enough reference oil test results to create a robust data set. Broad laboratory participation is needed to provide a representative sampling of the industry. To ensure the quality of the data obtained, donated tests are conducted on calibrated test stands. The surveillance panel shall arrange an appropriate number of donated tests and ensure completion of the test program in a timely manner.

A3.4  Intervals Between Reference Oil Tests—Under special circumstances, such as extended downtime caused by industry-wide parts or fuel shortages, the TMC may extend the intervals between reference oil tests.

A3.5  Introducing New Reference Oils—Reference oils produce various results. When new reference oils are selected, participating laboratories will be requested to conduct their share of tests to enable the TMC to recommend industry test targets. ASTM surveillance panels require a minimum number of tests to establish the industry test targets for new reference oils.

A3.6  TMC Information Letters—Occasionally it is necessary to revise the test method, and notify the test laboratories of the change, prior to consideration of the revision by Subcommittee D02.B0. In such a case, the TMC issues an Information Letter. Information Letters are balloted semi-annually by Subcommittee D02.B0, and subsequently by D02. By this means, the Society due process procedures are applied to these Information Letters.

A3.6.1   Issuing Authority—The authority to issue an Information Letter differs according to its nature. In the case of an Information Letter concerning a part number change which does not affect test results, the TMC is authorized to issue such a letter. Long-term studies by the surveillance panel to improve the test procedure through improved operation and hardware control may result in the issuance of an Information Letter. If obvious procedural items affecting test results need immediate attention, the test sponsor and the TMC issue an Information Letter and present the background and data supporting that action to the surveillance panel for approval prior to the semiannual Subcommittee D02.B0 meeting.

A3.7  TMC Memoranda—In addition to the Information Letters, supplementary memoranda are issued. These are developed by the TMC and distributed to the appropriate surveillance panel and participating laboratories. They convey such information as batch approvals for test parts or materials, clarification of the test procedure, notes and suggestions of the collection and analysis of special data that the TMC may request, or for any other pertinent matters having no direct effect on the test performance, results, or precision and bias.

A4. ASTM TEST MONITORING CENTER: RELATED INFORMATION

A4.1  New Laboratories—Laboratories wishing to become part of the ASTM Test Monitoring System will be requested to conduct reference oil tests to ensure that the laboratory is using the proper testing techniques. Information concerning fees, laboratory inspection, reagents, testing practices, appropriate committee membership, and rater training can be obtained by contacting the TMC Director.

A4.2  Information Letters: COTCO Approval—Authority for the issuance of Information Letters was given by the committee on Technical Committee Operations in 1984, as follows: “COTCO recognizes that D02 has a unique and complex situation. The use of Information Letters is approved providing each letter contains a disclaimer to the affect that such has not obtained ASTM consensus. These Information Letters should be moved to such consensus as rapidly as possible.”

A4.3  Precision Data—The TMC determines the precision of test methods by analyzing results of calibration tests conducted on reference oils. Precision data are updated regularly. Current precision data can be obtained from the TMC.

A5. ENGINE AND STAND PARTS

A5.1 Tables A5.1 – A5.6 list the engine and stand part numbers

Table A5.1 Assembled Test Engine

| ENGINE ASSEMBLY |  |  |
| --- | --- | --- |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| BB5Z-6006-A | BB5E-6006-AD | 2.0L ENGINE ASY LB |
|  | Table A5.2 Reusable Engine Parts |  |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| 1S7Z6507B | 1S7G6507D7G | VALVE - INLET |
| 1S7Z6514AA | 1S7G6514AE | RETAINER - VALVE SPRING |
| 1S7Z6518AA | 1S7G6518AD | KEY, VALVE SPRG |
| 1S7Z8501A | 1S7G8501BD | PUMP ASY - WATER |
| 8W9Z6C287A | AG9E6C287AA | TAPPET ASY, FU PMP |
| AG9Z6010B | AG9E6010A34B | CYLINDER BLOCK |
| AG9Z6135B | AG9E6135AA | PIN - PISTON |
| AG9Z6140A | AG9G6140BA | RETAINER - PISTON PIN |
| AG9Z6200D | AG9E6200CD | ROD - CONNECTING |
| AG9Z6250A | AG9E6A268AB | CAMSHAFT, LH (EXHAUST) |
| AG9Z6303A | BB5E6300A33A | CRANKSHAFT ASY |
| AG9Z6505A | AG9E6505AA | VALVE - EXHAUST |
| AG9Z6600B | AG9E6600AB | PUMP ASY - OIL |
| AG9Z6A785A | AG9G6A785CA | SEPARATOR ASY - OIL |
| AG9Z9350B | AG9E9D376AB | PUMP ASY - FUEL |
| AG9Z9P847A | AG9G9P847AA | BRACKET, FU INJ CLIP |
| BB5Z2A451C | BB5E2A451BD | PUMP ASY - VACUUM |
| BB5Z6019C | BB5E6019AF | COVER - CYLINDER FRONT |
| BB5Z6250A | BB5E6A267AB | CAMSHAFT, RH (INTAKE) |
| BB5Z6881A | BB5E6881AD | ADPT OIL FILTER |
| BB5Z6K269A | DB5E6K269AA | COUPLING - PUMP DRIVE |
| BB5Z9F593B | BB5E9F593BA | INJECTOR ASY |
| CJ5Z6049C | CJ5E6C032AC | CYLINDER HEAD ASY |
| CJ5Z6513A | CJ5E6513AA | SPRING - VALVE |
| CJ5Z6582A | CJ5E6K271BG | COVER - CYLINDER HEAD |
| CJ5Z6K254A | CJ5E6C271AA | TENSIONER, OIL PUMP DRIVE |
| CJ5Z6M280A | CJ5E6B297AA | SOLENOID - ENGINE VARIABLE TIMING |
| CJ5Z9D280A | CJ5E9D280BF | MANIFOLD ASY - FUEL SUPPLY |
| CJ5Z9D440A | CJ5E9B374BC | COVER - FUEL PUMP |
| CM5Z6652A | CM5E6652AA | GEAR, OIL PUMP DRIVE |
| CM5Z6A895A | CM5E6A895AA | CHAIN ASY - OIL PUMP DRIVE |
| CYFS12Y2 | CB5E12405AA | SPARK PLUG |
| AG9Z-6108-H | AG9E-6110-AC2 | PISTON- STD |
|  | Table A5.3 Fasteners |  |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| F5TZ6A785A | F57E6A785AC | SEPARATOR ASY - OIL, EXT |
| W500033S437 | W500033S437 | BOLT - FLANGED HEX. |
| W500114S442 | W500114S442 | BOLT |
| W500212S437 | W500212S437 | SCREW |
| W500214S437 | W500214S437 | BOLT - HEX.HEAD |
| W500221S437 | W500221S437 | BOLT - HEX.HEAD |
| W500224S437 | W500224S437 | BOLT |
| W500300S437 | W500300S437 | BOLT |
| W500301S437 | W500301S437 | BOLT |
| W500310S437 | W500310S437 | BOLT - HEX.HEAD |
| W500313S437 | W500313S437 | BOLT |
| W500328S437 | W500328S437 | BOLT |
| W500414S442 | W500414S442 | BOLT |
| W503275S437 | W503275S437 | BOLT - HEX. HEAD - FLANGED |
| W505531S442 | W505531S442 | SCREW |
| W506976S442 | W506976S442 | SCREW |
| W520214S440 | W520214S440 | NUT |
| W700115S437 | W700115S437 | SCREW AND WASHER ASY |
| W701183S300 | W701183S300 | DOWEL - BUSH |
| W701219S437 | W701219S437 | BOLT |
| W702426S303 | W702426S303 | BOLT - HEX.HEAD |
| W702492S437 | W702492S437 | STUD |
| W702700S437 | W702700S437 | STUD |
| W703383S437 | W703383S437 | BOLT |
| W703643S430 | W703643S430 | BOLT |
| W703649S300 | W703649S300 | PIN |
| W704474S437 | W704474S437 | STUD |
| W706282S430 | W706282S430 | BOLT |
| W706284S437 | W706284S437 | BOLT |
| W706487S437 | W706487S437 | BOLT-OIL COOLER FILTER |
| W711261S437 | W711261S437 | BOLT |
| W711574S439 | W711574S439 | STUD |
| W712022S430A | W712022S430 | BOLT - HEX.HEAD |
| W713095S403 | W713095S403 | NUT |
| W715323S300 | W715323S300 | WASHER - COPPER, T/C OIL LINE |
| W715638S443 | W715638S443 | STUD |
| W715848S437 | W715848S437 | BOLT |
| W716137S437 | W716137S437 | BOLT |
| W716735S437 | W716735S437 | BOLT |
| W716841S900 | W716841S900 | PIN, BELL HOUSING |
| 1L5Z6379AA | W706161S300 | BOLT |
| 1S7Z6A340AA | 1S7G6K340BC | BOLT, CRK SHFT PULLEY |
| 1S7Z6K282AA | 1S7G6K282AB | BOLT, CHAIN TEN |
| AG9Z6065A | AG9G6065BA | BOLT - HEX.HEAD, CYL HEAD |
| AG9Z6345A | AG9G6345AC | BOLT - BEARING CAP - HEX. HEAD |
| BB5Z6214A | BB5E6214CA | BOLT - CONNECTING ROD |
| CV6Z6279A | CV6E6279AA | BOLT, CAMSHAFT |
|  | Table A5.4 Test Parts List |  |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| 1S7Z6378AA | 1S7G6378AB | WASHER,CRK DIAMOND CRUSH |
| AG9Z-6148-A | AG9E-6148-AA | KIT-PISTON RING |
| 6M8Z6278A | 6M8G6278AA | WASHER, CAM, DIAMOND CRUSH |
| 7T4Z9601A | 7T439601AA | ELEMENT ASY - AIR CLEANER |
| CJ5Z6256B | CJ5E6C524AD | SPROCKET - CAMSHAFT, LH |
| CJ5Z6268A | CJ5E6268AA | BELT/CHAIN - TIMING |
| CJ5Z6306A | CJ5E6306AB | GEAR - CRANKSHAFT |
| CJ5Z6C525A | CJ5E6C525AD | SPROCKET - CAMSHAFT, RH |
| CJ5Z6K254B | CJ5E6K254AA | TENSIONER - TIMING CHAIN |
| CJ5Z6K255A | CJ5E6K255AB | ARM - TIMING CHAIN TENSIONER |
| CJ5Z6K297A | CJ5E6K297AB | GUIDE, TIMING CHAIN |
|  | Table A5.5 Gaskets List |  |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| CJ5Z6079D | CJ5E6079AC | KIT - GASKET |
| 1S7Z6571EA | 1S7G6A517BG | SEAL - VALVE STEM EX |
| 1S7Z6840AA | 1S7G6A636AD | GASKET, OIL FILTER ADPT |
| 1S7Z6B752AA | 1S7G6B752AC | GASKET, OIL SEP |
| 1S7Z6K301BA | 1S7G6A321AA | SEAL - CRANKSHAFT REAR OIL |
| 1S7Z8507AE | 1S7G8507AF | GASKET - WATER PUMP |
| 3M4Z6625AA | 3M4G6625AA | GASKET, OIL PMP P/U TUBE |
| 3M4Z8255A | 3M4G8K530AB | GASKET, T/STAT HSG |
| 3S4Z6571AA | 3S4G6A517AA | SEAL - VALVE STEM INT |
| 9L8Z9E936A | 9L8E9E936AA | GASKET, T/B |
| AA5Z9E583A | AA5E9E583AA | SEAL, FU PUMP |
| AG9Z9P431A | AG9G9P431AA | GASKET, T/C COOL LINE |
| BB5Z2A572B | BB5E2D224BB | GASKET - VACUUM PUMP |
| BB5Z6584A | BB5E6K260AB | GASKET, CAM COVER |
| BB5Z6L612A | BB536L612AA | GASKET, EXHAUST |
| BG9Z9229A | BG9E9U509AB | KIT - "O" RING, FU INJ |
| BR3Z6C535B | BR3E6P251BA | SEAL - VALVE VCT |
| CB5Z9276A | CJ5E9A420BA | GASKET, FU PUMP CVR |
| CJ5Z6051A | CJ5E6051EC | GASKET - CYLINDER HEAD |
| CJ5Z6N652A | CJ5E6N652AA | GASKET, T/C OIL DRAIN LINE |
| CJ5Z8255A | CJ5E8255AA | SEAL - THERMOSTAT |
| CJ5Z9439A | CJ5E9439AA | GASKET - INTAKE MANIFOLD |
| CJ5Z9448A | CJ5E9448BA | GASKET, EX MANIFOLD |
| CM5Z6700A | CM5E6700AB | SEAL ASY - CRKSHAFT OIL - FRT |
| Table A5.6 Test Stand Set Up Parts List |  |  |
| Current Ford Service Part Number | Current Ford Engineering Part Number | Description |
| AG9Z9D930B | AG9T9H589BE | WIRE ASY, FE INJ |
| 1S7Z12A699BB | 1S7A12A699BB | SENSOR - ENGINE KNOCK |
| 6M8Z6C315AA | 6M8G6C315AB | SENSOR - CRANKSHAFT POSITION - CPS |
| 8F9Z9F472A | 8F9A9Y460AB | SENSOR ASY, MAF |
| 8V2Z12B579A | 8V2112B579AA | SENSOR ASY |
| 9L8Z6G004E | 9L8A6G004BC | SENSOR ASY, CYL HD TMP |
| AA5Z9A600B | AA539A600AD | CLEANER ASY - AIR |
| AE5Z6A228A | AE5Q6A228AA | PULLEY ASY - TENSION BELT |
| AE5Z8620A | AE5Q6C301AA | V-BELT |
| AG9Z6K679A | AG9G6K679BC | PIPE - OIL FEED, T/C |
| AG9Z6K868A | CJ5E6K868AA | VALVE ASY, ENG PST OIL COOL |
| AG9Z6L092A | AG9G6K677BC | HOSE - T/C OIL DRAIN |
| AG9Z8555A | AG9G8A506BB | HOSE - WATER INLET, T/C |
| AG9Z9F479A | AG919F479AB | SENSOR ASY, MAP |
| AS7Z6B288A | AS7112K073AA | SENSOR - CAMSHAFT POSITION |
| BB3Z6A642A | BB3E6A810AA | KIT ENGINE OIL COOLER |
| BB5Z11002C | BB5T11000AA | STARTER MOTOR ASY |
| BB5Z5A231A | BB535A281AA | CLAMP - HOSE, T/C TO EXH |
| BB5Z6C640A | BB536K863CE | CONNECTION - AIR INLET T/B END |
| BB5Z6C640B | BB536K863DF | CONNECTION - AIR INLET, I/C END |
| BB5Z6C646C | BB536C646CD | DUCT - AIR, TURBO END |
| BB5Z6C646D | BB536C646DF | DUCT - AIR, INTERCOOLER END |
| BB5Z6C683A | BB5E6L663AA | FILTER ASY (T/C SCREEN) |
| BB5Z9647A | BB539647AB | BRACKET, AIRBOX |
| BB5Z9661A | BB539643AA | COVER, AIRBOX |
| BB5Z9B659B | BB539F805DE | HOSE - AIR, TURBO END |
| BB5Z9B659E | BB539F805CG | HOSE - AIR, AIR BOX END |
| BM5Z9F972A | BM5G9F972BA | SENSOR - FUEL INJECTOR PRESSURE |
| BR2Z9E499A | BR2E9E499AA | CONNECTOR, VAC CONTRL, T/C |
| CB5Z6K682F | CB5E6K682BF | TURBO CHARGER |
| CB5Z8592A | CB5E8592AB | CONNECTION - WATER OUT, T/C |
| CB5Z8K153B | CB5E8B535AC | TUBE - WATER OUTLET |
| CB5Z9424D | CB5E9424AF | MANIFOLD ASY - INTAKE |
| CB5Z9S468C | CB5E9S468AF | HOSE, EMS (VAC HARNESS) |
| CJ5Z9J323B | CJ5E9J323BC | TUBE ASY FE PMP TO FE MAN |
| CM5Z12029A | CM5E12A366CA | COIL ASY - IGNITION |
| CP9Z9E926A | CM5E9F991AD | THROTTLE BODY AND MOTOR ASY |
| D4ZZ7600A | D4ZA7120AB | SLEEVE, PILOT BEARING |
| DU5Z12A581U | DU5T12C508UE | WIRE ASY, ENGINE MAIN |
| YS4Z6766A | YS4G6766DA | CAP ASY - OIL FILLER |
| 5M6Z8509AE | 5M6Q8509AE | PULLEY - WATER PUMP |
| AG9Z6312B | AG9E6D334AA | PULLEY - CRANKSHAFT |
|  | Table A5.7 Special Parts List |  |
| OHT PART NUMBER | DESCRIPTION |  |
| OHTVH-002-1 | PAN, OIL MODIFIED, ASSY. (INCLUDING DIPSTICK AND PICK UP TUBE) |  |
| VH002-2 | TUBE, PICK UP |  |
| OHTVH-005-1 | HOUSING, FLYWHEEL |  |
| OHTVH-006-1 | FLYWHEEL, MODIFIED, 2.0L |  |
| VH006-8 | CLUTCH, ASSY. W/ PRESSURE PLATE |  |
| VH006-8-1 | CLUTCH |  |
| VH006-8-2 | PLATE, PRESSURE |  |
| OHTVH-007-1 | HARNESS, DYNO, 2.0L |  |
| OHTVH-008-1 | INLET, COOLANT |  |
| VH008-1 | CLIP, RETAINER, SENSOR, COOLANT INLET |  |
| VH008-2 | SEAL, COOLANT INLET |  |
| OHTVH-009-1 | OUTLET, COOLANT |  |
| VH009-6 | SEAL, COOLANT OUTLET |  |
| OHTVH-011-1 | SHIM, CLUTCH PRESSURE PLATE |  |
|  | CFM Balance Shaft Delete Kit |  |
|  | Table A5.8 - Service Tools |  |
| Camshaft alignment tool |  |  |
| Timing peg |  |  |
| Crankshaft position sensor alignment tool |  |  |

| CHAIN MEASUREMENT RIG PARTS (Table A5.9) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Description | Quantity | Manufacturer | Mfg PN | suggested Supplier | Supplier PN |
| PUSH PIN FOR END CAP | 6 | 80/20 | 3274 |  |  |
| PC DATA INPUT DEVICE | 1 | MITUTOYO | 264-012-10 | CLEVELAND SPECIALTY INSPECTION SERVICES, INC. | 264-012-10 |
| SPC CABLE | 1 | MITUTOYO | 905338 | CLEVELAND SPECIALTY INSPECTION SERVICES, INC. | 905338 |
| MITUTOYO ELECTRONIC DIAL INDICATOR | 1 | MITUTOYO | 543-792 | MSC | 60777216 |
| CLAMP | 1 | DESTACO | 609-B | MSC | 90968736 |
| BEARING, FOR GEARS | 2 | NICE | 3016DCTNTG18 | FASTENAL | 4194269 |
| PILLOW BLOCK BEARING, SPB12 | 4 | THOMPSON | SPB12 | GRAINGER | 2HXW8 |
| SHAFTS 24 IN | 2 | THOMPSON | QS 3/4 L 24 | GRAINGER | 5JW62 |
| T-NUT, SLIDE-IN, OFFSET, 80/20 3278 | 69 | 80/20 | 3278 |  |  |
| BRACKET, 4-HOLE, CORNER, 80/20, 4301 | 14 | 80/20 | 4301 |  |  |
| BRACKET, 2-HOLE, CORNER, 80/20, 4302 | 4 | 80/20 | 4302 |  |  |
| END CAP, 1515 LITE, 80/20, 2030 | 6 | 80/20 | 2030 |  |  |
| CRANKSHAFT GEAR, MODIFIED | 2 | FORD | CJ5Z-6306-A | MARSHALL FORD | CJ5Z-6306-A |
| NEODYMIUM DISC MAGNET, 1/4" DIAMETER, 1/4" THICK, 2.5 LBS. MAXIMUM PULL | 4 |  |  | MCMASTER | 58605K35 |
| NEODYMIUM DISC MAGNET, 3/8" DIAMETER, 1/8" THICK, 3 LBS. MAXIMUM PULL | 1 |  |  | MCMASTER | 5862K95 |
| MAGNETIC SWITCH | 2 |  |  | MCMASTER | 65985K14 |
| ROUND BUMPER, RUBBER, 1-1/2" DIAMETER, 5/16" DIAMETER HOLE, WITH WASHER | 4 |  |  | MCMASTER | 9540K756 |
| PARKER MPE SERIES 60 MM FRAME 2 STACK SERVO MOTOR WITH 2500 LINE ENCODER | 1 | PARKER | MPE0602A4E-KC1N | PARKER | MPE0602A4E-KC1N |
| PARKER ARIES 750 WATT SERVO DRIVE WITH CONTROLLER (REQUIRES PROGRAMMING) | 1 | PARKER | AR-08CE | PARKER | AR-08CE |
| PARKER MPE TO ARIES 25 FOOT POWER CABLE | 1 | PARKER | 71-030630-25 | PARKER | 71-030630-25 |
| PARKER MPE TO ARIES 25 FOOT FEEDBACK CABLE | 1 | PARKER | 71-030631-25 | PARKER | 71-030631-25 |
| 3.5MM AUDIO CABLE | 1 |  |  |  |  |

- A6. SAFETY PRECAUTIONS

- A6.1 The operating of engine tests can expose personnel and facilities to safety hazards. Personnel trained and experienced with engine testing should perform the design, installation, and operation of test stands.

- A6.2 Install guards (shields) around all external moving, hot, or cold components. Design the guard to contain the energy level of a rotating component should the component break free. Fuel, oil, coolant, and electrical wiring should be properly routed, guarded, grounded and kept in good order.

- A6.3 Keep the test stand free of oil and fuel spills and tripping hazards. Do not permit containers of oil or fuel, or both, to accumulate in the testing area. Fire fighting equipment should be immediately accessible. Observe normal precautions whenever using flammable solvents for cleaning purposes.

- A6.4 Safety masks, glasses, or hearing protection, or a combination thereof, should be worn by personnel working on the test stand. No loose or flowing clothing, including long hair or other accessory to dress, should be worn near rotating equipment. Caution personnel against working alongside the engine and driveline while the engine is running.

- A6.5 Interlocks should automatically shutdown the engine when an anomaly in any of the following occur: engine or dynamometer coolant temperature, engine oil pressure, dynamometer field current, engine speed, exhaust temperature, excessive vibration, or when the fire protection system is activated. The interlock should include a method to cut off the fuel supply to the engine at the injector pump (including the return line). A remote fuel cut off station (external to the test stand) is recommended.

- A6.6 Employ other safety precautions as required.

A7. ENGINE REBUILD TEMPLATES

A7.1 Piston ring setter

Fig. A7.1: Piston Ring Setter

Fig. A7.2: Cylinder Bore Ladder

A8. Engine Build Records

A8.1 Cylinder head build (Fig. A8.1.)

Figure A8.1: Cylinder Head Build Record

A8.2 Cylinder bore measurement (see Fig. A8.2)

Fig. A8.2: Cylinder Bore Measurement Record

A8.3 Bearing Journals Measurement (Fig. A8.3)

Figure A8.3: Bearing Journals Measurement Record

A9. Engine Part Photographs, Schematics, and Figures

Coolant out 					Coolant in

Coolant in and out connections and thermocouple locations

FIG. A9.1

Note 1—Observe temperature sensor locations in thermostat housing and at water pump inlet.

Note 2—Components of Engine Cooling System—

(1) Thermostat housing, coolant out with temperature sensor (OHTVH-009-1)

(2) Sight glass

(3) Flowmeter

(4) Flow control valve

(5) Optional temperature  sensor

(6) Fabricated coolant reservoir

(7) Constant full expansion tank

(8) Pressure radiator cap (MOTORCRAFT RS40 P/N D2YY-8100-A)

(9) Process water control valve (regulated by temperature controller with three remote set points)

(10) Heat exchanger (ITT Standard P/N 5-030-06-048-001 TYP.)

(11) Process water supply (shell side)

(12) Water pump inlet with temperature sensor (OHTVH-008-1)

(13) Turbocharger coolant return

(14) Engine coolant (tube side)

(15) Coolant system drain valve

(16) Coolant pressure regulator

(17) Coolant pressure gage

FIG. A9.2  Typical Engine Cooling System Schematic

Fig.A 9.3 Oil cooler showing temp measurement locations

Fig.A 9.3 Oil cooler showing temp measurement locations

| Legend |  |
| --- | --- |
| (1) | Vented reservoir cap |
| (2) | Coolant reservoir (fabricated) |
| (3) | Pressure control valve (optional) |
| (4) | Chilled process water control valve |
| (5) | System heat exchanger |
| (6) | F and P Co. flowrator tube, FF-1-35-G-10/448D053U06 |
| (7) | CCV Heat Exchanger |
| (8) | Inlet temperature sensor |
| (9) | Flow control valve |
| (10) | External heat source |
| (11) | Electric coolant pump DAYTON 6K581A |
| (12) | ABB Kent-Taylor flow element, 1330LZ08000-8375A |

FIG. A9.3 Typical CCV Heat Exchanger Heating and Cooling System

Figure A9.3 Motor mounts, front

Figure A9.4 Motor mounts, rear

Figure A9.5  Front Mount Bracket

Figure A9.6 Front Mount Bracket

Figure A9.8: Exhaust Measurements and Instrumentation

Figure A9.7

Vacuum System

FIG. A9.12 Typical air intake system

Figure A9.13: Intercooler Tubing Measurements and Instrumentation

Figure A9.14 Typical intercooler installation

Figure A9.15 Oil cooler showing oil gallery pressure location

Figure A9.16 Oil cooler showing oil temperature locations

Oil Out temperature location in oil filter adapter (Dimensions in mm)

Figure A2.16 Oil cooler showing oil temperature locations

Figure A9.17

Vacuum System

Typical Torque and temperature ramps

Figure A9.23

Typical Torque and temperature ramps

Figure A9.23 (cont)

Typical Torque and temperature ramps

Figure A9.23 (cont)

Typical Torque and temperature ramps

Figure A9.23 (cont)

A10.  CONTROL AND DATA ACQUISITION REQUIREMENTS

A10.1  General Description:

A10.1.1  The data acquisition system shall be capable of logging the operational data in digital format. It is to the advantage of the laboratory that the system be capable of real time plotting of controlled parameters to help assess test validity. The systems shall be capable of calculating real time quality index as this will be monitored throughout the test as designated in A2.5.

A10.1.2  Control capability is not dictated by this procedure. The control system shall be capable of keeping the controlled parameters within the limits specified in Table 4 (see 12.2.3 ) and maintain the quality index shown in A2.5.

A10.1.3  Design the control and data acquisition system to meet the requirements listed below. Use the recommendations laid out in the Instrumentation Task Force Report and Data Acquisition Task Force Report for any items not addressed in Annex A2.

A10.2  Digital Recording Frequency—The maximum allowable time period over which data can be accumulated is one second. This data can be filtered, as described in A2.6, and will be considered a reading.

A10.3  Steady State Operation:

A10.3.1  This portion of the test will be the entire time at Stage 1 and 2 conditions. Stage 1 and 2 conditions are reached by the end of the ramping periods. Calculate the quality index using values reported to the accuracy levels in Table A2.1.

TABLE A10.1 Accuracy Levels of Data Points to be Used in QI Calculations

| Parameter | Field Length |
| --- | --- |
| Speed |  |
| Humidity |  |
| Temperature |  |
| Torque |  |
| Intake Air Pressure |  |
| Exhaust Backpressure |  |
| Coolant Outlet Pressure |  |
| Coolant Flow |  |

TABLE A10.2 L and U Constants and Over and Under-Range Values

| Parameter | Stages | L | U | Over-Range | Under-Range |
| --- | --- | --- | --- | --- | --- |
| Coolflow | 1 |  |  |  |  |
| Cooloutt | 1 |  |  |  |  |
|  | 2 |  |  |  |  |
| Exhbprs | 1 |  |  |  |  |
|  | 2 |  |  |  |  |
| Humidity | 1, 2 |  |  |  |  |
| Intairpr | 1, 2 |  |  |  |  |
| Intairt | 1, 2 |  |  |  |  |
| Oilint | 1 |  |  |  |  |
|  | 2 |  |  |  |  |
| Speed | 1 |  |  |  |  |
|  | 3 |  |  |  |  |
| Torque | 1 |  |  |  |  |
|  | 2 |  |  |  |  |
| Cooloutp | 1, 2 |  |  |  |  |
| BBint | 1 |  |  |  |  |
|  | 2 |  |  |  |  |

TABLE A10.3 Maximum Allowable Time Constants

| Control Parameter | Time Constant, s |
| --- | --- |
| Engine speed, r/min | 0.5 |
| Torque, Nm | 0.7 |
| Engine oil in, °C | 0.6 |
| Engine coolant out, °C | 0.6 |
| Engine coolant flow, L/min | 8.0 |
| Blowby in, °C | 0.6 |
| Intake, air, °C | 0.6 |
| Intake air press, kPa | 0.2 |
| Exhaust back pressure, kPa | 0.2 |
| Engine coolant pressure | 2.0 |

A10.3.2  The time intervals between recorded readings shall not exceed 1 min. Data shall be recorded throughout the length of each stage.

A10.4  Transitions :

A10.4.1  The ramp requirements are listed in 12.2.3.3, Table 5.

A10.4.2  During the transition, the time intervals between all recorded readings shall not exceed 2 seconds..

A10.5  Quality Index:

TBD

A10.6  Time Constants:

A10.6.1  Filtering can be applied to all control parameters. The amount of filtering applied shall not allow time constants to exceed the values listed in Table A2.3. This time constant shall pertain to the entire system, running from the sensor to the display and data acquisition.

A10.6.2  Maximum allowable system time constants for the controlled parameters are shown in Table A3.3

APPENDIXES

(Nonmandatory Information)

X1.  SOURCES OF MATERIALS AND INFORMATION

X1.1 For convenience, some sources for materials and information are listed below:

X1.2 Test Engine Parts -

Ford Component Sales, Ford Motor Co., 290 Town Center Dr, Dearborn, MI 48126

X1.3 ASTM Test Monitoring Center  -

ASTM Test Monitoring Center, 6555 Penn Ave., Pittsburgh, PA 15206-4489

X1.4 Test Sponsor -

Ford Motor Company, Diagnostic Service Center II, 1800 Fairlane Drive, , Room 410, Allen Park, MI 48101

X1.5 Aeroquip Hose and Fittings -

Aeroquip Corp., 1225 W. Main, Van Wert, OH 45891

X1.6 Fuel Information and Availability -:

Haltermann Products, 1201 S. Sheldon Rd., P.O. Box 249, Channelview, TX 79530-0429

X1.7 Intake-Air Humidity Instruments -

Alnor Dewpointer; also dewpoint meters by EG & G, Foxboro, Hy-Cal, General Eastern, Protimeter

X1.8  Heat Exchangers -

ITT Standard Heat Exchangers , Kinetics Engineering Corp., 2055 Silber Road, Suite 101, Houston, TX 77055

X1.9 Fuel Flow Measurement -

Mass fuel flowmeters, Micro Motion Corp., 7070 Winchester Circle, Boulder, CO 80301

X1.10  Parts Washer and Chemicals -

Better Engineering Manufacturing, 8361 Town Court Center, Baltimore, MD 21236-4964

X1.11 Crankcase and Intake Air Pressure Gages -

Dwyer Instrument Co., Junction of Indiana State Highway 212 and U.S. Highway 12, P.O. Box 373,

Michigan City, IN 46360

X1.12  Blowby Heat Exchanger Coolant -

Nacool 2000 Engine Cooling System Treatment , Nalco Chemical Co. Functional Chemicals Group, One Nalco Ctr.,

Naperville, IL 60566-1024

X1.13 Lubricants -

EF-411, local distributors of ExxonMobil products.

X1.14  Tygon Hose -

Cadillac Plastic Co. distributors, or The Norton Co., 12 East Avenue, Tallmadge, OH 44278

X1.15  Special Test Engine  Tools -

To facilitate assembly and disassembly of the engine

Owatonna Tool Co., 2013 4th St., NW Owatonna, MN 55060

X1.16 Ultrasonic Parts Cleaner –

Tierra Tech model MOT500NS ultrasonic parts cleaner, or similar

Tierra Tech, 12252 S. Casey Cove, Riverton Utah, 84065

X1.17: Tierra Tech Ultrasonic solutions 7 and B -

Tierra Tech, 12252 S. Casey Cove, Riverton Utah, 84065

X1.18: Flex Hone -

Model: GB33432, W.W.Grainger, Inc., several locations, website www.grainger.com

X.1.19: Pneumatic Honing Drill –

Westward 1/2 Reversible Air Drill, Model: 5ZL26G , W.W.Grainger, Inc., several locations, website www.grainger.com

X1.20: Penmul L460 –

Penetone Corp., P.O. Box 22006, Los Angeles, CA 90022

X1.21: Parts Cleaning Soap –

(NAT-50 or PDN-50), Better Engineering Manufacturing, 8361 Town Court, Baltimore, MD 21236.

X1.22: Sanford Piston Ring Grinder –

Sanford Mfg. Co., 300 Cox St., P.O. Box 318, Roselle, NJ 07203.

X1.23: 3/16  in. carbide ring cutting burr -

No. 74010020, M. A. Ford.

X1.24: Sunnen soft stone -

No. JHU-820 Sunnen, Inc., 7910 Manchester, St. Louis, MO 63143.

X1.25: Ford camshaft alignment tool –

(Ford P/N 303-1565), Ford or Lincoln dealer

X1.26: Crankshaft TDC timing peg –

(Ford P/N 303-507), Ford or Lincoln dealer

X1.27 Dynamometer –

Dyne Systems, Inc., W209 N17391 Industrial Drive, Jackson, WI 53037

Dyno One, Inc. 14671 N 250, W Edinburgh, IN 46124 <info@dyno-one.com>

X1.28  Various Materials—

Oil pan and baffles, oil screen, flywheel, clutch, pressure plate, spacer, bell-housing, dynamometer and engine wire harnesses

OH Technologies, 9300 Progress Pkwy., Mentor, OH 44060, and/or --- Test Engineering, Inc.,12758 Cimarron Path, Ste. 102, San Antonio, TX 78249-3417

X1.29  Oil separator  -

Moroso Part number 85487, American Muscle Summit Racing

X1.30 Type 5 or Type 52 intercooler

FrozenBoost.com

X1.31 Chain Measurement Apparatus,

MCMR 1000, Lubrizol Corp. 29400 Lakeland Blvd., Wickliffe, OH 44092, attn.: George Szappanos, <George.Szappanos@lubrizol.com>

X1.32 Powertrain Control Module

Ford Motor Company, 290 Town Center Dr, Dearborn, MI 48126, attn.: Ron Romano, <rromano@ford.com>

X1.33 Shell Zone Dex-Cool

Keller-Heartt Oil, 4411 S. Tripp Ave., Chicago, Ill. 60632

X1.34 Chemtool B-12

Berryman Products, Inc., 3800 E. Randol Mill Rd., Arlington, TX 76011

X2. Engine Brackets

Fig. X2.1 Right Engine Bracket

X2.2 Left Engine Bracket

Table 10

Typical Dipstick Oil Level to Charge Conversions

This test method is under the jurisdiction of ASTM Committee D02 on Petroleum Products, Liquid Fuels, and Lubricants   and is the direct responsibility of Subcommittee D02.B0.01 on Passenger Car Engine Oils.

ASTM Test Monitoring Center (TMC), 6555 Penn Ave., Pittsburgh, PA 15206–4489.

For referenced ASTM standards, visit the ASTM website, www.astm.org, or contact ASTM Customer Service at service@astm.org. For  Annual Book of ASTM Standards volume information, refer to the standard's Document Summary page on the ASTM website.

4 The engine is based on the Ford Motor Co. 2012 Explorer engine, and a completely assembled new test engine is available from Ford Component Sales, Ford Motor Co., 290 Town Center Dr., Dearborn, MI 48126.