| # REFERENCE OIL 148-1 (30 Tests) |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Current Targets |  | Updated Severity Adjusted Targets |  |
|  | Mean | S.D. | Mean | S.D. |
| Average Carbon Varnish | 1.59 | 0.47 | 1.44 | 0.28 |
| Average Sludge | 0.76 | 0.19 | 0.73 | 0.21 |
| Viscosity Increase | 3.61 | 0.15 | 3.70 | 0.07 |
| Pentane | -0.95 | 0.39 | -0.73 | 0.28 |
| Toluene | -1.36 | 0.49 | -1.12 | 0.49 |

| # REFERENCE OIL 151-2 (30 Tests) |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | Current Targets |  | Updated Severity Adjusted Targets |  |
|  | Mean | S.D. | Mean | S.D. |
| Average Carbon Varnish | 1.81 | 0.40 | 1.66 | 0.45 |
| Average Sludge | 0.54 | 0.23 | 0.47 | 0.13 |
| Viscosity Increase | 3.62 | 0.15 | 3.57 | 0.10 |
| Pentane | 0.75 | 0.37 | 0.69 | 0.17 |
| Toluene | 0.26 | 0.50 | 0.19 | 0.26 |